## Slide 1
Measurement of the Hydrodynamic Radius, Rh
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
Kirkwood, J. Polym. Sci. 12 1(1953).
http://theor.jinr.ru/~kuzemsky/kirkbio.html
Rg/Rh
1.5 Theta
1.6 Expanded
0.774 Sphere
0.92 Draining Sphere
A Harmonic Mean
(based on an average of transport rates, D = kT/(6phRh))
An Arithmetic Mean

## Slide 2
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
Kirkwood, J. Polym. Sci. 12 1(1953).
http://theor.jinr.ru/~kuzemsky/kirkbio.html
Rg/Rh
1.5 Theta
1.6 Expanded
0.774 Sphere
0.92 Draining Sphere
Measurement of the Hydrodynamic Radius, Rh

## Slide 3
Rg/RH Ratio
Burchard, Schmidt, Stockmayer, Macro. 13 1265 (1980) (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/RgbyRhRatioBurchardma60077a045.pdf)
1.5
1.73
0.77
1.73

## Slide 4
Poiseuille’s Law (Q = V/time)

## Slide 5
Intrinsic “viscosity” as a linear displacement law
At very small f

## Slide 6
Intrinsic “viscosity” as a linear displacement law

## Slide 7
Shear Flow (may or may not exist in a capillary/Couette geometry)
Intrinsic, specific & reduced “viscosity”
hs = h0 (1+f[h])

## Slide 8
Intrinsic, specific & reduced “viscosity”
Shear Flow (may or may not exist in a capillary/Couette geometry)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
We can approximate (1) as:
Martin Equation
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1
Relative Viscosity
Reduced Viscosity
Intrinsic Viscosity
Reminiscent
of a virial expansion.

## Slide 9
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
We can approximate (1) as:
Martin Equation
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1
Huggins Equation
Kraemer Equation
(exponential expansion)
Relative Viscosity
Reduced Viscosity
Reduced Viscosity
Intrinsic, specific & reduced “viscosity”

## Slide 10
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Concentration Effect
Reduced
Viscosity
Reduced
Viscosity
Intrinsic, specific & reduced “viscosity”

## Slide 11
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Concentration Effect, c*
Reduced
Viscosity
Intrinsic, specific & reduced “viscosity”

## Slide 12
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Solvent Quality
Reduced
Viscosity
Intrinsic, specific & reduced “viscosity”

## Slide 13
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Molecular Weight Effect
Huggins Equation
Reduced
Viscosity
Intrinsic, specific & reduced “viscosity”

## Slide 14
V

## Slide 15
This is the “Zimm Model”
Or
Non-draining model

## Slide 16
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Temperature Effect
Viscosity itself has a strong temperature dependence. But intrinsic viscosity depends on temperature as far as coil expansion changes with temperature (RH3).
Weaker and
Opposite Dependency

## Slide 17
Arrhenius Behavior
Williams-Landel-Ferry (WLF) Equation
=exp=> exp=> exp=> exp
3 constants Tr, Ha, Sa; WLF has 3 constants TV, C1, C2
If exp(x) =10y then y =x/(ln(10)) = x/2.30
TV = (C2 – Tr); Sa = 2.30 C1; Ha = 2.30C1Tr
If you choose Tr = Tg then C1 ~ 17.44 and C2 ~ 51.6
If you choose Tr = Tg + 43K then C1 ~ 8.86 and C2 ~ 101.6
It might be best to measure H and S and find the Vogel temperature experimentally

## Slide 18
Intrinsic “viscosity” for colloids (Simha, Case Western)
For a solid object with a surface, v is a constant in molecular weight, depending only on shape
For a symmetric object (sphere) v = 2.5 (Einstein)
For ellipsoids v is larger than for a sphere,
J = a/b
prolate
oblate
a, b, b :: a>b
a, a, b :: a<b
https://physicstoday.scitation.org/do/10.1063/pt.4.2224/full/

## Slide 19
Hydrodynamic volume for “bound” solvent
Partial Specific Volume
Bound Solvent (g solvent/g polymer)
Molar Volume of Solvent
Intrinsic “viscosity” for colloids (Simha, Case Western)

## Slide 20
Long cylinders (TMV, DNA, Nanotubes)
J=L/d
End Effect term ~ 2 ln 2 – 25/12 Yamakawa 1975
Intrinsic “viscosity” for colloids (Simha, Case Western)

## Slide 21
Shear Rate Dependence for Polymers
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Capillary Viscometer

## Slide 22
Branching and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 23
Tortuosity
Connectivity
How Complex Mass Fractal Structures Can be Decomposed
z
df
p
dmin
s
c
R/d
27
1.36
12
1.03
22
1.28
11.2

## Slide 24
Branching and Intrinsic Viscosity
RH ~ p1/dmin
z ~ pc
RH ~ zcdmin = zdf
At low z; dmin = 2, c = 1; df = dminc = 2 (linear chain)
At high z; dmin => 1, c => 2 or 3; df = dminc => 2 or 3
(highly branched chain or colloid)

## Slide 25
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1
Keep in mind stars are a special case!
Branching and Intrinsic Viscosity

## Slide 26
Branching and Intrinsic Viscosity
(RH,B/ RH,L)2 ~ z2(df,B - df,L)
At low z; dmin = 2, c = 1; df = dminc = 2 (linear chain)
At high z; dmin => 1, c => 2 or 3; df = dminc => 2 or 3
(highly branched chain or colloid)
This is still just looking at density! There is not topological information here which is critical to describe branching

## Slide 27
Polyelectrolytes and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Very High Concentration
Low Concentration
Initially rod structures, increasing concentration
Followed by charge screening
Finally uncharged chains

## Slide 28
Polyelectrolytes and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
hsp = (h-1)/ h0
= f [h]

## Slide 29
hsp = (h-1)/ h0
= f [h]

## Slide 30
Hydrodynamic Radius from Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HiemenzRajagopalanDLS.pdf

## Slide 31
Correlation Functions (Tadmor and Gogos pp. 381)

## Slide 32
Correlation Functions (Tadmor and Gogos pp. 381)

## Slide 33
Correlation Functions (Tadmor and Gogos pp. 381)
Gross Uniformity: Gaussian distribution of samples, First order
Scale of Segregation: Second order
Diffusion/Gradient
Non-reversible
Shear strain
Reversible
0 to 1
Scale of Segregation
Laminar Flow Before/After

## Slide 34
Correlation Functions (Tadmor and Gogos pp. 381)

## Slide 35
Correlation Functions
DLS deals with a time correlation function at a given “q” = 2p/d

## Slide 36
Paul Russo Lab
Dynamic Light Scattering
LSU
Georgia Tech

## Slide 37
Fick’s Laws
Brownian Motion

## Slide 38
Paul Russo Lab
Not normalized second order correlation function (capital G, normalized is small g)

## Slide 39
Paul Russo Lab

## Slide 40
Paul Russo Lab

## Slide 41
Paul Russo Lab

## Slide 42
Paul Russo Lab

## Slide 43
Consider motion of molecules or nanoparticles in solution
Particles move by Brownian Motion/Diffusion
The probability of finding a particle at a distance x from the starting point at t = 0 is a Gaussian Function that defines the diffusion Coefficient, D
A laser beam hitting the solution will display a fluctuating scattered intensity at “q” that varies with q since the particles or molecules move in and out of the beam
I(q,t)
This fluctuation is related to the diffusion of the particles
The Stokes-Einstein relationship states that D is related to RH,

## Slide 44
For static scattering p(r) is the binary spatial auto-correlation function
We can also consider correlations in time, binary temporal correlation function
g1(q,τ)
For dynamics we consider a single value of q or r and watch how the intensity changes with time
I(q,t)
We consider correlation between intensities separated by t
We need to subtract the constant intensity due to scattering at different size scales
and consider only the fluctuations at a given size scale, r or 2π/r = q
Video of Speckle Pattern (http://www.youtube.com/watch?v=ow6F5HJhZo0)

## Slide 45
Dynamic Light Scattering (http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf)
Qe = quantum efficiency
R = 2π/q
Es = amplitude of scattered wave
q or K squared since size scales with the square root of time

## Slide 46
Dynamic Light Scattering
a = RH = Hydrodynamic Radius
The radius of an equivalent sphere following Stokes’ Law

## Slide 47
Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
my DLS web page
Wiki
https://en.wikipedia.org/wiki/Dynamic_light_scattering
Wiki Einstein Stokes
http://webcache.googleusercontent.com/search?q=cache:yZDPRbqZ1BIJ:en.wikipedia.org/wiki/Einstein_relation_(kinetic_theory)+&cd=1&hl=en&ct=clnk&gl=us

## Slide 48
Traditional Rheology: Place a fluid in a shear field, measure torque/force and displacement
Microrheology: Observe the motion of a tracer. Two types, passive or active microrheology. DWS is passive.
Diffusing Wave Spectroscopy (DWS)

## Slide 49
Diffusing Wave Spectroscopy (DWS)

## Slide 50
Viscous Motion
Elastic Motion
Diffusing Wave Spectroscopy (DWS)

## Slide 51
Diffusing Wave Spectroscopy (DWS)
For back scatter:

## Slide 52
Diffusing Wave Spectroscopy (DWS)
For back scatter:

## Slide 53
Link rheology to micelle structure
Ron Larson/Mike Weaver
Average
Micellar Length
Mesh
Size
Micelle
radius
Beth Schubert, 2003
1
2
tr
G0
c
bending
modes
G”min
Rouse
modes
Entanglement
Length
persistence
length
terminal
relaxation
Structure inferred from rheology, using Standard Cates Model and newer developments (Larson group, others…)
DWS = blue lines

## Slide 54
Quasi-Elastic Neutron (and X-ray) Scattering
In the early days of DLS there were two approaches:
Laser light flickers creating a speckle pattern that can be analyzed in the time domain
The flickering is related to the diffusion coefficient through an exponential decay of the time correlation function
A more direct method is to take advantage of the Doppler effect. Train whistle appears to change pitch as the train passes since the speed of the train is close to 1/w for the sound
If we know the frequency of the sound, we can determine the speed of the train
Measuring the spectrum from a laser, and the broadening of this spectrum after interaction with particles the diffusion coefficient can be determined from an exponential decay in the frequency, peak broadening. This is called quasi-elastic light scattering and measures the same thing as DLS by a different method.
For Neutrons and X-rays the time involved is too fast for correlators, pico- to nanoseconds. But line broadening can be observed (though there are no X-ray or neutron lasers i.e., monochromatic and columnated).
https://neutrons.ornl.gov/sites/default/files/QENSlectureNXS2019.pdf

## Slide 55
Neutron and X-ray “Lasers”
For X-rays a synchrotron with an undulator insertion device can produce close to monochromatic and fairly coherent radiation. NSLS II Brookhaven National Laboratory near Stony Brook, Long Island NY (near NYC)

## Slide 56
Neutron and X-ray “Lasers”
For neutrons, a spallation source with a time-of-flight detection system or a reactor with a velocity selector can result in a reasonably coherent and monochromatic (spectral in time) beam. SNS at Oak Ridge National Laboratory, Tennessee (near Knoxville) and NCNR at NIST Gaithersburg MD (near Washington DC).

## Slide 67
Rg/RH Ratio
Rg reflects spatial distribution of structure
RH reflects dynamic response, drag coefficient in terms of an equivalent sphere
While both depend on “size” they have different dependencies on the details of structure
If the structure remains the same and only the amount or mass changes the ratio between these parameters remains constant. So the ratio describes, in someway, the structural connectivity, that is, how the structure is put together.
This can also be considered in the context of the “universal constant”
Lederer A et al. Angewandte Chemi 52 4659 (2013). (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/DresdenRgbyRh4659_ftp.pdf)

## Slide 68
Rg/RH Ratio
Lederer A et al. Angewandte Chemi 52 4659 (2013). (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/DresdenRgbyRh4659_ftp.pdf)

## Slide 69
Rg/RH Ratio
Burchard, Schmidt, Stockmayer, Macro. 13 1265 (1980) (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/RgbyRhRatioBurchardma60077a045.pdf)
1.5
1.73
0.77

## Slide 70
Rg/RH Ratio
Burchard, Schmidt, Stockmayer, Macro. 13 1265 (1980) (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/RgbyRhRatioBurchardma60077a045.pdf)

## Slide 71
Rg/RH Ratio
Wang X., Qiu X. , Wu C. Macro. 31 2972 (1998). (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/RgbyRhPNIPAAMma971873p.pdf)
1.5 = Random Coil
~0.56 = Globule
Globule to Coil => Smooth Transition
Coil to Globule => Intermediate State
Less than (3/5)1/2 = 0.77 (sphere)

## Slide 72
Rg/RH Ratio
Wang X., Qiu X. , Wu C. Macro. 31 2972 (1998). (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/RgbyRhPNIPAAMma971873p.pdf)
1.5 = Random Coil
~0.56 = Globule
Globule to Coil => Smooth Transition
Coil to Globule => Intermediate State
Less than (3/5)1/2 = 0.77 (sphere)

## Slide 73
Rg/RH Ratio
Zhou K., Lu Y. , Li J., Shen L., Zhang F., Xie Z., Wu C. Macro. 41 8927 (2008). (http://www.eng.uc.edu/~gbeaucag/Classes/Properties/RgbyRhCoiltoGlobulema8019128.pdf)
1.5 to 0.92 (> 0.77 for sphere)

## Slide 74
Rg/RH Ratio
This ratio has also been related to the shape of a colloidal particle

## Slide 77
Static Scattering for Fractal Scaling

## Slide 81
For qRg >> 1
df = 2

## Slide 82
Ornstein-Zernike Equation
Has the correct functionality at high q
Debye Scattering Function =>
So,

## Slide 83
Ornstein-Zernike Equation
Has the correct functionality at low q
Debye =>
The relatoinship between Rg and correlation length differs for the two regimes.

## Slide 85
How does a polymer chain respond to external perturbation?

## Slide 86
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End to End Distance R
By Comparison The Energy to stretch a Thermally Equilibrated Chain Can be Written
Force
Force
Assumptions:
-Gaussian Chain
-Thermally Equilibrated
-Small Perturbation of Structure (so it is still Gaussian after the deformation)

## Slide 87
Tensile Blob
For weak perturbations of the chain
Application of an external stress to the ends of a chain create a transition size where the coil goes from Gaussian to Linear called the Tensile Blob.
For Larger Perturbations of Structure
-At small scales, small lever arm, structure remains Gaussian
-At large scales, large lever arm, structure becomes linear
Perturbation of Structure leads to a structural transition at a size scale

## Slide 88
For sizes larger than the blob size the structure is linear, one conformational state so the conformational entropy is 0. For sizes smaller the blob has the minimum spring constant so the weakest link governs the mechanical properties and the chains are random below this size.

## Slide 89: Semi-Dilute Solution Chain Statistics

## Slide 90
In dilute solution the coil contains a concentration c* ~ 1/[η]
for good solvent conditions
At large sizes the coil acts as if it were in a concentrated solution (c>>>c*), df = 2. At small sizes the coil acts as if it were in a dilute solution, df = 5/3. There is a size scale, ξ, where this “scaling transition” occurs.
We have a primary structure of rod-like units, a secondary structure of expanded coil and a tertiary structure of Gaussian Chains.
What is the value of ξ?
ξ is related to the coil size R since it has a limiting value of R for c < c* and has a scaling relationship with the reduced concentration c/c*
There are no dependencies on n above c* so (3+4P)/5 = 0 and P = -3/4
For semi-dilute solution the coil contains a concentration c > c*

## Slide 91
Coil Size in terms of the concentration
This is called the “Concentration Blob”

## Slide 92
Three regimes of chain scaling in concentration.

## Slide 93
Thermal Blob
Chain expands from the theta condition to fully expanded gradually.
At small scales it is Gaussian, at large scales expanded (opposite of concentration blob).

## Slide 94
Thermal Blob

## Slide 95
Thermal Blob
Energy Depends on n, a chain with a mer unit of length 1 and n = 10000
could be re cast (renormalized) as a chain of unit length 100 and n = 100
The energy changes with n so depends on the definition of the base unit
Smaller chain segments have less entropy so phase separate first.
We expect the chain to become Gaussian on small scales first.
This is the opposite of the concentration blob.
Cooling an expanded coil leads to local chain structure collapsing to a Gaussian structure first.
As the temperature drops further the Gaussian blob becomes larger until the entire chain is
Gaussian at the theta temperature.

## Slide 96
Thermal Blob
Flory-Krigbaum Theory yields:
By equating these:

## Slide 98
Digitized from Farnoux

## Slide 100
Fractal Aggregates and Agglomerates

## Slide 101
Polymer Chains are Mass-Fractals
RRMS = n1/2 l
Mass ~ Size2
3-d object
Mass ~ Size3
2-d object
Mass ~ Size2
1-d object
Mass ~ Size1
df-object
Mass ~ Sizedf
This leads to odd properties:
density
For a 3-d object density doesn’t depend on size,
For a 2-d object density drops with Size
Larger polymers are less dense

## Slide 104
Tortuosity
Connectivity
How Complex Mass Fractal Structures
Can be Decomposed
z
df
p
dmin
s
c
R/d
27
1.36
12
1.03
22
1.28
11.2

## Slide 106
Disk
Random Coil
Extended β-sheet
(misfolded protein)
Unfolded Gaussian chain

## Slide 107
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates

## Slide 108
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
http://www.phys.ksu.edu/personal/sor/publications/2001/light.pdf
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.koboproductsinc.com/Downloads/PS-Measurement-Poster-V40.pdf

## Slide 109
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.koboproductsinc.com/Downloads/PS-Measurement-Poster-V40.pdf

## Slide 110
For static scattering p(r) is the binary spatial auto-correlation function
We can also consider correlations in time, binary temporal correlation function
g1(q,τ)
For dynamics we consider a single value of q or r and watch how the intensity changes with time
I(q,t)
We consider correlation between intensities separated by t
We need to subtract the constant intensity due to scattering at different size scales
and consider only the fluctuations at a given size scale, r or 2π/r = q

## Slide 111
Dynamic Light Scattering
a = RH = Hydrodynamic Radius

## Slide 112
Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
my DLS web page
Wiki
http://webcache.googleusercontent.com/search?q=cache:eY3xhiX117IJ:en.wikipedia.org/wiki/Dynamic_light_scattering+&cd=1&hl=en&ct=clnk&gl=us
Wiki Einstein Stokes
http://webcache.googleusercontent.com/search?q=cache:yZDPRbqZ1BIJ:en.wikipedia.org/wiki/Einstein_relation_(kinetic_theory)+&cd=1&hl=en&ct=clnk&gl=us

## Slide 113
Gas Adsorption
http://www.chem.ufl.edu/~itl/4411L_f00/ads/ads_1.html
A + S <=> AS
Adsorption
Desorption
Equilibrium
=

## Slide 114
Gas Adsorption
http://www.chem.ufl.edu/~itl/4411L_f00/ads/ads_1.html
Multilayer adsorption

## Slide 115
http://www.eng.uc.edu/~gbeaucag/Classes/Nanopowders/GasAdsorptionReviews/ReviewofGasAdsorptionGOodOne.pdf

## Slide 116
From gas adsorption obtain surface area by number of gas atoms times an area for the adsorbed gas atoms in a monolayer
Have a volume from the mass and density.
So you have S/V or V/S
Assume sphere S = 4πR2, V = 4/3 πR3
So dp = 6V/S
Sauter Mean Diameter dp = <R3>/<R2>

## Slide 117
Log-Normal Distribution
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Geometric standard deviation and geometric mean (median)
Mean
Gaussian is centered at the Mean and is symmetric. For values that are positive (size) we need an asymmetric distribution function that has only values for greater than 1. In random processes we have a minimum size with high probability and diminishing probability for larger values.
http://en.wikipedia.org/wiki/Log-normal_distribution

## Slide 118
Log-Normal Distribution
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Geometric standard deviation and geometric mean (median)
Mean
Static Scattering Determination of Log Normal Parameters

## Slide 119
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf

## Slide 120
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Smaller Size = Higher S/V
(Closed Pores or similar issues)

## Slide 121
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Fractal Aggregate Primary Particles

## Slide 122
Fractal Aggregates and Agglomerates
http://www.eng.uc.edu/~gbeaucag/Classes/Nanopowders/AggregateGrowth.pdf
Aggregate growth
Some Issues to Consider for Aggregation/Agglomeration
Path of Approach, Diffusive or Ballistic (Persistence of velocity for particles)
Concentration of Monomers
persistence length of velocity compared to mean separation distance
Branching and structural complexity
What happens when monomers or clusters get to a growth site:
Diffusion Limited Aggregation
Reaction Limited Aggregation
Chain Growth (Monomer-Cluster), Step Growth (Monomer-Monomer to Cluster-Cluster) or a Combination of Both (mass versus time plots)
Cluster-Cluster Aggregation
Monomer-Cluster Aggregation
Monomer-Monomer Aggregation
DLCA Diffusion Limited Cluster-Cluster Aggregation
RLCA Reaction Limited Cluster Aggregation
Post Growth: Internal Rearrangement/Sintering/Coalescence/Ostwald Ripening

## Slide 123
Fractal Aggregates and Agglomerates
Aggregate growth
Consider what might effect the dimension of a growing aggregate.
Transport Diffusion/Ballistic
Growth Early/Late (0-d point => Linear 1-d => Convoluted 2-d => Branched 2+d)
Speed of Transport Cluster, Monomer
Shielding of Interior
Rearrangement
Sintering
Primary Particle Shape
DLA df = 2.5 Monomer-Cluster (Meakin 1980 Low Concentration)
DLCA df = 1.8 (Higher Concentration Meakin 1985)
Ballistic Monomer-Cluster (low concentration) df = 3
Ballistic Cluster-Cluster (high concentration) df = 1.95

## Slide 124
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes
Reaction Limited,
Short persistence of velocity

## Slide 125
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 126
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 127
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/MeakinVoldSunderlandEdenWittenSanders.pdf
Vold-Sutherland Model particles with random linear trajectories are added to a growing cluster of particles at the position where they first contact the cluster
Eden Model particles are added at random with equal probability to any unoccupied site adjacent to one or more occupied sites
(Surface Fractals are Produced)
Witten-Sander Model particles with random Brownian trajectories are added to a growing cluster of particles at the position where they first contact the cluster
Sutherland Model pairs of particles are assembled into randomly oriented dimers. Dimers are coupled at random to construct tetramers, then octoamers etc. This is a step-growth process except that all reactions occur synchronously (monodisperse system).
In RLCA a “sticking probability is introduced in the random growth process of clusters. This increases the dimension.
In DLCA the “sticking probability is 1. Clusters follow random walk.

## Slide 128
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 129
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 130
Fractal Aggregates and Agglomerates
From DW Schaefer Class Notes
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Primary: Primary Particles
Secondary: Aggregates
Tertiary: Agglomerates
Primary: Primary Particles
Tertiary: Agglomerates

## Slide 131
Hierarchy of Polymer Chain Dynamics

## Slide 132
Dilute Solution Chain
Dynamics of the chain
The exponential term is the “response function”
response to a pulse perturbation

## Slide 133
Dilute Solution Chain
Dynamics of the chain
Damped Harmonic
Oscillator
For Brownian motion
of a harmonic bead in a solvent
this response function can be used to calculate the
time correlation function <x(t)x(0)>
for DLS for instance
τ is a relaxation time.

## Slide 134
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Beads 0 and N are special
For Beads 1 to N-1
For Bead 0 use R-1 = R0 and for bead N RN+1 = RN
This is called a closure relationship

## Slide 135
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
The Rouse unit size is arbitrary so we can make it very small and:
With dR/dt = 0 at i = 0 and N
Reflects the curvature of R in i,
it describes modes of vibration like on a guitar string

## Slide 136
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Describes modes of vibration like on a guitar string
For the “p’th” mode (0’th mode is the whole chain (string))

## Slide 137
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts
Relaxation time follows N2 (actually follows N3/df)
Diffusion constant follows 1/N (zeroth order mode is translation of the molecule) (actually follows N-1/df)
Both failings are due to hydrodynamic interactions (incomplete draining of coil)
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution

## Slide 138
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts
Relaxation time follows N2 (actually follows N3/df)
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution

## Slide 139
Hierarchy of Entangled Melts

## Slide 140
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/SukumaranScience.pdf
Chain dynamics in the melt can be described by a small set of “physically motivated, material-specific paramters”
Tube Diameter dT
Kuhn Length lK
Packing Length p
Hierarchy of Entangled Melts

## Slide 141
Quasi-elastic neutron scattering data demonstrating the existence of the tube
Unconstrained motion => S(q) goes to 0 at very long times
Each curve is for a different q = 1/size
At small size there are less constraints (within the tube)
At large sizes there is substantial constraint (the tube)
By extrapolation to high times
a size for the tube can be obtained
dT

## Slide 142
There are two regimes of hierarchy in time dependence
Small-scale unconstrained Rouse behavior
Large-scale tube behavior
We say that the tube follows a “primitive path”
This path can “relax” in time = Tube relaxation or Tube Renewal
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 143
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 144
Reptation predicts that the diffusion coefficient will follow N2 (Experimentally it follows N2)
Reptation has some experimental verification
Where it is not verified we understand that tube renewal is the main issue.
(Rouse Model predicts D ~ 1/N)

## Slide 145
Reptation of DNA in a concentrated solution

## Slide 146
Simulation of the tube

## Slide 147
Simulation of the tube

## Slide 148
Plateau Modulus
Not Dependent on N, Depends on T and concentration

## Slide 149
Kuhn Length- conformations of chains <R2> = lKL
Packing Length- length were polymers interpenetrate p = 1/(ρchain <R2>)
where ρchain is the number density of monomers

## Slide 150
this implies that dT ~ p

## Slide 155
McLeish/Milner/Read/Larsen Hierarchical Relaxation Model
http://www.engin.umich.edu/dept/che/research/larson/downloads/Hierarchical-3.0-manual.pdf

## Slide 156
Block Copolymers
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/BCP%20Section.pdf

## Slide 157
Block Copolymers
SBR Rubber

## Slide 158
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Amphiphilic.pdf

## Slide 159
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/BCP%20Modeling.pdf

## Slide 160
Hierarchy in BCP’s and Micellar Systems
We consider primary structure as the block nature of the polymer chain.
This is similar to hydrophobic and hydrophilic interactions in proteins.
These cause a secondary self-organization into rods/spheres/sheets.
A tertiary organizaiton of these secondary structures occurs.
There are some similarities to proteins but BCP’s are extremely simple systems by comparison.
Pluronics (PEO/PPO block copolymers)

## Slide 161
What is the size of a Block Copolymer Domain?
-For and symmetric A-B block copolymer
-Consider a lamellar structure with Φ = 1/2
-Layer thickness D in a cube of edge length L, surface energy σ
- so larger D means less surface and a lower Free Energy F.
-The polymer chain is stretched as D increases. The free energy of
a stretched chain as a function of the extension length D is given by
- where N is the degree of polymerization for A or B,
b is the step length per N unit, νc is the excluded volume for a unit step
So the stretching free energy, F, increases with D2.
-To minimize the free energies we have
Masao Doi, Introduction to Polymer Physics

## Slide 163
Chain Scaling (Long-Range Interactions)
Long-range interactions are interactions of chain units separated by such a
great index difference that we have no means to determine if they are from the same chain
other than following the chain over great distances to determine the connectivity. That is,
Orientation/continuity or polarity and other short range linking properties are completely lost.
Long-range interactions occur over short spatial distances (as do all interactions).
Consider chain scaling with no long-range interactions.
The chain is composed of a series of steps with no orientational relationship to each other.
So <R> = 0
<R2> has a value:
We assume no long range interactions so that the second term can be 0.