## Slide 1
Long Range Interactions

## Slide 2
van der Waals’ Equation
p = nRT/V
i.g. from kinetic theory of gasses
Atoms can pass through each other
No enthalpy of interaction
Totally entropic
Modify for excluded volume “b”
p = nRT/(V-b)
Which increases pressure
Modify for excluded volume “b”
and
Attractive enthalpic interaction
“a”
p = nRT/(V-b) – a(n/V)2
-TDS + DH
n/V = r ~ f or c
Binary attractive interactions (can form a liquid)
Which decreases pressure

## Slide 3
Van der Waals’ Equation
p = nRT/(V-b) – a(n/V)2 Van der Waals Equation
Compressibility Factor Z = pVmolar/RT = p/rRT = 1 + B2 r + … Virial Expansion
B2 has units of molar volume
Solve for B2 using the van der Waals Equation
B2 = b – a/RT for molar volume or B2 = b – a/kBT for molecular volume
Flory and Krigbaum knew they needed an energy for an expanded chain of the van der Waals form
Molar Energy = pVmolar = RT (1 + B2 / Vmolar)
Where: B2 = Excluded Volume – Attractive Potential/RT = b – a/RT
Energy = Ideal + repulsive “b” and attractive “a”
When T* = a/Rb, interactions disappear, B2 = 0, and system becomes “ideal”. This is a “critical point” just before phase separation.

## Slide 4
Van der Waals’ Equation
p = nRT/(V-b) – a(n/V)2 Van der Waals Equation
Compressibility Factor Z = pVmolar/RT = p/rRT = 1 + B2 r + … Virial Expansion
B2 has units of molar volume
ZVdW = pVmolar/RT = V/(V-b) – ar = 1/(1-br) – ar/RT
Geometric series Sark = a/(1-r) sum from 0 to ∞
So, 1/(1-br) = Sark = 1 + br + (br)2 + … and for br = b/V is very small
ZVdW = 1/(1-br) – ar/RT = 1 + (b – a/RT) r + (br)2 +…
Compare with the virial expansion
Z = pVmolar/RT = p/rRT = 1 + B2 r + B3 r2 + …
B2 = b – a/RT and B3 = b2

## Slide 5
Van der Waals’ Equation
p = nRT/(V-b) – a(n/V)2 + c (n/V)3 Van der Waals Equation with repulsive ternary interactions
Compressibility Factor Z = pVmolar/RT = p/rRT = 1 + B2 r + B3 r2 + … Virial Expansion
B2 has units of molar volume
ZVdW = pVmolar/RT = V/(V-b) – ar/RT = 1/(1-br) – ar/RT + cr2/RT
Geometric series Sark = a/(1-r) sum from 0 to ∞
So, 1/(1-br) = Sark = 1 + br + (br)2 + … and for br = b/V is very small
ZVdW = 1/(1-br) – ar/RT = 1 + (b – a/RT) r + (b2 + c/RT) r2 +…
Compare with the virial expansion
Z = pVmolar/RT = p/rRT = 1 + B2 r + B3 r2 + …
B2 = b – a/RT and B3 = b2 + c/RT
For an immiscible system B2 is negative or very small (low temperature)
B3 can be positive leading to a discrete phase transition or negative leading to a continuous transition
Red detracts from Black

## Slide 6
Long-Range Interactions
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End-to-End Distance R
By Comparison, The Energy to stretch a Thermally Equilibrated Chain Can be Written
For a Chain with Long-Range Interactions There is and Additional Term
So,
Flory-Krigbaum Theory
Result is called a Self-Avoiding Walk
The Secondary Structure for Synthetic Polymers
Number of pairs

## Slide 9
Linear Polymer Chains have Two Possible Secondary Structure States:
Self-Avoiding Walk
Good Solvent
Expanded Coil
(The Normal Condition in Solution)
The Secondary Structure for Synthetic Polymers
These are statistical features. That is, a single simulation of a SAW and a GC could look identical.
Gaussian Chain
Random Walk
Theta-Condition
Brownian Chain
(The Normal Condition in the Melt/Solid)

## Slide 10
Self-Avoiding Walk
Good Solvent
Expanded Coil
(The Normal Condition in Solution)
Gaussian Chain
Random Walk
Theta-Condition
Brownian Chain
(The Normal Condition in the Melt/Solid)
Concentration driven contraction
Consider going from dilute conditions, c < c*, to the melt by increasing concentration.
The transition in chain size is gradual not discrete.
Synthetic polymers at thermal equilibrium accommodate concentration changes through a scaling transition. Primary, Secondary, Tertiary Structures.
Linear Polymer Chains have Two Possible Secondary Structure States:
The Secondary Structure for Synthetic Polymers

## Slide 11
Self-Avoiding Walk
Good Solvent
Expanded Coil
(The Normal Condition in Solution)
Gaussian Chain
Random Walk
Theta-Condition
Brownian Chain
(The Normal Condition in the Melt/Solid)
Thermally driven expansion
Consider going from Theta Temperature, T = q, to the expanded coil by increasing temperature.
The transition in chain size is gradual not discrete.
Synthetic polymers at thermal equilibrium accommodate thermal changes through a scaling transition. Primary, Secondary, Tertiary Structures.
Linear Polymer Chains have Two Possible Secondary Structure States:
The Secondary Structure for Synthetic Polymers

## Slide 12
Problem: The transition in chain size is gradual not discrete as predicted by FK theory.

## Slide 13
We have considered an athermal hard core potential (excluded volume, ‘b’, from VdW equation)
But Vc actually has an inverse temperature component associated with attractive enthalpic interactions between monomers and solvent molecules (attractive binary interactions, ‘a’, from VdW equation)
The interaction (attractive) energy between a monomer and the polymer/solvent system is on average <E(R)> for a given end-to-end distance R (defining a conformational state). This modifies the probability of a chain having an end-to-end distance R by the Boltzmann probability,
<E(R)> is made up of pp, ps, ss interactions with an average change in attractive energy on solvation of a polymer Δε = (εpp+εss-2εps)/2
For a monomer with z sites of interaction we can define a unitless attractive energy parameter
χ = zΔε/kT that reflects the average enthalpy of attractive interaction per kT per monomer
p = nRT/(V-b) – a(n/V)2
B2 = b – a/RT
PV = RT + RT B2/V (Virial Expansion)
Energy = Ideal + repulsive “b” and attractive “a”
VdW equation
Excluded volume like “b”

## Slide 14
For a monomer with z sites of interaction we can define a unitless energy parameter
χ = zΔε/kT that reflects the average enthalpy of attractive interaction per kT for a monomer
The volume fraction of monomers in the polymer coil with a conformational state of end-to-end distance R is nVc/R3
And there are n monomers in the chain, attractive chain energy “nc”, so,
We can then write the energy of the chain as, (remember c ~ 1/T)
This indicates that when χ = ½ the coil acts as if it were an ideal chain, excluded volume disappears. This condition is called the theta-state and the temperature where χ = ½ is called the theta-temperature. It is a critical point for the polymer coil in solution.
PV = RT(1 + B2/V)
B2 = b – a/RT
When T* = a/Rb interactions disappear

## Slide 15
The effective excluded volume is now Vex = V0 (1/2-c)
The Flory-Krigbaum result for coil size is:
Using this approximation for conditions of large molecular weight:
where
χ = zΔε/kT

## Slide 16
This Solves the Problem: The transition in chain size is gradual not discrete as predicted by FK theory.

## Slide 18
PV = RT(1 + B2/V)
B2 = b – a/RT
When T* = a/Rb interactions disappear
χ = zΔε/kT
Average attractive enthalpy of interaction
For a single polymer coil
B2 = Vc/2 – Vc c
χ = zΔε/kT
For a polymer mixture (polymer/polymer or polymer/solvent)
Flory-Huggins Equation

## Slide 19
Lower-Critical Solution Temperature (LCST)
Polymers can order or disorder on mixing leading to a noncombinatorial entropy term, A in the interaction parameter.
If the polymer orders on mixing then A is positive and the energy is lowered.
If the polymer-solvent shows a specific interaction then B can be negative.
This Positive A and Negative B favors mixing at low temperature and demixing at high temperature, LCST behavior.

## Slide 20
Lower-Critical Solution Temperature (LCST)
Poly vinyl methyl ether/Water
PVME/PS
Also see Poly(N-isopropylacrylamide)/Water

## Slide 21
Two Phases
at Equilibrium
One
Phase
DGm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
Miscibility Limit
Binodal
Spinodal
Critical Point

## Slide 22
Flory-Huggins Equation
Miscibility Limit
Binodal
Spinodal
Critical Point
All three equalities apply
At the critical point
http://rkt.chem.ox.ac.uk/lectures/liqsolns/regular_solutions.html
Hildebrandt Regular Solution Model

## Slide 24
Tc = θ(1-2Φc)
Linear Relationship

## Slide 25
Consider also f* which is the coil composition, generally below the critical composition for normal n or N
Overlap Composition

## Slide 26
Overlap Composition
Φ*
Both f* and fc depend on 1/√N
Below f* the composition is fixed since the coil can not be diluted!

## Slide 27
Overlap Composition
Φ*
Both f* and fc depend on 1/√N
Below f* the composition is fixed since the coil can not be diluted!
So, there is a region (yellow) of coil collapse below the binodal at f* in composition and temperature
Coil
Collapse

## Slide 28
Φ*
Coil
Collapse
Phase
Separation
Θ
Coil
GS-Coil
Overlap Composition
Both f* and fc depend on 1/√N
Below f* the composition is fixed since the coil can not be diluted!
So, there is a regime of coil collapse below the binodal at f* in composition and temperature

## Slide 29
For a polymer in solution there is an inherent concentration to the chain
since the chain contains some solvent
The polymer concentration is Mass/Volume, within a chain
When the solution concentration matches c* the chains “overlap”
Then an individual chain is can not be resolved and the chains entangle
This is called semi-dilute since the solution is still of very low concentration.
The regime below c* is called dilute. Very high concentrations, q-coil, are called concentrated.

## Slide 30
In concentrated solutions with chain overlap
chain entanglements lead to a higher solution viscosity
J.R. Fried Introduction to Polymer Science
Later called ce, entanglement concentration

## Slide 31
Structure and linear viscoelasticity of flexible polymer solutions: comparison of polyelectrolyte and neutral polymer solutions R. Colby, Rheo. Acta 49 425-442 (2010)
h = h0 (1 + [h]c)
hsp= (h - h0)/h0
[h] = limc=>0 (hsp/c)
[h] = Vcoil/m = 1/c* = m3/df - 1

## Slide 32
Structure and linear viscoelasticity of flexible polymer solutions: comparison of polyelectrolyte and neutral polymer solutions R. Colby, Rheo. Acta 49 425-442 (2010)
Red circles neutral good solvent ce
Red stars neutral good solvent c*
Blue circles polyelectrolyte ce
Blue stars polyelectrolyte c*
-2
-0.8
This can be explained if you consider that c* is on a chain size-scale while ce is on a bulk size scale, that is ce is for bulk network pathways while c* is for the coil pathway. ce behaves the same in rigid rods and coils because both make a self-avoiding network on large size scales, c* is different because one chain is a rod the other a self-avoiding walk.
df = 5/3 -0.8
df = 2 -0.5
df = 1. -2

## Slide 33
Extensional Flow

## Slide 34
Extensional Flow
Trouton Viscosity = 3 Shear Viscosity for a Newtonian fluid
For a constant extensional strain rate, g’zz = dvz/dz = constant
So, vz = dz/dt = constant z
dz/z = constant dt
z = exp(Kt)
You need to stretch the fluid with exponentially increasing length.
That is hard to do in a lab.

## Slide 35
How dilute are dilute solutions in extensional flows? C. Clasen, J. P. Plog,, W.-M. Kulicke, M. Owens, C. Macosko, L. E. Scriven, M. Verani and G. H. McKinley, J. Rheol. 50 849-881 (2006);
Diameter from capillary thinning experiments

## Slide 36
How dilute are dilute solutions in extensional flows? C. Clasen, J. P. Plog,, W.-M. Kulicke, M. Owens, C. Macosko, L. E. Scriven, M. Verani and G. H. McKinley, J. Rheol. 50 849-881 (2006);
SAOS = small amplitude oscillatory shear
Shear Measurement

## Slide 37
How dilute are dilute solutions in extensional flows? C. Clasen, J. P. Plog,, W.-M. Kulicke, M. Owens, C. Macosko, L. E. Scriven, M. Verani and G. H. McKinley, J. Rheol. 50 849-881 (2006);
Extensional Measurement

## Slide 38
Structure and linear viscoelasticity of flexible polymer solutions: comparison of polyelectrolyte and neutral polymer solutions R. Colby, Rheo. Acta 49 425-442 (2010)

## Slide 39
Structure and linear viscoelasticity of flexible polymer solutions: comparison of polyelectrolyte and neutral polymer solutions R. Colby, Rheo. Acta 49 425-442 (2010)

## Slide 40
Coil Collapse Following A. Y. Grosberg and A. R. Khokhlov “Giant Molecules”
Grosberg uses:
Rather than the normal definition used by Flory:
What Happens to the left of the theta temperature?
Coil Expansion Factor a

## Slide 41
Coil Collapse Following A. Y. Grosberg and A. R. Khokhlov “Giant Molecules”
Grosberg uses:
Rather than the normal definition used by Flory:
What Happens to the left of the theta temperature?
Short-Range Interactions
We had C∞ = R2/R20 = nKlK2/n0l02 = LlK/Ll0 = lK/l0
Long-Range Interactions
Flory a = R2/R20 = n6/5l2/nl2 ~ n1/5
Grosberg
a2 = R2/R20 :: a ~ n1/10
Page 167

## Slide 42
Coil Collapse Following A. Y. Grosberg and A. R. Khokhlov “Giant Molecules”
Grosberg uses:
Rather than the normal definition used by Flory:
What Happens to the left of the theta temperature?

## Slide 46
Flory-Krigbaum couldn’t integrate R2 P(R) so they took the derivative and found the maximum probability for R2 P(R).
Grosberg takes a different approach that leads to the same answer.
Write the single chain free energy in terms of the coil expansion factor, a, then find the minimum free energy by taking the derivative in a of the free energy and setting it to 0 to find the equilibrium a*

## Slide 47
Van der Waals
dF(a)/da = 0
This is an exact solution by Grosberg’s method

## Slide 48
Van der Waals’ Equation
p = nRT/(V-b) – a(n/V)2 + c (n/V)3 Van der Waals Equation with repulsive ternary interactions
Compressibility Factor Z = pVmolar/RT = p/rRT = 1 + B2 r + B3 r2 + … Virial Expansion
B2 has units of molar volume
ZVdW = pVmolar/RT = V/(V-b) – ar = 1/(1-br) – ar + cr2
Geometric series Sark = a/(1-r) sum from 0 to ∞
So, 1/(1-br) = Sark = 1 + br + (br)2 + … and for br = b/V is very small
ZVdW = 1/(1-br) – ar = 1 + (b – a/RT) r + (b2 + c/RT) r2 +…
Compare with the virial expansion
Z = pVmolar/RT = p/rRT = 1 + B2 r + B3 r2 + …
B2 = b – a/RT and B3 = b2 + c/RT
For an immiscible system B2 is negative or very small (low temperature)
B3 can be positive leading to a discrete phase transition or negative leading to a continuous transition
Red detracts from Black

## Slide 49
B changes sign, positive for miscible, negative for phase separation below the Boyle temperature TB = a/b (B = b – a/T so “a” (or c) is negative for miscibility/repulsive pp)
C is always positive, i.e., favors coil expansion.
C is important below the theta temperature to model the coil to globule transition at high monomer density
For simplicity we ignore higher order terms because C is enough to give the gross features
of this transition.
Generally, it is known that this transition can be either first-order for
biopolymers such as protein folding, or second-order for synthetic polymers.
First-order means that the first derivative of the free energy is not continuous, i.e., a jump in
free energy at a discrete transition temperature, such as a melting point, heat of melting.
Second order, free energy, volume, entropy etc. are continuous through the transition, slope changes in T (heat capacity, thermal expansion coefficient).
n ~ z/R3

## Slide 50
Blob model for coil collapse
Gaussian
Scaling of
g* Blobs
df = 2 for coil
df = 3 for blob
-The expanded coil transitions to a Gaussian chain by locally forming Gaussian “blobs” called “thermal blobs” (will cover later). Neutron scattering provides evidence.
-These blobs grow as the theta point is approached.
-Thermally driven structural changes occur from the bottom up.
-Propose a similar model for the collapse of the theta coil using a different kind of “blob” in analogy to “thermal blobs” but 3d blobs not 2d thermal blobs.

## Slide 51
Blob model for coil collapse
Gaussian
Scaling of
g* Blobs
df = 2 for coil
df = 3 for blob
Number of
Blobs = z/g*

## Slide 52
Number of Blobs (z/g*) times kT is the Confinement Entropy
Entropic Part of Collapse Free Energy
Total Collapse Free Energy
kT C n3 = kT C z3/R3
= kT C/(a6l6)

## Slide 53
α > 1 for expansion
α < 1 for contraction
Free Energy Including Third Virial Coefficient

## Slide 54
Ratio of C/B determines behavior
The collapsed coil is 3d

## Slide 55
x ~ B; y ~ C
B ~ 1/T; a ~ V1/3
Maxwell Construction

## Slide 56
Maxwell Construction
Isotherm of a Cubic Equation of State
in the Two-Phase Region of Temperature
There are three possible roots, two points are at equilibrium, middle is not real.
Lieden the Netherlands
van der Waals place

## Slide 57
EOS Calculation
Phase Diagram
x ~ B; y ~ C
B ~ 1/T; a ~ V1/3

## Slide 58
EOS Calculation
Phase Diagram
x ~ B; y ~ C
B ~ 1/T; a ~ V1/3

## Slide 59
x ~ B; y ~ C
B ~ 1/T; a ~ V1/3

## Slide 60
Generally, it is known that this transition can be either first-order for
biopolymers such as protein folding, or second-order for synthetic polymers.
First order means that the first derivative of the free energy is not continuous, i.e. a jump in
Free energy at a discrete transition temperature, such as a melting point.
x ~ B; y ~ C
B ~ 1/T; a ~ V1/3

## Slide 61
Generally, it is known that this transition can be either first-order for
biopolymers such as protein folding, or second-order for synthetic polymers.
First order means that the first derivative of the free energy is not continuous, i.e. a jump in
Free energy at a discrete transition temperature, such as a melting point.
x ~ B; y ~ C
B ~ 1/T; a ~ V1/3
First-Order
Discrete change in a
Second-Order
a is Continuous

## Slide 62
1.5 Theta
1.6 Expanded
0.774 Sphere
0.92 Draining Sphere
(We will Look at this
further)

## Slide 63
1.5 Theta
1.6 Expanded
0.774 Sphere
0.92 Draining Sphere
(We will Look at this
further)

## Slide 64
Size of a Chain, “R”
(You can not directly measure the End-to-End Distance)

## Slide 65
What are the measures of Size, “R”, for a polymer coil?
Radius of Gyration, Rg
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf

## Slide 66
What are the measures of Size, “R”, for a polymer coil?
Radius of Gyration, Rg
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf

## Slide 67
Radius of Gyration, Rg
2.45 Rg = Reted
Rg is a direct measure of the end-to-end distance for a linear Gaussian chain
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What are the measures of Size, “R”, for a polymer coil?
eted

## Slide 68
Moment of Intertia, I is <Rg2> weighted by mass
For M = 1
Rg/R
Disk/Cylinder Hoop Sphere Rod
Sym. Axis Sym. Axis Solid Center
1/√2=0.707 1 √(2/5)=0.632 1/√12=0.289
Cylinder Hoop Sph. Shell Rod Rg/L
Center Diameter End
√(1/4+(L2/R2)/12) 1/√2=0.707 √(2/3)=0.816 √(1/3)=0.577

## Slide 69
For a distribution of chain lengths/object sizes what moment of the distribution is Rg?
Typically, low order moments are desired such as the mean (first order)

## Slide 70
For a polydisperse sample
what moment of Rg is obtained form scattering?
Polydispersity Index,
D = Mw/Mn = <M2>/<M1>2
D = 1 is monodisperse
2 is most probable distribution
Commercial PE is D=14 and bimodal

## Slide 71
For a polydisperse sample
what moment of Rg is obtained form scattering?
At low qRg2
For polydisperse Rg’s weighted by
For a beach with sand, rocks, and boulders we only measure the boulders with Rg

## Slide 72
For a polydisperse sample
what moment of Rg is obtained form scattering?
R. J. Roe p. 170 Methods of X-Ray and Neutron Scattering in Polymer Science (2000)

## Slide 73
Static Light Scattering for Rg
Guinier’s Law
Guinier Plot linearizes this function
The exponential can be expanded at low-q and linearized to make a Zimm Plot

## Slide 80
p

## Slide 91
Static Light Scattering for Radius of Gyration
Guinier’s Law
Beaucage G J. Appl. Cryst. 28 717-728 (1995).
Lead Term is
A particle with no surface
Consider binary interference at a distance “r” for a particle with arbitrary orientation
Rotate and translate a particle so that two points separated by r lie in the particle for all rotations
and average the structures at these different orientations
Binary Autocorrelation
Function
Scattered Intensity is the Fourier Transform of
The Binary Autocorrelation Function

## Slide 95
Debye Scattering Function for Gaussian Polymer Coil

## Slide 96
What are the measures of Size, “R”, for a polymer coil?
Radius of Gyration, Rg
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf

## Slide 97
Debye Paper Deriving this Equation

## Slide 98
Low-q and High-q Limits of Debye Function
At high q the last term => 0
Q-1 => Q
g(q) => 2/Q ~ q-2
Which is a mass-fractal scaling law with df = 2
At low q, exp(-Q) => 1-Q+Q2/2-Q3/6+…
Bracketed term => Q2/2-Q3/6+…
g(q) => 1-Q/3+… ~ exp(-Q/3) = exp(-q2Rg2/3)
Which is Guinier’s Law

## Slide 99
Ornstein-Zernike Function, Limits and Related Functions
The Zimm equation involves a truncated form of the Guinier Expression intended
For use at extremely low-qRg:
If this expression is generalized for a fixed composition and all q, Rg is no longer
the size parameter and the equation is empirical (no theoretical basis) but has a form
similar to the Debye Function for polymer coils:
This function is called the Ornstein-Zernike function and ξ is called a correlation length.
The inverse Fourier transform of this function can be solved and is given by
(Benoit-Higgins Polymers and Neutron Scattering p. 233 1994):
This function is empirical and displays the odd (impossible) feature that the correlation
function for a “random” system is not symmetric about 0, that is + and – values for r
are not equivalent even though the system is random. (Compare with the normal
behavior of the Guinier correlation function.)

## Slide 100
The Flory Expression indicates a linear dependence of osmotic pressure in concentration at low concentration and a dependence on concentration to the power 2 at high concentration.
From Gert Strobl, Polymer Physics

## Slide 101
Ornstein-Zernike Function, Limits and Related Functions
Low-q limit
High-q limit
Ornstein-Zernike (Empirical)
Debye (Exact)

## Slide 102
Ornstein-Zernike Function, Limits and Related Functions
Empirical Correlation Function
Transformed Empirical Scattering Function
Ornstein-Zernike Function
Debye-Bueche Function
Teubner-Strey Function
(F Brochard and
JF Lennon 1975
J. de Phy. 36(11) 1035)
Sinha Function
c2 is negative to create a peak
Correlation function in all of these cases is not symmetric about 0 which is physically impossible for a random system. The resulting scattering functions can be shown to be non-physical, that is they do not follow fundamental rules of scattering. Fitting parameters have no physical meaning.

## Slide 103
At q => 0 this is 1/osmotic compressibility, dP/df = 1/N + fB2 = (1/N + (1-2c)f)
Zimm Plot (Berry Plot)

## Slide 104
Zimm Plot
In a GPC you have f ~ 0 for each fraction
Measure light scattering at a few angles and extrapolate q2 to 0 to find weight average MW for each fraction. For each fraction the polydispersity, Mw/Mn ~ 1 so Mw = Mn = Mz

## Slide 105
Reprinted (adapted) with permission from McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020, https://doi.org/10.1021/acs.macromol.9b02429. Copyright 2020 American Chemical Society
The license of the image source clearly states that it can be used for commercial and noncommercial purposes and there is no need to ask permission from or provide credit to the photographer or Unsplash, although it is appreciated when possible.
Mean-Field Interactions
Specific Interactions
Behavior of the Lead Term (isothermal compressibility)

## Slide 106
Figure 1 – For dilute dispersions, all structural features can be observed (left). With increasing concentration (going from left to right), the nano-aggregates begin to overlap and the larger features become obscured by the screening phenomenon (dotted line). Above the overlap concentration, the largest observable structural feature is the mesh size. At even higher concentrations, the mesh size decreases further and large-scale structural information is lost.

## Slide 107
Pedersen Sommer Paper 2005

## Slide 108
Random Phase Approximation (RPA) Equation
At high-q, I0(q) is small and 1/I0(q) is much larger than 2c.
At low-q, I0(q) is large, and 2c is much larger than 1/I0(q).
Negative 2c indicates miscibility, positive, phase separation.
Concentration
Temperature, c ~ B/T, high T small c
Polymer in Solution

## Slide 109
How to observe the concentration blob?
Concentration
Contrast match the solvent with a mixture of deuterated and hydrogenous solvents
Tag one chain by deuteration (1% of chains)

## Slide 110
Two types of correlation: Mean Field and Specific Interactions are Experimentally Observed

## Slide 111
These are related to Thermodynamics:
Virial Coefficient = Mean Field = FH c
EOS like Van der Waals = Specific Interaction
(There is overlap)
Non-woven fabric
(fleece, tissue, paper)
Woven
fabric
At large-scale (q => 0)
they appear the same.
We expect I/f(q=>0) to drop at higher concentrations as a measure of 1/(f B2) for both.

## Slide 112
Critical ordering concentration
Rishi, K.; Pallerla, L.; Beaucage, G.; Tang, A. Dispersion of Surface-Modified, Aggregated, Fumed Silica in Polymer Nanocomposites. J. Appl. Phys. 2020, 127 (17), 174702.

## Slide 118
Go to slides 2 second half

## Slide 120
Measurement of the Hydrodynamic Radius, Rh
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
Kirkwood, J. Polym. Sci. 12 1(1953).
http://theor.jinr.ru/~kuzemsky/kirkbio.html

## Slide 122
Intrinsic, specific & reduced “viscosity”
Shear Flow (may or may not exist in a capillary/Couette geometry)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
We can approximate (1) as:
Martin Equation
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1

## Slide 123
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Concentration Effect

## Slide 124
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Concentration Effect, c*

## Slide 125
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Solvent Quality

## Slide 126
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Molecular Weight Effect

## Slide 129
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Temperature Effect

## Slide 130
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
We can approximate (1) as:
Martin Equation
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1
Huggins Equation
Kraemer Equation
(exponential expansion)

## Slide 131
Intrinsic “viscosity” for colloids (Simha, Case Western)
For a solid object with a surface v is a constant in molecular weight, depending only on shape
For a symmetric object (sphere) v = 2.5 (Einstein)
For ellipsoids v is larger than for a sphere,
J = a/b
prolate
oblate
a, b, b :: a>b
a, a, b :: a<b

## Slide 132
Intrinsic “viscosity” for colloids (Simha, Case Western)
Hydrodynamic volume for “bound” solvent
Partial Specific Volume
Bound Solvent (g solvent/g polymer)
Molar Volume of Solvent

## Slide 133
Intrinsic “viscosity” for colloids (Simha, Case Western)
Long cylinders (TMV, DNA, Nanotubes)
J=L/d
End Effect term ~ 2 ln 2 – 25/12 Yamakawa 1975

## Slide 134
Shear Rate Dependence for Polymers
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Capillary Viscometer

## Slide 135
Branching and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 136
Branching and Intrinsic Viscosity
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1

## Slide 137
Polyelectrolytes and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 138
Polyelectrolytes and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 139
Hydrodynamic Radius from Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HiemenzRajagopalanDLS.pdf

## Slide 140
Consider motion of molecules or nanoparticles in solution
Particles move by Brownian Motion/Diffusion
The probability of finding a particle at a distance x from the starting point at t = 0 is a Gaussian Function that defines the diffusion Coefficient, D
A laser beam hitting the solution will display a fluctuating scattered intensity at “q” that varies with q since the particles or molecules move in and out of the beam
I(q,t)
This fluctuation is related to the diffusion of the particles
The Stokes-Einstein relationship states that D is related to RH,

## Slide 141
For static scattering p(r) is the binary spatial auto-correlation function
We can also consider correlations in time, binary temporal correlation function
g1(q,τ)
For dynamics we consider a single value of q or r and watch how the intensity changes with time
I(q,t)
We consider correlation between intensities separated by t
We need to subtract the constant intensity due to scattering at different size scales
and consider only the fluctuations at a given size scale, r or 2π/r = q

## Slide 142
Dynamic Light Scattering
a = RH = Hydrodynamic Radius
The radius of an equivalent sphere following Stokes’ Law

## Slide 143
Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
my DLS web page
Wiki
http://webcache.googleusercontent.com/search?q=cache:eY3xhiX117IJ:en.wikipedia.org/wiki/Dynamic_light_scattering+&cd=1&hl=en&ct=clnk&gl=us
Wiki Einstein Stokes
http://webcache.googleusercontent.com/search?q=cache:yZDPRbqZ1BIJ:en.wikipedia.org/wiki/Einstein_relation_(kinetic_theory)+&cd=1&hl=en&ct=clnk&gl=us

## Slide 144
Diffusing Wave Spectroscopy (DWS)
Will need to come back to this after introducing dynamics
And linear response theory
http://www.formulaction.com/technology-dws.html

## Slide 145
Static Scattering for Fractal Scaling

## Slide 149
For qRg >> 1
df = 2

## Slide 150
Ornstein-Zernike Equation
Has the correct functionality at high q
Debye Scattering Function =>
So,

## Slide 151
Ornstein-Zernike Equation
Has the correct functionality at low q
Debye =>
The relatoinship between Rg and correlation length differs for the two regimes.

## Slide 153
How does a polymer chain respond to external perturbation?

## Slide 154
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End to End Distance R
By Comparison The Energy to stretch a Thermally Equilibrated Chain Can be Written
Force
Force
Assumptions:
-Gaussian Chain
-Thermally Equilibrated
-Small Perturbation of Structure (so it is still Gaussian after the deformation)

## Slide 155
Tensile Blob
For weak perturbations of the chain
Application of an external stress to the ends of a chain create a transition size where the coil goes from Gaussian to Linear called the Tensile Blob.
For Larger Perturbations of Structure
-At small scales, small lever arm, structure remains Gaussian
-At large scales, large lever arm, structure becomes linear
Perturbation of Structure leads to a structural transition at a size scale

## Slide 156
For sizes larger than the blob size the structure is linear, one conformational state so the conformational entropy is 0. For sizes smaller the blob has the minimum spring constant so the weakest link governs the mechanical properties and the chains are random below this size.

## Slide 157: Semi-Dilute Solution Chain Statistics

## Slide 158
In dilute solution the coil contains a concentration c* ~ 1/[η]
for good solvent conditions
At large sizes the coil acts as if it were in a concentrated solution (c>>>c*), df = 2. At small sizes the coil acts as if it were in a dilute solution, df = 5/3. There is a size scale, ξ, where this “scaling transition” occurs.
We have a primary structure of rod-like units, a secondary structure of expanded coil and a tertiary structure of Gaussian Chains.
What is the value of ξ?
ξ is related to the coil size R since it has a limiting value of R for c < c* and has a scaling relationship with the reduced concentration c/c*
There are no dependencies on n above c* so (3+4P)/5 = 0 and P = -3/4
For semi-dilute solution the coil contains a concentration c > c*

## Slide 159
Coil Size in terms of the concentration
This is called the “Concentration Blob”

## Slide 160
Three regimes of chain scaling in concentration.

## Slide 161
Thermal Blob
Chain expands from the theta condition to fully expanded gradually.
At small scales it is Gaussian, at large scales expanded (opposite of concentration blob).

## Slide 162
Thermal Blob

## Slide 163
Thermal Blob
Energy Depends on n, a chain with a mer unit of length 1 and n = 10000
could be re cast (renormalized) as a chain of unit length 100 and n = 100
The energy changes with n so depends on the definition of the base unit
Smaller chain segments have less entropy so phase separate first.
We expect the chain to become Gaussian on small scales first.
This is the opposite of the concentration blob.
Cooling an expanded coil leads to local chain structure collapsing to a Gaussian structure first.
As the temperature drops further the Gaussian blob becomes larger until the entire chain is
Gaussian at the theta temperature.

## Slide 164
Thermal Blob
Flory-Krigbaum Theory yields:
By equating these:

## Slide 166
Fractal Aggregates and Agglomerates

## Slide 167
Polymer Chains are Mass-Fractals
RRMS = n1/2 l
Mass ~ Size2
3-d object
Mass ~ Size3
2-d object
Mass ~ Size2
1-d object
Mass ~ Size1
df-object
Mass ~ Sizedf
This leads to odd properties:
density
For a 3-d object density doesn’t depend on size,
For a 2-d object density drops with Size
Larger polymers are less dense

## Slide 170
Tortuosity
Connectivity
How Complex Mass Fractal Structures
Can be Decomposed
z
df
p
dmin
s
c
R/d
27
1.36
12
1.03
22
1.28
11.2

## Slide 172
Disk
Random Coil
Extended β-sheet
(misfolded protein)
Unfolded Gaussian chain

## Slide 173
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates

## Slide 174
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
http://www.phys.ksu.edu/personal/sor/publications/2001/light.pdf
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.koboproductsinc.com/Downloads/PS-Measurement-Poster-V40.pdf

## Slide 175
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.koboproductsinc.com/Downloads/PS-Measurement-Poster-V40.pdf

## Slide 176
For static scattering p(r) is the binary spatial auto-correlation function
We can also consider correlations in time, binary temporal correlation function
g1(q,τ)
For dynamics we consider a single value of q or r and watch how the intensity changes with time
I(q,t)
We consider correlation between intensities separated by t
We need to subtract the constant intensity due to scattering at different size scales
and consider only the fluctuations at a given size scale, r or 2π/r = q

## Slide 177
Dynamic Light Scattering
a = RH = Hydrodynamic Radius

## Slide 178
Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
my DLS web page
Wiki
http://webcache.googleusercontent.com/search?q=cache:eY3xhiX117IJ:en.wikipedia.org/wiki/Dynamic_light_scattering+&cd=1&hl=en&ct=clnk&gl=us
Wiki Einstein Stokes
http://webcache.googleusercontent.com/search?q=cache:yZDPRbqZ1BIJ:en.wikipedia.org/wiki/Einstein_relation_(kinetic_theory)+&cd=1&hl=en&ct=clnk&gl=us

## Slide 179
Gas Adsorption
http://www.chem.ufl.edu/~itl/4411L_f00/ads/ads_1.html
A + S <=> AS
Adsorption
Desorption
Equilibrium
=

## Slide 180
Gas Adsorption
http://www.chem.ufl.edu/~itl/4411L_f00/ads/ads_1.html
Multilayer adsorption

## Slide 181
http://www.eng.uc.edu/~gbeaucag/Classes/Nanopowders/GasAdsorptionReviews/ReviewofGasAdsorptionGOodOne.pdf

## Slide 182
From gas adsorption obtain surface area by number of gas atoms times an area for the adsorbed gas atoms in a monolayer
Have a volume from the mass and density.
So you have S/V or V/S
Assume sphere S = 4πR2, V = 4/3 πR3
So dp = 6V/S
Sauter Mean Diameter dp = <R3>/<R2>

## Slide 183
Log-Normal Distribution
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Geometric standard deviation and geometric mean (median)
Mean
Gaussian is centered at the Mean and is symmetric. For values that are positive (size) we need an asymmetric distribution function that has only values for greater than 1. In random processes we have a minimum size with high probability and diminishing probability for larger values.
http://en.wikipedia.org/wiki/Log-normal_distribution

## Slide 184
Log-Normal Distribution
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Geometric standard deviation and geometric mean (median)
Mean
Static Scattering Determination of Log Normal Parameters

## Slide 185
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf

## Slide 186
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Smaller Size = Higher S/V
(Closed Pores or similar issues)

## Slide 187
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Fractal Aggregate Primary Particles

## Slide 188
Fractal Aggregates and Agglomerates
http://www.eng.uc.edu/~gbeaucag/Classes/Nanopowders/AggregateGrowth.pdf
Aggregate growth
Some Issues to Consider for Aggregation/Agglomeration
Path of Approach, Diffusive or Ballistic (Persistence of velocity for particles)
Concentration of Monomers
persistence length of velocity compared to mean separation distance
Branching and structural complexity
What happens when monomers or clusters get to a growth site:
Diffusion Limited Aggregation
Reaction Limited Aggregation
Chain Growth (Monomer-Cluster), Step Growth (Monomer-Monomer to Cluster-Cluster) or a Combination of Both (mass versus time plots)
Cluster-Cluster Aggregation
Monomer-Cluster Aggregation
Monomer-Monomer Aggregation
DLCA Diffusion Limited Cluster-Cluster Aggregation
RLCA Reaction Limited Cluster Aggregation
Post Growth: Internal Rearrangement/Sintering/Coalescence/Ostwald Ripening

## Slide 189
Fractal Aggregates and Agglomerates
Aggregate growth
Consider what might effect the dimension of a growing aggregate.
Transport Diffusion/Ballistic
Growth Early/Late (0-d point => Linear 1-d => Convoluted 2-d => Branched 2+d)
Speed of Transport Cluster, Monomer
Shielding of Interior
Rearrangement
Sintering
Primary Particle Shape
DLA df = 2.5 Monomer-Cluster (Meakin 1980 Low Concentration)
DLCA df = 1.8 (Higher Concentration Meakin 1985)
Ballistic Monomer-Cluster (low concentration) df = 3
Ballistic Cluster-Cluster (high concentration) df = 1.95

## Slide 190
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes
Reaction Limited,
Short persistence of velocity

## Slide 191
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 192
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 193
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/MeakinVoldSunderlandEdenWittenSanders.pdf
Vold-Sutherland Model particles with random linear trajectories are added to a growing cluster of particles at the position where they first contact the cluster
Eden Model particles are added at random with equal probability to any unoccupied site adjacent to one or more occupied sites
(Surface Fractals are Produced)
Witten-Sander Model particles with random Brownian trajectories are added to a growing cluster of particles at the position where they first contact the cluster
Sutherland Model pairs of particles are assembled into randomly oriented dimers. Dimers are coupled at random to construct tetramers, then octoamers etc. This is a step-growth process except that all reactions occur synchronously (monodisperse system).
In RLCA a “sticking probability is introduced in the random growth process of clusters. This increases the dimension.
In DLCA the “sticking probability is 1. Clusters follow random walk.

## Slide 194
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 195
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 196
Fractal Aggregates and Agglomerates
From DW Schaefer Class Notes
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Primary: Primary Particles
Secondary: Aggregates
Tertiary: Agglomerates
Primary: Primary Particles
Tertiary: Agglomerates

## Slide 197
Hierarchy of Polymer Chain Dynamics

## Slide 198
Dilute Solution Chain
Dynamics of the chain
The exponential term is the “response function”
response to a pulse perturbation

## Slide 199
Dilute Solution Chain
Dynamics of the chain
Damped Harmonic
Oscillator
For Brownian motion
of a harmonic bead in a solvent
this response function can be used to calculate the
time correlation function <x(t)x(0)>
for DLS for instance
τ is a relaxation time.

## Slide 200
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Beads 0 and N are special
For Beads 1 to N-1
For Bead 0 use R-1 = R0 and for bead N RN+1 = RN
This is called a closure relationship

## Slide 201
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
The Rouse unit size is arbitrary so we can make it very small and:
With dR/dt = 0 at i = 0 and N
Reflects the curvature of R in i,
it describes modes of vibration like on a guitar string

## Slide 202
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Describes modes of vibration like on a guitar string
For the “p’th” mode (0’th mode is the whole chain (string))

## Slide 203
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts
Relaxation time follows N2 (actually follows N3/df)
Diffusion constant follows 1/N (zeroth order mode is translation of the molecule) (actually follows N-1/df)
Both failings are due to hydrodynamic interactions (incomplete draining of coil)
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution

## Slide 204
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts
Relaxation time follows N2 (actually follows N3/df)
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution

## Slide 205
Hierarchy of Entangled Melts

## Slide 206
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/SukumaranScience.pdf
Chain dynamics in the melt can be described by a small set of “physically motivated, material-specific paramters”
Tube Diameter dT
Kuhn Length lK
Packing Length p
Hierarchy of Entangled Melts

## Slide 207
Quasi-elastic neutron scattering data demonstrating the existence of the tube
Unconstrained motion => S(q) goes to 0 at very long times
Each curve is for a different q = 1/size
At small size there are less constraints (within the tube)
At large sizes there is substantial constraint (the tube)
By extrapolation to high times
a size for the tube can be obtained
dT

## Slide 208
There are two regimes of hierarchy in time dependence
Small-scale unconstrained Rouse behavior
Large-scale tube behavior
We say that the tube follows a “primitive path”
This path can “relax” in time = Tube relaxation or Tube Renewal
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 209
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 210
Reptation predicts that the diffusion coefficient will follow N2 (Experimentally it follows N2)
Reptation has some experimental verification
Where it is not verified we understand that tube renewal is the main issue.
(Rouse Model predicts D ~ 1/N)

## Slide 211
Reptation of DNA in a concentrated solution

## Slide 212
Simulation of the tube

## Slide 213
Simulation of the tube

## Slide 214
Plateau Modulus
Not Dependent on N, Depends on T and concentration

## Slide 215
Kuhn Length- conformations of chains <R2> = lKL
Packing Length- length were polymers interpenetrate p = 1/(ρchain <R2>)
where ρchain is the number density of monomers

## Slide 216
this implies that dT ~ p

## Slide 221
McLeish/Milner/Read/Larsen Hierarchical Relaxation Model
http://www.engin.umich.edu/dept/che/research/larson/downloads/Hierarchical-3.0-manual.pdf

## Slide 222
Block Copolymers
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/BCP%20Section.pdf

## Slide 223
Block Copolymers
SBR Rubber

## Slide 224
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Amphiphilic.pdf

## Slide 225
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/BCP%20Modeling.pdf

## Slide 226
Hierarchy in BCP’s and Micellar Systems
We consider primary structure as the block nature of the polymer chain.
This is similar to hydrophobic and hydrophilic interactions in proteins.
These cause a secondary self-organization into rods/spheres/sheets.
A tertiary organizaiton of these secondary structures occurs.
There are some similarities to proteins but BCP’s are extremely simple systems by comparison.
Pluronics (PEO/PPO block copolymers)

## Slide 227
What is the size of a Block Copolymer Domain?
-For and symmetric A-B block copolymer
-Consider a lamellar structure with Φ = 1/2
-Layer thickness D in a cube of edge length L, surface energy σ
- so larger D means less surface and a lower Free Energy F.
-The polymer chain is stretched as D increases. The free energy of
a stretched chain as a function of the extension length D is given by
- where N is the degree of polymerization for A or B,
b is the step length per N unit, νc is the excluded volume for a unit step
So the stretching free energy, F, increases with D2.
-To minimize the free energies we have
Masao Doi, Introduction to Polymer Physics

## Slide 229
Chain Scaling (Long-Range Interactions)
Long-range interactions are interactions of chain units separated by such a
great index difference that we have no means to determine if they are from the same chain
other than following the chain over great distances to determine the connectivity. That is,
Orientation/continuity or polarity and other short range linking properties are completely lost.
Long-range interactions occur over short spatial distances (as do all interactions).
Consider chain scaling with no long-range interactions.
The chain is composed of a series of steps with no orientational relationship to each other.
So <R> = 0
<R2> has a value:
We assume no long range interactions so that the second term can be 0.