## Slide 1
Small-Angle Scattering from Hierarchical Materials
Greg Beaucage, University of Cincinnati
Kammler HK, Beaucage G, Kohls DJ, Agashe N. Ilavsky J
J Appl. Phys. 97(2005) (Article 054309).

## Slide 2
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae
Definition of Semi-Dilute Conditions
  Aggregation/Agglomeration (Immiscible System)
  Mean Field Behavior in Scattering
  Specific Interactions in Scattering
Summary

## Slide 3
Definition of Dilute

## Slide 4
For a complex structure in solution there is an inherent concentration associated with the structure since the structure contains some solvent. For a sphere this is the excluded volume 8V, c* = r/8
The fractal concentration is Mass/Volume, within a structure
When the solution concentration matches c* the structures “overlap”
Then an individual structure can not be resolved and the structures entangle
The regime above c* is called semi-dilute
and the regime below c* is called dilute

## Slide 5
In concentrated solutions with chain overlap
chain entanglements lead to a higher solution viscosity
J.R. Fried Introduction to Polymer Science

## Slide 6
Figure 1 – For dilute dispersions, all structural features can be observed (left). With increasing concentration (going from left to right), the nano-aggregates begin to overlap and the larger features become obscured by the screening phenomenon (dotted line). Above the overlap concentration, the largest observable structural feature is the mesh size. At even higher concentrations, the mesh size decreases further and large-scale structural information is lost.
Structural Screening
At least initially we want to work with dilute samples
You must determine if your sample is dilute
The screening length is a useful parameter to obtain

## Slide 7
≈ ideally diluted
entangled
The “screening effect” and the screening parameter ν
Concentrated micelle system

## Slide 8
Understanding Contrast

## Slide 9
Understanding Contrast
X-rays image mostly counterions
Neutrons and light image hydrocarbons
Similar Worm-Like Micelle Samples
-2 power-law for the shell
-4 power-law for the surface

## Slide 10: Understanding the local structure of worm-like micelles SAXS / CRYSOL / Simulation
Sketch of the micelle cross-section and estimated parameter values involved in the core-shell model. The inset in the upper-right corner is a snapshot of the simulated micelle cross-section with accumulated ions.
Measured, fitted, simulated scattering curves of mixed surfactant sample. The inset in the lower-left corner is a snapshot of the simulated micelle segment.
Jiang, H.; Vogtt, K.; Koenig, P; Jiang, R.; Beaucage, G.; Weaver, M. Coupled simulation and scattering for evaluation of the local structure of worm-like micelles. 2018, submitted.

## Slide 11
Definition of Dilute
Scaling Features in Scattering

## Slide 12
Scattering Observation of the Persistence Length
A power-law decay of -1 slope has only one structural interpretation.
Scaling Behavior of Dilute Synthetic Polymers
θ
Scaling Regimes over a range of q
At low end: a size for that structural level
At the high end a different structural level
R
ri

## Slide 13
Worm-Like Micelles
cross
section
large scale structure
subunit
R
G1 = 10 cm-1
R1 = 20 Å
L1 = 500 Å
sR,1 = 3 Å
z = 6
dmin = 1.1
df = 2.46
c = 2.2
nbr = 2
Cp = 1.46
Rg,2 = 350 Å
G2 = 60 cm-1
circular
R1 = 20 Å
7
With a newly developed approach, the local as well as the global structure can be characterized on the basis of I(q). Using a hybrid scattering function, the local structure (cylinders) and the overall structure (tortuous and/or branched network) are determined.

## Slide 14
5mm LAT 16mm HAB
Typical Branched Aggregate
dp = 5.7 nm
z = 350
c = 1.5, dmin = 1.4, df = 2.1
fbr = 0.8
Branched Aggregates
Beaucage G, Determination of branch fraction and minimum dimension of fractal aggregates Phys. Rev. E 70 031401 (2004).
APS UNICAT
Silica Premixed Flames
J. Appl. Phys 97 054309 Feb 2005

## Slide 15
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
Note:
Guinier’s law works for all q. It is sufficient to describe the structural size for a particular structural level.
Power-laws have two problems.
  The overestimate the intensity at low-q near the Guinier Regime.
  They over estimate the intensity at high-q where the Guinier regime for the next structural level occurs.
We need structurally-limited power-laws to unify (sum) Guinier and power-law scattering.

## Slide 16
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
Derivation of Guinier’s Law from the Correlation Function
This will provide a framework for structurally limited power-laws

## Slide 17
Porod’s Characteristic Function
Rotationally averaged
centro-symmetric structures (Debye)
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function

## Slide 20
For a sphere

## Slide 22
At high-q Porod’s Law
I(q) = 9 Nne2 (qR/(qR)3)2 = 9 Nne2/(qR)4
= 2pNVre2 (S/V) q-4
At low-q Guinier’s Law
cos x = 1 – x2/2! + x4/4!-…
sin x = x – x3/3! + x5/5!-…
exp(-x) = 1-x2/2!+x3/3!-..
I(q) = Nne2exp(-q2Rg2/3)

## Slide 25
Consider the origin of the vector r

## Slide 34
Beaucage, G. "Approximations leading to a unified exponential/power-law approach to small-angle scattering." Journal of Applied Crystallography 28.6 (1995): 717-728.

## Slide 36
Guinier’s Law
Beaucage G J. Appl. Cryst. 28 717-728 (1995).
Lead Term is
A particle with no surface
Consider binary interference at a distance “r” for a particle with arbitrary orientation
Rotate and translate a particle so that two points separated by r lie in the particle for all rotations
and average the structures at these different orientations
Binary Autocorrelation
Function
Scattered Intensity is the Fourier Transform of
The Binary Autocorrelation Function
Guinier’s Law describes a particle with no surface or internal structure

## Slide 40
G = Nne2
Rayleigh, 1914
Scattering Function for Monodisperse Spheres
-4 Power-law for Porod scattering
Solid Surface

## Slide 41
The Debye (1947) Scattering Function for a Polymer Coil
-2 Power-law for Gaussian Chain
df = 2

## Slide 42
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
Derivation of Guinier’s Law from the Correlation Function
Limitations of Power-Laws at Low and High q

## Slide 44
I(q) ~ N ne2
ne Reflects the number of electrons in a particle
N is total number of particles
Second Premise of Scattering All Structures Have a Surface.

## Slide 45
The only location for contrast between phases is
at the interface (for every vector r there is a vector r/2)
I(q) ~ N ne2
ne Reflects the number of electrons in a particle
N is total number of particles
Second Premise of Scattering All Structures Have a Surface.

## Slide 46
At the other extreme we consider a surface.
We can fill the interface with spheres of size r
N = S/(πr2)
I(q) ~ N ne2
ne Reflects the number of electrons in a particle
N is total number of particles
Second Premise of Scattering All Structures Have a Surface.

## Slide 47
N = S/(πr2)
Porod’s Law can be thought of as the
Second Premise of Scattering:
All “Particles” have a surface reflected by S/V.
(dp = (S/V)-1)

## Slide 48
For a Rough Surface: ds < 3
(This Function decays to Porod’s Law at small sizes)

## Slide 49
Beaucage, G. "Approximations leading to a unified exponential/power-law approach to small-angle scattering." Journal of Applied Crystallography 28.6 (1995): 717-728.

## Slide 50
At low-q sin(qr)/qr = 1
(sin x = x – x3/3! + x5/5!-…)
Integrate g(r)r2 => particle volume
Integrals for Gaussian and Sphere match at large r
At high-q only the small r values matter
g(r) for a sphere and Porod match at small r
Slope at r = 0 is S/4V (0 for Gaussian, particle with no surface; it is the same value for sphere and Porod)

## Slide 51
Structurally-Limited Porod’s Law
r x S gives surface volume
Consider ½ of surface doesn’t contribute to scattering
Orientation gives a factor of ½
<cos2q> = ½
Model fails at large r (small q)
Due to curvature of the surface
This leads to an over estimation of the scattering near Rg.

## Slide 52
Particle Translation/Rotation are used to obtain a Gaussian characteristic function and Guinier’s Law

## Slide 53
A similar approach can be used to describe the limitation to Porod’s Law at low-q near Rg
Consider an “average” Gaussian particle
This sometimes results in a Porod condition (a probability that drops following a Gaussian decay with q or 1/r)
Without translation this doesn’t meet the Porod condition
With translation it meets the Porod condition, effectively shortening rb to the same size as ra. The translation makes low-q is like high-q

## Slide 54
The translation effectively reduces r for the original figure. Reduced r ~ increased q.
Due to the Gaussian probability we effectively see high-q scattering at low-q

## Slide 55
By modification of q rather than the scattering function this is a universal function that can work with any object that displays a radius of gyration and follows Guinier’s Law

## Slide 56
We consider one orientation of the vector r (1-d) for 3d translation of the structure
Integrate for all displacement distances
A Gaussian probability following the Guinier derivation

## Slide 57
This describes the 1-d probability (one r vector) due to finite structure
Cube to get 3-d probability that modifies g(r) in the Debye Function
So qr in the denominator becomes q*r with q* =q/(erf(qRg/√6)3
As an approximation we also substitute sin(qr) with sin(q*r)
Which enables substitution of q* for q in any power-law
This integral is an error function

## Slide 58
By modification of q rather than the scattering function this is a universal function that can work with any object that displays a radius of gyration and follows Guinier’s Law

## Slide 59
For Porod’s Law we write
This can be summed with Guinier’s Law to yield the Unified scattering function.
Beaucage, G. "Approximations leading to a unified exponential/power-law approach to small-angle scattering." Journal of Applied Crystallography 28.6 (1995): 717-728.

## Slide 60
When is this an appropriate approximation? (Most of the time)
Approximation is exact at high-q, q > 2p/Rg
sin(qr)/qr = sin(qr)/q*r = sin(q*r)/q*r
Approximation is good at very low-q
sin(qr)/q*r = sin(q*r)/q*r
(See two thin dashed curves in Fig. 7)
Between p/Rg < q < 2p/Rg
(See bottom two solid curves in Fig. 7)
Approximation leads to steeper decay in integral
This is inconsequential for surface scattering
For mass-fractal scattering the calculated scattering curve is within 95% of actual. An empirical prefactor for Rg of kMass Fractal = 1.06 improves the match to 99.2%.

## Slide 61
High q-Limit to Power laws
Power-laws terminate at the next structural level since the conditions for the power-law, such as mass fractal structure, are no longer descriptive of the material at that size scale. The functional form for this loss of power-law scattering is the same as for Guinier’s Law for the next smaller structural level
This high-q limit to power-laws naturally occurs for the scattering functions for disks and rods
Beaucage, G. "Approximations leading to a unified exponential/power-law approach to small-angle scattering." Journal of Applied Crystallography 28.6 (1995): 717-728.

## Slide 62
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low and High q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology

## Slide 63
Beaucage, G. "Approximations leading to a unified exponential/power-law approach to small-angle scattering." Journal of Applied Crystallography 28.6 (1995): 717-728.
erf(x): Error function.
Index i=1, 2,… correspond to different structure levels.
Rg,i : Radius of gyration correspond to structural level i
Pi : Power-law decay slope for level i
ki : Correction factor = 1 for Pi > 3 and 1.06 for Pi < 3
The Unified Function

## Slide 64
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low and High q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering

## Slide 65
Nanoparticle Formation
Solution Route
-Separation
-Surface Tension
(Pore/Particle Collapse)
-Solvent Disposal
-Reaction Rate is Slow
-Transport is Slow
-Batch Process
Aerosol Route
-Particles are Pre-Separated
-No Surface Tension Issues
-No Solvent Disposal
-Reaction Rate is Fast
-Continuous Process
-Rapid Supersaturation & Dilution
Kelvin
Laplace

## Slide 66
Nano-particles form far from equilibrium.
T ~ 2500°K
Time ~ 100 ms
fv ~ 1 x 10-6
dp ~ 5 to 50 nm

## Slide 67
Kammler HK, Beaucage G, Kohls DJ, Agashe N. Ilavsky J
J Appl. Phys. 97(2005) (Article 054309).

## Slide 68
X-ray, λ
2θ
d = λ/(2 sin θ) = 2π/q
Branched Aggregates

## Slide 69
Guinier’s Law
X-ray, λ
2θ
d = λ/(2 sin θ) = 2π/q

## Slide 70
Guinier and
Porod Scattering
X-ray, λ
2θ
d = λ/(2 sin θ) = 2π/q
Structure of Flame Made Silica Nanoparticles
By Ultra-Small-Angle X-ray Scattering
Kammler/Beaucage Langmuir 2004 20 1915-1921

## Slide 71
Polydispersity
Particle size distributions from small-angle scattering using global scattering functions, Beaucage, Kammler, Pratsinis J. Appl. Cryst. 37 523-535 (2004).
X-ray, λ
2θ
d = λ/(2 sin θ) = 2π/q

## Slide 72
Linear Aggregates
Beaucage G, Small-angle Scattering from Polymeric Mass Fractals of Arbitrary Mass-Fractal Dimension, J. Appl. Cryst. 29 134-146 (1996).
X-ray, λ
2θ
d = λ/(2 sin θ) = 2π/q

## Slide 73
Branched Aggregates
Beaucage G, Determination of branch fraction and minimum dimension of fractal aggregates Phys. Rev. E 70 031401 (2004).
X-ray, λ
2θ
d = λ/(2 sin θ) = 2π/q

## Slide 74
Large Scale (low-q) Agglomerates

## Slide 75
Small-scale Crystallographic Structure

## Slide 76
5mm LAT 16mm HAB
Typical Branched Aggregate
dp = 5.7 nm
z = 350
c = 1.5, dmin = 1.4, df = 2.1
fbr = 0.8
Branched Aggregates
Beaucage G, Determination of branch fraction and minimum dimension of fractal aggregates Phys. Rev. E 70 031401 (2004).
APS UNICAT
Silica Premixed Flames
J. Appl. Phys 97 054309 Feb 2005

## Slide 78
f* same for all flames!
TiCl4 Diffusion Flame Nucleation and Growth

## Slide 79
Activated growth
for z
Titania Diffusion Flame from TiCl4
Beaucage G, Agashe N, Kohls D, Londono D, Diemer B

## Slide 80
Silica Diffusion Flame
Axial Particle Growth follows
Classic Diffusion Limited
Surface Growth, d ~ t1/2

## Slide 81
Kammler HK, Beaucage G, Kohls DJ, Agashe N. Ilavsky J
J Appl. Phys. 97(2005) (Article 054309).
Summary:
SAXS as a tool for in situ
observation of structure
2) Homogeneous nucleation
appears to be a common
feature of flame growth.
3) A wide range of particle
growth mechanisms can
be involved
4) Branching can be monitored
in terms of the mass fractal
dimension but
5) A much richer description of
aggregate growth is give by
inclusion of new model for
branched structure.

## Slide 82
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low and High q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering

## Slide 83
Tortuosity
Connectivity
How Complex Mass Fractal Structures
Can be Decomposed
z
df
p
dmin
s
c
R/d
27
1.36
12
1.03
22
1.28
11.2

## Slide 84
Disk
Random Coil
Extended β-sheet
(misfolded protein)
Unfolded Gaussian chain

## Slide 85
Branch Content from Scattering
G Beaucage, Physical Review E (2004)
A S Kulkarni and G Beaucage, Journal of Polymer Science, Part B: Polymer Physics (2006)
R2
R1
dmin
p

## Slide 86
Branch Content from Scattering
G Beaucage, Physical Review E (2004)
A S Kulkarni and G Beaucage, Journal of Polymer Science, Part B: Polymer Physics (2006)
R2
R1
dmin
p

## Slide 87
Branch Content from Scattering
G Beaucage, Physical Review E (2004)
A S Kulkarni and G Beaucage, Journal of Polymer Science, Part B: Polymer Physics (2006)
R2
R1
dmin
p
c
dmin

## Slide 88
G Beaucage, Physical Review E, 70, 031401 (2004)
AS Kulkarni, G Beaucage, J Polym Sci, Part B: Polym Phy, 44, 1395 (2006)
-2
Topological information can be extracted from this feature arising from combining Local Scattering Laws
 |  |  | df = c x dmin
dmin | 2 | 1 | 2
c | 1 | 2 | 2

## Slide 89
Determination of dmin, c and df.
Beaucage G, Determination of branch fraction and minimum dimension of fractal aggregates Phys. Rev. E 70 031401 (2004).
There appears to be a quantifiable difference in scattering for different dmin and the same df.

## Slide 90
Determination of dmin, c and df.
Beaucage G, Determination of branch fraction and minimum dimension of fractal aggregates Phys. Rev. E 70 031401 (2004).
df c dmin
Gaussian
Chain 2 1 2
Disk 2 2 1
Static scattering can be
used to obtain dmin.

## Slide 91
Branched polystyrene
in a good solvent
dmin should be 5/3 (1.67) for
self-avoiding walk
Mw/Mn ~ 2
Good Solvent Scaling for c = 1 and c > 1

## Slide 92
Hyperbranched polyesteramides
Sample Rg,2 df dmin c Description Mn* Mw*
1 17.2 (15.5) 1.3 1 1.3 Regular 1.5 3.6
2 22.2 (21.6) 1.64 1.67 1 Linear 1.8 5.9
3 26.8 (30.5) 1.60 (1.63) 1.09 1.47 Close to Regular 2.4 11.0
4 57.5 1.74 (1.68) 1.59 1.09 Close to Linear 2.4 59.0
5 288.3 1.63 (1.63) 1.34 1.21 Branched 2.8 248
One pot synthesis semi-random
Dendrimers
For samples 3 & 4 polydispersity
is apparent due to linear
vs branched chains.
Linear is local persistent branching
Regular is global structural branching
*Mn & Mw in kg/mole
Molecular Structure Characterization of Hyperbranched Polyesteramides ETF Gelade, B Goderis, K. Mortensen et al. Macromolecules 34 3552-58 (2001)

## Slide 93
Branched Polymers at Thermal
Equilibrium: Model Systems for LCB
For Polymers dmin is the
Thermodynamically Relevant
Dimension (5/3 = 1.67 or 2)
df = dmin c
~ thermo x branching
PDI ~ 1.05
F5
“2D Slice”
F2

## Slide 94
Mole fraction of Branches

## Slide 95: Multi-Arm Star Polymers
# | Sample | Rg (Å) | df | dmin | c | fbr | Theoretical fbr
1 | 3 Arm Star | 6.87 | 2.00 | 1.33 | 1.49 | 0.39 | 0.33
2 | 6 Arm Star | 78.27 | 2.00 | 1.25 | 1.59 | 0.71 | 0.67
3 | 18 Arm Star | 4.37 | 2.27 | 1.61 | 1.40 | 0.81 | 0.88
Horton et al., Macromolecules, 22, 681 (1989)
US Jeng, TL Lin, LY et al. App Phys A, 74, S487 (2002).

## Slide 96: Hyperbranched Polymers
E. De Luca, R. W. Richards, I. Grillo, and S. M. King, J. Polym. Sci.: Part B: Polym. Phys. 41, 1352 (2003).
Geladé, E. T. F.; Goderis, B.; et al. Macromolecules, 34, (2001).
AS Kulkarni, G Beaucage, Macromolecular Rapid Communications, accepted, (2007).
SANS on Hyperbranched Polymers: Beaucage model correctly describes transition from good-solvent to Q - solvent collapsed state for the minimum path dimension.
a)
b)

## Slide 97
 | Mn (g/mol) | Index LCBI | Mole Fraction of Branches φbr | NMR nbr/104 C
PE 0 | 46,500 | 0.04 | 0 | 0
PE 2 | 11,500 | 0.91 | 0.39±0.005 | 0.36
PE 3 | 37,900 | 2.27 | 0.63±0.004 | 0.91
Model Based on
Mole Fraction of
Branches
This Approach Can Quantify LCB in Polyolefins.

## Slide 98
Mw/Mn ~ 4
Large aggregates
Growth kinetics show
dmin => 1
df => 1.8 for RLCA
Predicted previously
by Meakin
Model Polydisperse Simulations

## Slide 99
R
a
L
N = a (
R
/
a
)
d
f
How Dense?
(
/
a
) = (
R
/
a
)
dmin
Minimum Path Dim.
1≤
d
f
≤ 3
1≤
dmin
≤ df
C = d
f
/dmin How Branched?
Linear C = 1; Reg. C = df
Mean Aggregate Size, "R"
Mean Primary Particle Size, "a"
Specific Surface Area related to 1/
a
"
R
" is related to "
a
", "N", and Structure
"
S
t
r
u
c
t
u
r
e
"
i
s
R
e
l
a
t
e
d
t
o
G
r
o
w
t
h
M
e
c
h
a
n
i
s
m
"
a
"
i
s
R
e
l
a
t
e
d
t
o
E
a
r
l
y
S
t
a
g
e
"
N
"
a
n
d
"
R
"
t
o
L
a
t
e
r
S
t
a
g
e

## Slide 100
1
0
0
n
m
1
0
0
n
m
1
0
0
n
m
Nano-Aggregates Can Act as Springs
From:
S. K. Friedlander, H. D. Jang, K. H. Ryu
Appl. Phys. Lett.
72
173 (1998).
Static
Stressed
Released
F
F
E
s
e
E
Aggregate
= E
Oxide
(
a
/
R
)
3+
dmin
From:
T. A. Witten, M. Rubinstein, R. H. Colby
J. Phys. II France
3
, 367 (1993).
R
a
dmin is Dimension
of Stressed
Path

## Slide 101
Summary of Witten/Rubinstein/Colby Theory
for Mechanics of Springy Aggregates in Elastomers
E
Aggregate
= E
Oxide
(
a
/
R
)
3+
dmin
R
a
dmin is Dimension
of Stressed
Path
Aggregates are only Effective
below a Critical Size,
R
critical
R
critical
=
a
(E
Oxide
/E
Rubber
)
1/(3+
dmin
)
A Critical Concentration is Predicted Beyond which
There is No Higher Reinforcing Effect,
f
critical
f
critical
= (
R
/a)
df-3
The Modulus for a Critical Concentration Composite, E
composite
is given by:
E
composite
= E
Oxide
f
critical
(3+
dmin
)/(3-df)
Test these Propositions using Tuned Nano-Composites

## Slide 102
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low and High q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering

## Slide 103
Unfolded proteins
Is the molten golbule a third phase of proteins? VS Pande & DS Rohksar, PNAS 95 1490-94 (1998)
Simulation Results,
g is denaturant
-Unfolded state is analogous to gas state (following
Flory random walk model as applied by Pande)
-Dense states not associated with biological activity
could be analogous to glassy state (molten globule)
-0 conformational entropy native state is analogous to
crystalline state
-Unfolded state contains some:
Chain persistence associated with fluctuating
helicies and b-sheets
Crosslink/disulfide/cystine-cystine bonds that act as
branching sites
hydrophobic interactins that may appear to be
branching sites
-Conformational transitions should show increase in
df and c towards a regular 3d structure

## Slide 104
Unfolded proteins
“a Gaussian-like conformation”
Mapping the cytochrome C
folding landscape
Julia G. Lyubovitsky
Caltech 2003 Biochemistry
Rg df dmin c
125Å 2.05 1.07 1.90
This is almost a regular structure
with dimension 2:
A crumpled sheet!!

## Slide 105
Rg PDI
94.0Å 1.08
This is and almost sperical
domain of
24.3 nm diameter.
Deviation from PDI = 1
can be due to polydispersity
or asymmetry.
Cytochrome C
Native State Space Filling Model

## Slide 106
Rg PDI
Native 94.0 Å 1.08
MG 99.0 Å 2.90
(Both also
Show Aggregates at
Low-q)
Model of cytochrome b562
A) MG B) N
Cytochrome C
Molten Globule State
Alberts B, Bray D, Lewis J, Raff M, Roberts K, Watson JD. Chapter 5: Protein Function. Molecular Biology of the Cell 3rd Ed. Garland Publishing, New York. 1994. pg 213 & 215.

## Slide 107
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering

## Slide 108
Descriptors
Beaucage, G. Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E – Statistical, Nonlinear, and Soft Matter Physics 2004, 70, 031401-1–031401-10.
Rai, D., Beaucage, G., Jonah, E. O., Britton, D. T., Sukumaran, S., & Härting, M. Quantitative investigations of aggregate systems. J. Chem. Phys. 2012, 137, 044311–1–044311-6.
Ramachandran, R., Beaucage, G., Kulkarni, A. S., McFaddin, D., Merrick-Mack, J., & Galiatsatos, V. Branch content of metallocene polyethylene.
Macromolecules 2009, 42, 4746–4750.

## Slide 109
Unified Fit :
Parameters from Unified Fit used to determine topological parameters:
Scattering
Beaucage, G. Approximations Leading to a Unified Exponential/Power-Law Approach to Small-Angle Scattering J. Appl. Cryst. 1995, 28 (6), 717–728.
Herrmann, H. J., & Stanley, H. E. The fractal dimension of the minimum path in two- and three-dimensional percolation. Journal of Physics A: Mathematical and General 1988, 21, L829–L833.
Meakin, P., Majid, I., Havlin, S., & Stanley, H. E. Topological properties of diffusion limited aggregation and cluster-cluster aggregation. Journal of Physics A: Mathematical and General 1984, 17, L975–L981.
Witten, T. A., & Sander, L. M. Diffusion-limited aggregation. Physical Review B 1983, 27, 5686–5697.
Sorensen, C. M. Light scattering by fractal aggregates: A review. Aerosol Sci. Tech. 2001, 35, 648–687.

## Slide 110
Algorithm:
Input z and a sticking probability
Randomly grow aggregates
Compute the scattering parameters, p, R, nBr etc.
Iterate by varying sticking probability until computed matches experimental
A. Mulderig, G. Beaucage, K. Vogtt, H. Jiang and V. Kuppa, Quantification of branching in fumed silica, J. Aerosol Sci. 2017, 109, 28–37.

## Slide 111
A. Mulderig, G. Beaucage, K. Vogtt, H. Jiang and V. Kuppa, Quantification of branching in fumed silica, J. Aerosol Sci. 2017, 109, 28–37.
Experimental
Simulation

## Slide 112
A. Mulderig, G. Beaucage, K. Vogtt, H. Jiang and V. Kuppa, Quantification of branching in fumed silica, J. Aerosol Sci. 2017, 109, 28–37.

## Slide 113
A. Mulderig, G. Beaucage, K. Vogtt, H. Jiang and V. Kuppa, Quantification of branching in fumed silica, J. Aerosol Sci. 2017, 109, 28–37.

## Slide 114
A. Mulderig, G. Beaucage, K. Vogtt, H. Jiang and V. Kuppa, Quantification of branching in fumed silica, J. Aerosol Sci. 2017, 109, 28–37.

## Slide 115
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae

## Slide 116
We often have an ideal nanoscale structure that aggregates, agglomerates, becomes convoluted, becomes branched. For example, protein aggregation and agglomeration.
-Form factor at nanoscale is available
-Unified can describe larger-scale power-law scaling regimes composed of perfect structures
Two examples:
Worm-Like Micelles: Polydisperse rods form tortuous and branched chains.
Polymer Crystals: Stacked lamellae (form factor and structure factor from Brämer Function) form fibers and spherulites.
Hybrid Unified Functions:

## Slide 117: The Unified Function for a Rod Structure
The Unified Function allows decomposing a given structure into its elements e.g. a rod consisting of spherical subunits. The total scattering is the sum of all contributions.
This strategy can be applied to WLMs, too. These exhibit a local cylindrical geometry, so it would be an advantage, to take this explicitly into account.
⟶ The new function employs for the structural level i = 1 the form factor of a cylinder

## Slide 118: The Unified Function
The unified function expresses the scattered intensity I(q) of mass fractal-like systems via an exponential Guinier-Term and a power-law term B q-d. In principle an arbitrary number of structural levels can be described in this manner
i = 1
i = 2
Beaucage (2004), Phys. Rev. E, 70:031401, Ramachandran et al. (2008), Macromolecules, 41:9802
(for branched structures)

## Slide 119: A Hybrid Unified Function: The Cylindrical Subunits
Fit model:
Unified model for large scale structure, form factor and G1 = I0 for cylindrical subunits
Assuming that micelles can be structurally approximated by solid, homogenous cylinder or a cylindrical shell
Self avoiding walk in good solvent ® fixed dmin = 1.67
radius R1 polydisperse (Log-Normal distribution with scale parameter sR1)
No end-caps taken into account

## Slide 120: Input and fitting parameters
fitting
parameter
meaning
L1
length of cylinders
R1
radius of cylinders
sR1
standard deviation
of radii distribution
n
screening parameter
(virial coefficient)
G2
zero-angle scattering
of global structure
Rg,2
radius of gyration of
global structure
df,2
fractal dimension of
global structure
input
parameters
meaning
f
volume fraction
Dr
scattering length density
contrast; from mass den-sities of micelles or bead
density from MD-
simulations (shell model)
dmin,2
(fractal) dimension of chain
without branches (= 1.67)
Cp
polydispersity factor for size
of large scale structure
(Mz/Mw)
Based on the model a function describing the scattering patters can be formulated. The model
distuingishes between the local, cylindrical structure (index 1) and the large scale assembly of
the cylinders (index 2).

## Slide 121
Structural hierarchies of worm-like micelles: impact on rheological properties
Dreiss (2007), Soft Matter, 3:956
Contour and subunit lengths of WLMs have a large impact on the macroscopic viscoelastic properties. Interestingly, branching reduces the zero-shear viscosity.
⟶ WLM-systems are vastly employed in liquid soaps, drag reducers and fracking fluids
⟶ structure-function relationship
k
k
k
k

## Slide 122
Structural hierarchies of worm-like micelles (WLMs): An assembly of rods
The WLMs are approximated as a chain of cylinders with length L1 and radius R1
With symbol z as number of subunits the contour length L equals z⨉L1
The contributions of the cylinders and the overall chain to the total scattered intensity I(q) can be separated ⟶ “hybrid function” for fitting
i
struct. element
1
cylindrical sub-unit ⟶ P(q) of a cylinder
2
Overall chain (branching, tortuosity) ⟶ Unified Function

## Slide 123
The scattered intensity I(q) and the structural domains
cross
section
large scale structure
subunit
R
G1 = 10 cm-1
R1 = 20 Å
L1 = 500 Å
sR,1 = 3 Å
z = 6
dmin = 1.1
df = 2.46
c = 2.2
nbr = 2
Cp = 1.46
Rg,2 = 350 Å
G2 = 60 cm-1
circular
R1 = 20 Å
7
With a newly developed approach, the local as well as the global structure can be characterized on the basis of I(q). Using a hybdrid scattering function, the local structure (cylinders) and the overall structure (tortuous and/or branched network) are determined.

## Slide 124
Structural hierarchies of WLMs: Fitting I(q)

## Slide 125
Structural hierarchies of WLMs: Addition of salt
⟶ upon addition of NaCl basically just the large scale structure changes
⟶ number of subunits increases
⟶ possibly onset of branching at 5.0% NaCl
0.232% mixed surf.
Vogtt et al., Langmuir 31:8228-8234

## Slide 126
Addition of salt and branching
trend of branch content with NaCl-concentration as expected
error bars are large due to minimum q of SANS-measurements (~ 0.003 Å-1)
further data at low q (USANS, SLS) is required

## Slide 127
Structural hierarchies of WLMs: The influence of salt
approximately exponential increase of number of subunits with [NaCl] over the whole observed range
an according increase of zero-shear viscosity is observed
⟶ trend is as predicted for wormlike micelles

## Slide 128
Structural hierarchies of WLMs: The influence of salt
⟶ dependence of specific viscosity on contour length L2 as expected for diluted regime
Vogtt et al., Langmuir 31:8228-8234

## Slide 129
Summary
A hybrid scattering function was developed to describe the structure of wormlike chains. It employs the unified function for the large-scale structure and the form factor of a cylinder for the local geometry.
The function is relatively simple, easy to understand and accounts for branching.
In principle any form factor P(q) can be employed for the local structure.
The function successfully describes the scattered intensity obtained from wormlike micelles.
The fitting results agree with the expected structural changes upon addition of NaCl.
Error bars for large-scale parameters in present data set are large ⟶ data from USANS or SLS are required for an improvement

## Slide 130
Neutron Scattering Function for
Branched Worm-Like Micelles
Greg Beaucage Karsten Vogtt (POSTER 311 at 11) (Durgesh Rai)
Chemical and Materials Engineering
University of Cincinnati

## Slide 132
Link rheology to micelle structure
Ron Larson/Mike Weaver
Average
Micellar Length
Mesh
Size
Micelle
radius
Beth Schubert, 2003
1
2
tr
G0
c
bending
modes
G”min
Rouse
modes
Entanglement
Length
persistence
length
terminal
relaxation
Structure inferred from rheology, using Standard Cates Model and newer developments (Larson group, others…)

## Slide 133
Size Scales of Interest
Average
Micellar Length
Mesh
Size
Micelle
radius
Beth Schubert, 2003
Entanglement
Length
persistence
length
Structure inferred from rheology, using Standard Cates Model and newer developments (Larson group, others…)
Micelle Radius/Diameter, rcs (dispersion)
Persistence Length, lp
Micelle Shape (Elliptical or Round)
Contour Length, L
Mesh Size, ξΜ
Branch Length, Lbr
Number of Branches, nbr

## Slide 134: Scaling Model
z Kuhn steps, Dimension df , Size R
Minimum path p : dimension dmin
Kuhn Segment : size lk or 2lp
TORTUOSITY
CONNECTIVITY
Connective path s : dimension c
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 135
G1
G2
R2
R1
df
Bf
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
SANS From Persistent Polymer Chains
z = G2/G1
df from slope
Notes: …..So all the sizes and dimensions that are obtained from such an analysis is used in the scaling approach to quantify the branch content…

## Slide 136: Quantification of Branching
Mole-Fraction LCB Content
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Ramachandran, R.; Beaucage, G.; Kulkarni, A. S.; McFaddin, D.; Merrick-Mack, J.; Galiatsatos, V., Branch Content of Metallocene Polyethylene. Macromolecules 2009, 42 (13), 4746-4750.
Average number of branch points per chain

## Slide 137: Quantification of Branching
Hyperbranch Content (Branch-on-Branch)
Average LCB length
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Ramachandran, R.; Beaucage, G.; Kulkarni, A. S.; McFaddin, D.; Merrick-Mack, J.; Galiatsatos, V., Branch Content of Metallocene Polyethylene. Macromolecules 2009, 42 (13), 4746-4750.
Notes: …So in order to obtain these sizes and dimensions to quantify the branched structure, we use….

## Slide 138
Hybrid Unified Function for worm-like micelles

## Slide 140
ν = A2 φ

## Slide 141
SLES
1 wt. %
3 wt. % NaCl
Simple Rod Structure

## Slide 142
SLES
1 wt. %
6 wt. % NaCl
9 cylinder subunits
About 2 branches

## Slide 143
0.26 wt. % SLES + additive
6 wt. % NaCl
12 cylinder subunits
1 branch for 7 chains

## Slide 144
Summary
-Hybrid Unified Function for worm-like micelles is introduced.
-Function can be coupled with tools to quantify chain topology to yield quantitative measures of the average branching in the micelles.
-Parameterization is being coupled with rheological models to predict dynamic viscosity by Ron Larson.

## Slide 145
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae

## Slide 146
Pradhan, D.; Ehrlich, P. Morphologies of Microporous Polyethylene and Polypropylene Crystallized from Solution in Supercritical Propane. J. Polym. Sci. Part B Polym. Phys. 1995, 33 (7), 1053–1063. https://doi.org/10.1002/polb.1995.090330709.
Semi-Dilute to Concentrated Lamellae

## Slide 147
The Brämer Function
.
Brämer, R. Eindimensionale Röntgenkleinwinkelstreuformeln Parakristalliner Lamellenclusterstrukturen. Kolloid-Zeitschrift Zeitschrift für Polym. 1972, 250 (11–12), 1034–1038. https://doi.org/10.1007/BF01498885.
Brämer, R.; Gerdes, C.; Wenig, W. Analysis of the Small-Angle X-Ray Scattering of Linear Polyethylene by a Paracrystalline Lattice Model. Colloid Polym. Sci. 1983, 261 (4), 293–298. https://doi.org/10.1007/BF01413934.
Stribeck, N. Small-Angle X-Ray Scattering Functions in the Vicinity of Zero Scattering Angle with an Application to Polymer Blends. Macromolecules 1996, 29 (22), 7217–7220. https://doi.org/10.1021/ma951656t.
Burger, C.; Zhou, H. W.; Wang, H.; Sics, I.; Hsiao, B. S.; Chu, B.; Graham, L.; Glimcher, M. J. Lateral Packing of Mineral Crystals in Bone Collagen Fibrils. Biophys. J. 2008, 95 (4), 1985–1992. https://doi.org/10.1529/biophysj.107.128355.
Che, J.; Locker, C. R.; Lee, S.; Rutledge, G. C.; Hsiao, B. S.; Tsou, A. H. Plastic Deformation of Semicrystalline Polyethylene by X-Ray Scattering: Comparison with Atomistic Simulations. Macromolecules 2013, 46 (13), 5279–5289. https://doi.org/10.1021/ma4005007.

## Slide 148
Not Perfect Lamellae
So Power -2 is incorrect
Locally perfect globally tortuous
Pradhan, D.; Ehrlich, P. Morphologies of Microporous Polyethylene and Polypropylene Crystallized from Solution in Supercritical Propane. J. Polym. Sci. Part B Polym. Phys. 1995, 33 (7), 1053–1063.

## Slide 149
Terminate Lamellar Regime
Terminate Tortuous Regime
Power-Law Regime for Tortuosity of Lamellae
The Unified-Hybrid Brämer Function

## Slide 150
Not Perfect Lamellae
So Power -2 is incorrect
Locally perfect globally tortuous
Pradhan, D.; Ehrlich, P. Morphologies of Microporous Polyethylene and Polypropylene Crystallized from Solution in Supercritical Propane. J. Polym. Sci. Part B Polym. Phys. 1995, 33 (7), 1053–1063.

## Slide 152
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae
Definition of Semi-Dilute Conditions
  Aggregation/Agglomeration (Immiscible System)
  Mean Field Behavior in Scattering
  Specific Interactions in Scattering

## Slide 153
Phase Separation/Immiscible System
-Particles can form mass-fractals structures in aggregation above the overlap concentration
-Particles can form 3d agglomerates
These are both dealt with as a new level of structure in the Unified Approach

## Slide 154
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae
Definition of Semi-Dilute Conditions
  Aggregation/Agglomeration (Immiscible System)
  Mean Field Behavior in Scattering
  Specific Interactions in Scattering

## Slide 155
The RPA Equation
Reduced high-q intensity remains unchanged,
Reduced low-q intensity is diminished with concentration increase
The q => 0 intercept is a measure of the strength of binary interactions (the Second Order Virial Coefficient)
This assumes no specific interactions. A mean field is considered.

## Slide 156
Pedersen Sommer Paper 2005
Van der Waals Model
A2 = b – a/T
b = excluded volume
a = attractive interaction

## Slide 157
ν = A2 φ

## Slide 158
≈ ideally diluted
entangled
The “screening effect” and the screening parameter ν
Concentrated micelle system

## Slide 159: Understanding the local structure of worm-like micelles SAXS / CRYSOL / Simulation
Sketch of the micelle cross-section and estimated parameter values involved in the core-shell model. The inset in the upper-right corner is a snapshot of the simulated micelle cross-section with accumulated ions.
Measured, fitted, simulated scattering curves of mixed surfactant sample. The inset in the lower-left corner is a snapshot of the simulated micelle segment.
Jiang, H.; Vogtt, K.; Koenig, P; Jiang, R.; Beaucage, G.; Weaver, M. Coupled simulation and scattering for evaluation of the local structure of worm-like micelles. 2018, submitted.

## Slide 160
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae
Definition of Semi-Dilute Conditions
  Aggregation/Agglomeration (Immiscible System)
  Mean Field Behavior in Scattering
  Specific Interactions in Scattering

## Slide 161
McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020
The license of the image source clearly states that it can be used for commercial and noncommercial purposes and there is no need to ask permission from or provide credit to the photographer or Unsplash, although it is appreciated when possible.
Mean Field System
Specific Interaction System

## Slide 162
Mean field (RPA4,5):
4 Pedersen, J. S.; Sommer, C. Temperature dependence of the virial coefficients and the chi parameter in semi-dilute solutions of PEG In Scattering Methods and the Properties of Polymer Materials; Springer: Berlin, 2005; Vol. 130, p 70.
5 Vogtt, K.; Beaucage, G.; Jiang, H.; Weaver, M. Thermodynamic stability of wormlike micelle solutions. Soft Matter 2017, 13 (36), 6068−6078.
Specific interactions:
Reprinted (adapted) with permission from McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020, https://doi.org/10.1021/acs.macromol.9b02429. Copyright 2020 American Chemical Society
Mean Field
Specific Interactions

## Slide 163
2 Beaucage, G. Approximations Leading to a Unified Exponential/Power-Law Approach to Small-Angle Scattering J. Appl. Cryst. 1995, 28 (6), 717–728.
3 Aggregate simulation code from Mulderig, A.; Beaucage, G.; Vogtt, K.; Jiang, H.; Kuppa, V. Quantification of branching in Fumed Silica. J. Aerosol Sci. 2017, 109 (March), 28–37.
Unified Fit2 :
Reprinted (adapted) with permission from McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020, https://doi.org/10.1021/acs.macromol.9b02429

## Slide 164
For specific interactions we consider the structure factor S(q)
I(q) = F2(q) S(q)
S(q) = I(q)/f (f0/I0(q))

## Slide 165
6 Percus, J.K. and Yevick, G.J. Analysis of Classical Statistical Mechanics by Means of Collective Coordinates. Phys. Rev. 1958, 110, 1-13.
Wertheim, M. S. Exact Solution of the Percus-Yevick Integral Equation for Hard Spheres. Phys. Rev. Lett. 1963, 10, 321-323.
7 Guinier, A. and Fournet, G. Small Angle Scattering of X-rays; John Wiley & Sons: New York, US, 1955.
1 McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020, https://doi.org/10.1021/acs.macromol.9b02429
Percus-Yevick Fit6
Born-Green Fit7
Polydisperse Born-Green Fit1
Reprinted (adapted) with permission from McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020, https://doi.org/10.1021/acs.macromol.9b02429. Copyright 2020 American Chemical Society

## Slide 166
McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020

## Slide 167
8 Data from Anderson, B. J. and Zukoski, C.F. Rheology and Microstructure of Polymer Nanocomposite Melts: Variation of Polymer Segment− Surface Interaction. Langmuir 2010, 26, 8709−8720.
9 Data from Jin, Y.; Beaucage, G.; Vogtt, K.; Jiang, H.; Kuppa, V.; Kim, J.; Ilavsky, J.; Rackaitis, M.; Mulderig, A.; Rishi, K.; et al. A Pseudo- Thermodynamic Description of Dispersion for Nanocomposites. Polymer 2017, 129, 32-43.
McGlasson, A.; Rishi, K.; Beaucage, G.; Chauby, M.; Kuppa, V.; Ilavsky, J.; Rackaitis, M. Quantification of Dispersion for Weakly and Strongly Correlated Nanofillers in Polymer Nanocomposites. Macromolecules 2020

## Slide 168
Ordering criterion:
Adapted from Rishi, K.; Pallerla, A.; Beaucage, G.; Tang, A. Dispersion of surface-modified, aggregated, fumed silica in polymer nanocomposites, J. Appl. Phys. 127 (2020) 174702.

## Slide 169
Rishi, K.; Pallerla, A.; Beaucage, G.; Tang, A. Dispersion of surface-modified, aggregated, fumed silica in polymer nanocomposites, J. Appl. Phys. 127 (2020) 174702.

## Slide 170
Lamellar Stacking Using Unified and Born-Green Approach
Born-Green Function for Correlated Structures
1-d correlations normal to lamellae
Accounting for random orientation of stacks
Packing factor for stacked lamellae

## Slide 171
Lamellar Stacking Using Unified and Born-Green Approach
Born-Green Function for Correlated Structures
Account for orientationally and interfacial disorder (Debye-Waller Type)
Account for finite crystals and packing disorder (Scherrer Type)
Five parameter model

## Slide 172
Lamellar Stacking Using Unified and Born-Green Approach
Five parameter model
Extend to additional structural levels

## Slide 173
Hierarchical structures in block copolymer polyolefins

## Slide 174
Definition of Dilute
Scaling Features in Scattering
Guinier’s Law and Power-Laws
  Derivation of Guinier’s Law from the Correlation Function
  Limitations of Power-Laws at Low- and High-q
The Unified Function for Hierarchical Materials
  Mass-Fractal Scattering
  Quantification of Branching and Topology
  Dilute Unfolded Protein Scattering
Simulated Structures from Scattering
Hybrid Unified Functions
  Worm-like Micelles
  Hybrid Brämer Function
  Correlated Lamellae
Definition of Semi-Dilute Conditions
  Aggregation/Agglomeration (Immiscible System)
  Mean Field Behavior in Scattering
  Specific Interactions in Scattering
Summary

## Slide 175
Steps for analysis of SAXS/SANS from Hierarchical Materials
Determine if your system is dilute or semi-dilute by estimating c*
If your system isn’t dilute, find a way to make it dilute if within reason
Identify the source of contrast in your system with the scattering technique you are using. SAXS, SALS/LS and SANS from WLMs are quite different
Make preliminary measurements on as wide a range of scattering vector as experimentally possible, USAXS (Ilavsky), Multiple range and instrument SANS (ORNL/NIST/ILL)
Identify reasonable power-law regimes in a log-log plot to determine the number of structural levels that are present. You are looking for -4 slope, -2’ish slopes, -1 slopes. Do local Guinier fits between the power-laws to get ball park sizes
Make an assessment of the structural hierarchy, draw a cartoon, compare with micrographs, theory, reason. Make sure your sizes are accurate based on your model and the data. If you are comfortable with your model then determine the scattering range of interest and collect more data. When you run into problems go to step 1 again.
Consider hybrid approach if your base structure is close to perfect and can be quantified, native state protein, rod substructure, spherical substructure. Otherwise use generic Unified Function with constraints dictated by your model.
Consider higher concentrations. Is your system: aggregating (mass fractal), agglomerating (Porod/surface fractal), mean field interactions (random phase approximation), specific interactions (simple Born-Green or other models). For specific interactions determine the structure factor using the dilute scattering curve and fit. Make sure you understand what range of q can be fit with your model for correlations (often large scale aggregates or agglomerates impact the data at low-q).