## Slide 1: USAXS/SAXS from Organic Pigment Samples August 2014 Dr. Greg Beaucage, University of Cincinnati Ms. Hanqiu Jiang, PhD Student, University of Cincinnati Dr. Karsten Vogtt, Post Doctoral Scientist, University of Cincinnati Dr. Jan Ilavsky, Scientist, Argonne National Laboratory Department of Chemical and Materials Engineering, University of Cincinnati, Cincinnati OH 45221-0012, 513 373 3454, beaucag@uc.edu, gbeaucage@gmail.com
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 2
Outline:
-Example Fit
-Table of Fit Results for 0.05% Samples
-Plots for Concentration Series and 1µm Films on Mylar
-Plots of Sample Groups for Comparison
-Summary
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 3
Samples Run at APS August 2014
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 4
Example Fit
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 5
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 6
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 7
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 8
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 11
Concentration Series

## Slide 12
Concentration Series

## Slide 13
Concentration Series

## Slide 14
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 15
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 16
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 17
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 18
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 19
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 20
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 21
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 22
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 23
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 24
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 25
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 26
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 27
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 28
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 29
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 30
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 31
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 32
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 33
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 34
Summary
16x5 Samples Run
80 Samples (+ 8 Dilutions)
2) 0.05% Samples fit and tabulated
16 Samples
3) Generally concentration series qualitatively follow the RPA formulation
In some cases it didn’t, e.g. PB15:1
4) Generally 1µm Films on Mylar showed enhanced aggregation
In some cases they didn’t, specifically the PY14 samples except Py14 RSb
5) More analysis is needed but this will take several weeks
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 35
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 36: Scaling Model
z Primary Particles, Dimension df , Size dp
Minimum path p : dimension dmin
Primary Particle Size, dp
TORTUOSITY
CONNECTIVITY
Connective path s : dimension c
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Notes: How tortuous/How twisty ..So essentially with the scaling model, we have resolved a complex structure into a topological network of branch sites and a tortuous path through the structure.

## Slide 37
G1
G2
R2
R1
df
Bf
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
SANS From Persistent Chains
Notes: …..So all the sizes and dimensions that are obtained from such an analysis is used in the scaling approach to quantify the branch content…

## Slide 38: Quantification of Branching
Mole-Fraction LCB Content
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Ramachandran, R.; Beaucage, G.; Kulkarni, A. S.; McFaddin, D.; Merrick-Mack, J.; Galiatsatos, V., Branch Content of Metallocene Polyethylene. Macromolecules 2009, 42 (13), 4746-4750.
Average number of branch points per chain

## Slide 39: Quantification of Branching
Mole-Fraction LCB Content
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Ramachandran, R.; Beaucage, G.; Kulkarni, A. S.; McFaddin, D.; Merrick-Mack, J.; Galiatsatos, V., Branch Content of Metallocene Polyethylene. Macromolecules 2009, 42 (13), 4746-4750.
Average number of branch points per chain

## Slide 40: Quantification of Branching
Hyperbranch Content (Branch-on-Branch)
Average LCB length
Beaucage, G., Determination of branch fraction and minimum dimension of mass-fractal aggregates. Physical Review E 2004, 70 (3).
Ramachandran, R.; Beaucage, G.; Kulkarni, A. S.; McFaddin, D.; Merrick-Mack, J.; Galiatsatos, V., Branch Content of Metallocene Polyethylene. Macromolecules 2009, 42 (13), 4746-4750.
Notes: …So in order to obtain these sizes and dimensions to quantify the branched structure, we use….

## Slide 41
lp = √3Rg,2 = 14.9 nm
R = 4 Rg,1/√3 = 8.3 nm
φBr = 0.52
nBr = 0.7
zBr = 22
z = 180
L = 0.9 µm
Literature Data, Dreiss (2007)

## Slide 42
Work of Nikhil Agashe C. I. Pigment Yellow 14
C. I. PY 14

## Slide 43
Work of Nikhil Agashe C. I. Pigment Yellow 14
C. I. PY 14

## Slide 48
Concentration Series

## Slide 56
http://www.eng.uc.edu/~beaucag/SunVideo/SunVideos.html

## Slide 57
Summary:
-Yellow-14 pigment particles form aggregated structures on the nanoscale that can influence their optical performance. From past studies found large, dense aggregates (df ~ 2.7, and z ~ 300) are observed in polypropylene dispersions.
-In this study smaller aggregates are observed in surfactant stabilized aqueous dispersions of pigment with about 16 primary particles and a low density with a fractal dimension of 1.34 and about three branches per aggregate.
-The MTB milled sample has primary particles of 36.6 nm Sauter mean diameter. In the previous study the 5% PY14 in polypropylene sample had primary particles of about 80 nm diameter.
-The primary particle size was 60 nm for Microtron milling and 62 nm for Silverson milling. The degree of aggregation dropped to about 4 for the milled samples. The polydispersity of aggregates and primary particles was about the same for all of the aqueous dispersion samples.
-The RPA equation could describe scattering from higher concentration aqueous suspensions with some variation in the enthalpic interaction term, χ, and the volume ratio in Table 1.

## Slide 58
Summary:
-Light scattering from the highest concentration 29% samples displayed multiple scattering and/or screening effects that were not seen for x-ray scattering. This may be related to the higher angles used in light scattering or to differences in contrast between x-rays and light. The one percent dispersions didn't match well the light scattering data in the overlapping region.
-LS for the five percent dispersions seemed to agree with USAXS data. All three of the one percent samples displayed highly polydisperse domains or clusters larger than 50 μm in light scattering. The five percent samples displayed mass fractal scattering with mass fractal dimensions of 1.7 and 2.0 for the Microtron sample. The Microtron sample also displayed 12.5 μm clusters while the other two samples displayed fractal clusters larger than 50 μm.
-Distinctions can be made between the Silverson and Microtron milled samples from the five percent light scattering data and from the one percent USAXS data. On the nanoscale, the pigment makes smaller primary particles with a lower degree of aggregation for the Microtron samples. The Silverson aggregates are probably branched to some extent though this couldn’t be quantified from the USAXS data. In light scattering, the Microtron sample has much smaller clusters of fractal aggregates with a higher density and mass fractal dimension for the five percent aqueous dispersion. This is consistent with the optical micrographs shown in Figure 11.