## Slide 1
Dependencies of the Heat of Formation
Reference State: Elemental ground state at STP has an enthalpy of formation of 0 N2, O2, He etc.
Generally, energy is released on formation of a molecule from the elements if the molecule is stable, so the heat of formation is generally negative. For unstable molecules such as NO which is a radical formed at high temperatures, the heat of formation is positive (endothermic).

## Slide 2
Ellingham Diagrams

## Slide 3
Ellingham Diagrams

## Slide 4
Relative magnitude of heat of formation from elements, oxides, heat of fusion, heat of transition
Spinel
Olivine
Spinel
b

## Slide 5
Heats of formation for various titanium oxides
Values are almost identical

## Slide 6
Electronegativity, the ability of an atom to attract electrons in a bond
Linus Pauling

## Slide 7
Factors involved in the heat of formation: electronegativity and atomic size
Difference in electronegativity between the two compounds
Average electronegativity of the two compounds
Van Arkel–Ketelaar triangle
Jensen’s quantitative triangle
Norman’s quantitative triangle

## Slide 8
e.g. molten Na and Cl2 gas
Energetics of compound formation
Hess’s Law
“Electron gain”

## Slide 9
Energetics of compound formation

## Slide 10
Energetics of compound formation
Electrostatic attraction +-
Electron electron repulsion
Van der Waals or dispersion (d+ makes d- leads to net attraction)
Polarization (shifting within compound of electrons)
Crystal field effects

## Slide 11
Electrostatic interactions in NaCl
Nearest neighbors of Na+ and Cl-
Repulsive cationic terms, second nearest neighbors
Third nearest neighbors, attraction between M+ and X-
Generally:

## Slide 12
Repulsion and Dispersion Terms
Leonard-Jones (6-12) Potential
12 is repulsive since dE/dr = F is positive (guessed)
6 is van der Waals attractive force (calculated)
Buckingham Potential
Exponential term works better for ceramics

## Slide 13
Less electroneg. Halides
Less stable
Less electroneg. Alkalies
Less stable
Lattice
Lattice
Less electroneg. Alkalies
More stable

## Slide 14
Trends in Enthalpy of Formation Alkali Metals
Lattice cancels atomization and ionization
DHlattice drops others constant across halides Fig. 7.4 a c
Less electroneg. alkalies
Electroneg. Halide big impact

## Slide 15
“Extra electrons (12) are not screening the nuclear charge effectively, resulting in a much higher ionization enthalpy for the group 12 elements and a less negative enthalpy of formation for the group 12 compounds compared with the group 2 compounds.” (book)

## Slide 16
Transition Metal Enthalpy of Formation

## Slide 17
p-orbitals
6 valence electrons
(more acidic to right)
s-orbitals
2 valence electrons
(more basic to right)
Acidic
Basic
d-orbitals
10 valence electrons
Transition
Metals
f-orbitals
14 valence electrons
Basic (at low oxidation state)
Acidic (at high oxidation state)

## Slide 18
f-orbitals
14 valence electrons

## Slide 19
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory
Crystal Field Theory

## Slide 20
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 21
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 22
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 23
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 24
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 25
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 26
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 27
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 28
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 29
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 30
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 31
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory
26-3 = 23 = 2+2+6+2+6+(5 d). Unpaired electrons => Paramagnetic

## Slide 32
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Supplemental_Modules_and_Websites_(Inorganic_Chemistry)/Crystal_Field_Theory/Crystal_Field_Theory

## Slide 33
Depending on the crystallographic environment the d-orbital energies split
This impacts the Enthalpy of Formation
Crystal Field Effect

## Slide 34
Crystal Field Stabilization Energy

## Slide 35
Crystal Field Stabilization Energy

## Slide 36
Transition metal lattice stabilization due to d-orbital splitting
First series chlorides, oxides and fluorides
Increasing d electrons
Atomization Component
Ionization Component
Lattice Component
Crystal Field Stabilization due to d-orbital splitting
(not for Ca, Mn, Zn)

## Slide 37
Heat of Formation for Transition Metal Oxides
in Different Oxidation States
Cr, Mo, W
3d, 4d, 5d

## Slide 38
Acid-Base Model for Heat of Formation of Ternary Oxides
SiO2
Na2O
Base transfers its oxygen
s-block oxides
Acid accepts oxygen p-block oxides
SiO42-
MgO < CaO < SrO < BaO
Basicity
Al < Si < P < S
Acidity
SiNa2O3

## Slide 39
p-orbitals
6 valence electrons
(more acidic to right)
s-orbitals
2 valence electrons
(more basic to right)
Acidic
Basic
d-orbitals
10 valence electrons
Transition
Metals
f-orbitals
14 valence electrons
Basic (at low oxidation state)
Acidic (at high oxidation state)

## Slide 40
Most Basic Oxide
BaO
Sulfate most stable since SO3 most acidic

## Slide 41
Ionic potential
e-/ionic radius (Å)
q/r
<2 strong base
2-4 basic
4-7 amphoteric
>7 acidic
From UV spectra of probe ion
Ionic potential ratio

## Slide 42
Atomic Size
Perovskite structure
Calcium titanate CaTiO3
Embed cations in the structure for engineered properties
One is solar energy absorption in Graetzel cells
These are the most promising low-temperature formation PV devices
(silicon solar cells require high temperature reduction of silica and chemical purification)
Cubic/Orthorhombic-like structure
Can accommodate many transition metals
ABX3
A is much larger than B cations, X is anion (oxide)
B has 6-fold coordination surrounded by octahedron of anions
A has 12-fold cubahedral coordination
Red O2-
Blue Ti4+
Green Ca2+ or Ba2+

## Slide 43
t = 1 Perfect Cubic
0.8 < t < 1.1
A is simple cubic
With O in the face center positions
And B in the body center positions

## Slide 45
Methyl Ammonium Lead Halide

## Slide 46
Schematic of a sensitized perovskite solar cell in which the active layer consist of a layer of mesoporous TiO2which is coated with the perovskite absorber. The active layer is contacted with an n-type material for electron extraction and a p-type material for hole extraction. b) Schematic of a thin-film perovskite solar cell. In this architecture in which just a flat layer of perovskite is sandwiched between two selective contacts. c) Charge generation and extraction in the sensitized architecture. After light absorption in the perovskite absorber the photogenerated electron is injected into the mesoporous TiO2 through which it is extracted. The concomitantly generated hole is transferred to the p-type material. d) Charge generation and extraction in the thin-film architecture. After light absorption both charge generation as well as charge extraction occurs in the perovskite layer.

## Slide 47
spiro Ometad p-type semi-conductor

## Slide 48
Enthalpy of Formation versus Number of Valence Electrons
TiC with ne = 4 has a high enthalpy of formation since the Fermi level falls in a pronounced gap in density of electronic states separating bonding and anti-bonding electron bands.
Reduced electrons in bonding state
Increased electrons in anti-bonding state
Fermi level falls in gap between bonding and anti-bonding at 4

## Slide 49
Zeolites (Natural are aluminosilicate rocks, synthetic can be a variety of materials often based on SiO2)
Microscopic structure of a zeolite (mordenite) framework, assembled from tetrahedra. Sodium is present as an extra-framework cation (in green).
Can form meso or micro pores (colloidal- or nano-scale) (These are terms from gas adsorption field.)

## Slide 50
Synthetic Zeolites can have meso (colloidal) or micro (nano) pores depending on the templating material and synthesis conditions. Usually start with TEOS and a surfactant or block copolymer
Reference 29

## Slide 51
Molar Volume
Enthalpy relative to quartz
Surface effect as we saw earlier except that this is on a molecular/nano scale

## Slide 52
Energy of Formation for Substitutional Solid Solutions
Atomic Radii => Volume of compounds
Hume-Rothery Rule limited solubility if size difference exceeds 15%
Electronegativity
Large difference in binary system leads to negative enthalpy of mixing Pd-Zr and is small for systems with low or no electronegativity and size difference Ti-Zr
Valence electron density
Binary components have the same crystal structure
Large enthalpy of mixing is related to large number of intermetallic phases
Elastic contribution to the enthalpy of mixing, small mixes well with large
ci are constants xi mole fractions V molar volumes
Sub-regular solution model

## Slide 54
Energy of Formation for Interstitial Solid Solutions
Elastic interactions
Electronic interactions
Gas solubility in metals
Temperature
Pressure solubility for H2 x ~ √p
Sievert’s Law
Solubility of gasses in metals

## Slide 55
6 kJ/mole difference in formation enthalpy
Reduction temperature is 600K higher for hexagonal
Cubic reduced SrMnO2.5 is more stable
Octahedral corners shared in cubic, faces shared in hexagonal
High vacancies in faces make reduced hexagonal unfavorable

## Slide 56
Liquid-Liquid Miscibility
Mixing of acidic (SiO2) and Basic (CaO) oxides Si4+ has coordination number 4 and Ca2+ has 6
SiO2 mixes well with CaO but CaO has a harder time mixing with SiO2
Increasing basicity
Ortho-silicate
Ca2SiO4
ZrF4 strong acid
Increasing basicity
ZrF62-

## Slide 57
Liquid Salt Mixtures
Size parameter, d = (dA – dB)/(dA + dB)
Common Anions mix with negative enthalpy of mixing
Common cations do not mix due to anion-anion repulsion

## Slide 58
Conformational Enthalpy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
Carbon has a tetrahedral bonding arrangement
For a chain of carbon, the two side groups interact with the side groups of neighboring carbons
“Trans” is sterically the most favorable arrangement
“Gauche +” and “Gauche -” are less favorable
The Boltzmann equation gives the probability of a particular conformation, Z is the partition function or the sum of all the different Boltzmann expressions in an ensemble
For Butene

## Slide 59
Conformational Enthalpy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
Carbon has a tetrahedral bonding arrangement
For a chain of carbon, the two side groups interact with the side groups of neighboring carbons
“Trans” is sterically the most favorable arrangement
“Gauche +” and “Gauche -” are less favorable
The Boltzmann equation gives the probability of a particular conformation, Z is the partition function or the sum of all the different Boltzmann expressions in an ensemble
Neumann Projection
For Butene

## Slide 60
Conformational Enthalpy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
Carbon has a tetrahedral bonding arrangement
For a chain of carbon the two side groups interact with the side groups of neighboring carbons
“Trans” is sterically the most favorable arrangement
“Gauche +” and “Gauche -” are less favorable
The Boltzmann equation gives the probability of a particular conformation, Z is the partition function or the sum of all of the different Boltzmann expressions in an ensemble
For Butene

## Slide 61
Conformational Energy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
Carbon has a tetrahedral bonding arrangement
For a chain of carbon, the two side groups interact with the side groups of neighboring carbons
Helmholtz Free Energy and Entropy
Boltzmann equation where Z is number of states (which depend on temperature and energy barriers)
For Butene
U = FP + SPT
-SUV
H A(F)
-pGT
Internal Energy

## Slide 62
Conformational Enthalpy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
For a polymer with N carbons there are N-2 covalent bonds
The number of discrete conformation states per chain is nN-2 where n is the number of discrete rotational states for the chain, tttt, g-g-g-g-,g+g+g+g+,g+ttt, etc. for N = 4; N1=1, N4=4, etc. assuming no end effects
Average rotational angle
Characteristic Ratio
q is the bond angle
180°-109° = 71°
Eg+- = 2100 J/mole
C∞ = 3.6
Exp. 6.7