## Slide 1
Phase Diagrams
Gibbs Phase Rule
Eutectic Phase Diagram Ag + Cu
Univariant Equilibrium
Liquidus
Solidus
Invariant Equilibrium
Eutectic
Lever Rule
Tieline (conode)
and
Silver acts like a solvent to copper and copper acts like a solvent to silver with limited solubility that is a function of temperature with a solubility limit at the eutectic point (3 phases in equilibrium)
L => a + B

## Slide 2
From Thermo-Calc Program (Solder Demo)

## Slide 3
Phase Diagrams
Gibbs Phase Rule
Eutectic Phase Diagram Ag + Cu
Univariant Equilibrium
Liquidus
Solidus
Invariant Equilibrium
Eutectic
Lever Rule
Tieline (conode)
and

## Slide 4
Phase Diagrams

## Slide 5
Phase Diagrams
Slow Cool Morphology
Consider the morphology in a slow cool from T1 (liquid) to T3 (solid). Just below T1 domains of Cu/Ag at about 98% Cu form in the liquid matrix. The fraction Cu/Ag solid increases as temperature drops, probably growing on the seeds formed at T1. By T2 the matrix is solid with domains of liquid. The composition of the matrix is richer in Ag at the outside, close to 95% Cu. At the eutectic domains of Cu/Ag with 15% Cu become immersed in a matrix of about 95% Cu/Ag. The entire system is solid so diffusion essentially stops and the structure is locked.
Rapid Quench Morphology
For a rapid quench to T3, domains of 10% Cu form in a matrix of 97% Cu.

## Slide 6
Y. Li, M. Stein, B.-J. Jungnickel, Colloid Polym. Sci. 269, 772 (1991); and ‘Mitteilungen aus dem
Deutschen Kunststoff-Institut’, Nr. 53, April, Darmstadt, 1991
N1 = N2
N1 ≠ N2

## Slide 7
Common Tangent Construction
Does dG/dxi = dG/dni = mi?
Not exactly
dG/dni = dG/dxi dxi/dni
dxi/dni = d(ni/(ni+nj))/dni = 1/(ni+nj) – ni/(ni+nj)2
T3
Solid Solutions
Both have diamond cubic structure

## Slide 8
Si-Ge phase diagram
Si-Ge Gibbs Free Energy
Single crossing of solid/liquid free energy curves

## Slide 9
Pressure Expression: Mix two ideal gasses, A and B
p = pA + pB
pA is the partial pressure pA = xAp
For single component molar G = m
m0 is at p0,A = 1 bar
At pressure pA for a pure component isothermal ideal gas
mA = m0,A + RT ln(p/p0,A) = m0,A + RT ln(p)
For a mixture of A and B with a total pressure ptot = p0,A = 1 bar and pA = xA ptot
For component A in an ideal binary mixture
mA(xA) = m0.A + RT ln (xA ptot/p0,A) = m0.A + RT ln (xA)
-S U V
H A
-p G T
dG=SdT+Vdp
Isothermal and Ideal Gas
dG = RTdp/p
mA* = m0.A if p = 1
Isothermal and Real Gas

## Slide 10
Solve for xBSS xBliq since xA + xB =1
Ideal
Cp(T) is constant
Calculate the Phase Diagram for a Solid Solution
For Ideal you can solve the phase diagram knowing the melting points and heats of fusion.
xA + xB =1

## Slide 12
https://webbook.nist.gov/chemistry/name-ser/

## Slide 13
Solid solution is flatter than ideal (Pos. deviation or destabilized) Liquid is deeper than ideal (Neg. Deviation or stabilized)
Deviations are associated with minima in phase diagram
Double crossing of solid/liquid free energy curves
~1005 K
Congruent Melting

## Slide 14
Solid solution is flatter than ideal (Pos. deviation or destabilized) Liquid is deeper than ideal (Neg. Deviation or stabilized)
Deviations are associated with minima in phase diagram
Phase diagram is split into two solid solutions by the congruent melting point

## Slide 15
Azeotrope
Heteroazeotrope
Liquid/Vapor Equilibria
Ideal
Solid/Liquid Equilibria
Ideal
Eutectic
Non-Ideal
Congruent melting solid solution
Phase diagram is split into two phase diagrams with a special composition that acts as a pure component
Same crystallographic structure in solid solution phase
Different crystallographic structures in solid solution phases
L => a
L => a + b
L => a + L
Liquid/Liquid
Equilibria

## Slide 16
Eutectic Phase Diagram with Three Crystallographic Phases, Two Cubic and One Hexagonal

## Slide 17
Regular Solution Modeling for Phase Diagrams
GE/RT = xA ln gA + xB ln gB Generic expression using activity coefficient
GE/RT = W xA xB Hildebrand Regular Solution expression
Two unknowns & Two equations:
We found that a solution of RT ln gA = W xB2 and RT ln gB = W xA2 worked
Two unknowns, xBSS, xBliq & Two equations
Solve numerically
Generate Phase diagram since Dµ is a function of T
Positive W is necessary for phase separation
DGm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
Knowing 2 omegas and the temperatures and heats of fusion you can predict the phase diagram

## Slide 18
Two Different Crystallographic
Phases at Equilibrium
One Crystallographic
Phase
g => a + b

## Slide 19
Polyvinylmethyl Ether/Polystyrene (LCST Phase behavior)
DGm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
must have a temperature dependence for UCST
W = A + B/T so that it gets smaller with increasing temperature this is a non-combinatorial entropy i.e. ordering on mixing
2-Phase
Single Phase
2-Phase
Single Phase

## Slide 20
Pure A and B melt at 800 and 1000 K with the entropy of fusion of both compounds set to 10 J K–1 mol–1 typical for metals. The interaction coefficients of the two solutions have been varied systematically in order to generate nine different phase diagrams.
Solid & liquid Ideal
Wliq = -15 kJ
Wss = 0
Wliq = 0
Wss = 0
Wliq = +15 kJ
Wss = 0
Congruent melting
Congruent melting

## Slide 21
Pure A and B melt at 800 and 1000 K with the entropy of fusion of both compounds set to 10 J K–1 mol–1 typical for metals. The interaction coefficients of the two solutions have been varied systematically in order to generate nine different phase diagrams.
Solid & liquid Ideal
Wliq = -15 kJ
Wss = 0
Liquid stabilized
Wliq = 0
Wss = 0
Wliq = +15 kJ
Wss = 0
Liquid destablized
congruently melting solid solution
congruently melting solid solution

## Slide 22
Pure A and B melt at 800 and 1000 K with the entropy of fusion of both compounds set to 10 J K–1 mol–1 typical for metals. The interaction coefficients of the two solutions have been varied systematically in order to generate nine different phase diagrams.
Solid destabilized
Wliq = -15
Wss = 15 kJ
Solid destabilized
& liquid stabilized
Wliq = 0 kJ
Wss = 15 kJ
Wliq = +15 kJ
Wss = +15 kJ
Solid & Liquid
destablized
Eutectic
Eutectic

## Slide 23
Pure A and B melt at 800 and 1000 K with the entropy of fusion of both compounds set to 10 J K–1 mol–1 typical for metals. The interaction coefficients of the two solutions have been varied systematically in order to generate nine different phase diagrams.
Solid stabilized
liquid destabilized
Wliq = 0
Wss = -10 kJ
Solid stabilized
Wliq = +10 kJ
Wss = -10 kJ
Wliq = -10 kJ
Wss = -10 kJ
Solid & Liquid
stablized
Congruent melting

## Slide 24
If it is assumed that
Then you need only one W
(The solid state doesn’t mix)
Regular solution model has only a few parameters
This means that experimentally you need only determine a few points of equilibrium composition to predict the entire phase diagram.

## Slide 25
Invariant Phase Equilibria
There are three degrees of freedom for a binary system. If three phases meet the conditions are invariant. This means that the phase composition acts like a pure component. An azeotrope or congruent melting point splits the phase diagram into two phase diagrams. There are several types of “invariant reactions”.
Azeotrope V => L Composition fixed, xi = yi
Congruent melting point L => S Composition fixed, xis = xil
Hex to Cubic Phase transition of Y2O3 Comp. fixed
Peritectic Reaction
Peritectoid = 3 solid phases
Eutectic Reaction
Eutectoid = liquid & 2 solid phases
Monotectic Reaction L1 => S + L2
Syntectic Reaction L1 + L2 => S
F = C – P + 2 for binary F = 4 – P composition diagram holds one DOF constant

## Slide 26
Stoichiometric Intermediate Phase, CaZrO3
Stoichiometric Intermediate Phase
Only stable at one exact composition where it has a very low free energy

## Slide 27
The intermediate phases in the system Si–Ti display also a variety of other features. While TiSi2 and Ti5Si3 are congruently melting phases (melt and crystal have same composition), Ti5Si4 and TiSi melt incongruently. Finally, Ti3Si decomposes to b-Ti and Ti5Si3 at T = 1170 K, in a peritectoid reaction (3 solid phases) while b-Ti decomposes eutectoidally (L and 2S) on cooling forming a-Ti + Ti3Si at T = 862 K.
Intermediate Phases

## Slide 28
Antimony

## Slide 29
Monotectic Phase Diagram
L1 => L2 + a
Self-lubricating bearings
Nano-structure Bi

## Slide 30
Freezing Point Depression
dµB,Solid = VmB,Solid dP – SmB,Solid dT + RT d(lnaB,Solid)
Pure solid in equilibrium with a binary solution following Henry’s Law
Isobaric, pure component B so lnaB,Solid = 0
dµB,Solid = – SmB,Solid dTfp
Binary solution following Henry’s Law
dµB,Solution = – SmB,Solultion dTfp + RTfp d(lnyB,Solution)P,T
For small x: e-x = 1 - x + … or ln(1-x) = -x
So for small yB,Solution: lnyB,Solution ~ -yA,Solution
So, if dµB,Solid = dµB,Solution
SmB,Solid dTfp = SmB,Solution dTfp + RTfp dyA,Solution
dyA,Solution = (SmB,Solid - SmB,Solution)/(RTfp) dTfp ~ -DSmB/(RTfp) dTfp = -DHmB/(RTF) (dTfp)/Tfp
yA,Solution = -DHmB/(RTF) ln(Tfp/TF) For small x: ln(x) = x – 1
yA,Solution = -DHmB/(RTF) (Tfp/TF - 1) = -DHmB/(RT2F) DT
Tfp = TF - yA,SolutionRT2F/DHmB
-S U V
H A
-p G T
dG = Vdp – SdT
dG=-SdT+Vdp
Isothermal and Ideal Gas
dG = RTdp/p
G = RT ln(p/p0) = RT ln(a)
dG = RT d(ln(a))
For solution
dG = RT d(ln(x/x0)) = RT d(ln(x))

## Slide 31
DT = -RT2FyA,Solution/ DHmB

## Slide 32
Ternary Phase Diagram, xA, xB, xC
With no grid you can get the composition
From the normals
Go clockwise
0 at start 1 at corner
Phase point is where parallel lines meet
Plot is isothermal, isobaric, isochoric
xA + xB + xC = 1
This can be read if the plot has a grid
You can also use intersection lines to get the composition

## Slide 34
Predominance Diagram (Which species is dominant)
pH = -log [H+]
pCr = -log [Cr]

## Slide 36
Chapter 18 Electrolytes
Strong Electrolyte NaCl in water (strong dielectric, ions completely formed)
Weak Electrolyte Acetic Acid in water (use dissociation constant)

## Slide 37
Chapter 18 Electrolytes
Handbook of Aqueous Electrolyte Thermodynamics

## Slide 38
Colligative (counting) Properties
Melting Point Depression
Osmotic Pressure P/RT = (c/Mw) (1 + B2 c + …)
Boiling Point Elevation (for non-volatile solute)
yH2O P = P = xH2OPH20Sat

## Slide 42
Speciation and dissociation constant Ka,298, charge balance
aH+ is dimensionless, [H+] is moles/liter (molarity, MH+)
A neutral solution is pure water so aH2O = 1
With temperature changes [H+] changes due to thermal expansion
Molality, number of moles of H+ per kg of H2O is used, mH+

## Slide 44
Concentration with speciation
Acetic Acid in water
Apparent concentration: g/liter you put in of C2H4O2
True concentration has to do with the dissociation species (based on a model)
VLE is based on the true concentration of undissociated species

## Slide 45
pH
pH = -log10(aH+)
aH+ is molal (molar as an approximation)

## Slide 46
Electrolyte Equilibrium Constant
Succinic Acid

## Slide 47
Water of hydration and hydronium ion
Cations have water of hydration associated with the ion
Degree of hydration changes with concentration
At high concentrations ion pairs with the counter ion form

## Slide 48
Acids and conjugate bases

## Slide 49
Strong Acid
[H+] is large so [OH-] is very small, can be ignored
pH ~ pCA

## Slide 50
Strong Base
[OH-] is large so [H+] is very small, can be ignored
pOH ~ pCB

## Slide 51
Weak monoprotic Acid (Acetic Acid pKa,A = 4.7)

## Slide 52
Weak monoprotic Based (Acetate ion pKa,B = 9.3)
Start with sodium acetate which is a strong electrolyte, the resulting acetate ion is a weak base
Convert to an acid equation and work with weak acid

## Slide 53
Acid or Base Added to water

## Slide 54
Acid
Base
Standard acid form of eqn. 18.38
At 298K, Ka,B = 6.18 e-13 from eqn. 18.39
Ka,A = 1e-14/6.18e-13 = 0.0162 or pKa,A = 1.79
Fluconazole is protonated below pH = 1.8 and neutral (undissociated) above
pH = 7
None is dissociated so:

## Slide 55
Acid
Base
Standard acid form of eqn. 18.39
At 298K, Ka,B = 6.18 e-13 from eqn. 18.39
Ka,A = 1e-14/6.18 e-13 = 0.0162 or pKa,A = 1.79
Fluconazole is protonated below pH = 1.8 and neutral (undissociated) above
pH = 1.5
About half is dissociated:

## Slide 56
Sillén Diagram or Bjerrum Plot or Hägg Diagram
4.76 = pKa

## Slide 57
Sillén Diagram

## Slide 60
When [OAc-] = [HOAc] then Ka,A = [H+]
When one component is small the other is CB
Strong Base/Weak Acid, Answer is Basic
In Basic region [H+] << [HOAc]
So [HOAc] ~ [OH-] for solution at pH 8.4
[HOAc] is parallel to [H+] when [H+] is small
[H+]=10-14/[OH-] so [OAc-] is parallel to [OH-] when [OH-] is small
[OH-][H+]=10-14 so log [OH-]+log[H+] = 14 (two lines as drawn)

## Slide 69
Amino Acids (Zwiterions)

## Slide 70
Amino Acids (Zwiterions)

## Slide 72
Charge balance (18.67) is reached about where 1.1[H2Gly+] = [Gly-], a little above pH = 6

## Slide 73
Buffer: a salt and an acid that share a common ion
Acetic Acid and Sodium Acetate
Henderson-Hasselbalch Equation

## Slide 74
Buffer: a salt and an acid that share a common ion
Acetic Acid and Sodium Acetate
Better equation:

## Slide 75
Isoelectric Point
For a zwitterion like an amino acid amines protonate at neutral pH and carboxylic acids are deprotonated. When there is no net charge the pH = pI is the isoelectric point. Solubility is at a minimum at the isoelectric point.

## Slide 76
Ionic Strength (salt concentration)
For low ionic strength, as ionic strength increases, solubility increases (salting in).
For high ionic strength, as ionic strength increases, solubility decreases (salting out).
Maximum solubility at intermediate salt concentrations.
Salting in

## Slide 77
Donnan Equilibria

## Slide 78
Solubility
Solubility and vapor pressure rely on equilibria with the un-ionized species. So solubility depends on pH. Remember, the activity of a solid is 1.
KSLE = 0.0180 at 298K; pH 1.5 [H+] = 0.0316; pH 7 [H+] = 1e-7; Ka = 6.18 e-13; pKa = 1.8 so protonated below pH 1.8 and undissociated above pH 7
From slide 18 example 18.4

## Slide 79
Common ion effect
Add NaCl to a KCl saturated solution causes precipitation

## Slide 80
Redox Reactions OILRIG
Lose or gain electrons
Electrochemical Cell (discharge)
Anode:
Cathode:
3.9 Volts
Oxidation (OIL)
Reduction (RIG)
Reference voltage is platinum electrode:H2(g) electrode at pH = 0; 298K; 1 bar
Reduction of H+ Potential set to 0 as reference

## Slide 82
Redox Reactions OILRIG

## Slide 86
Bioprocess Engineering (Fermentation)
Degree of Reduction
Stoichiometry
Oxidation State
O2 is 0; in products is -2
Moles of electrons transferred to oxygen
The degree of reduction multipliers are +4 for C; +1 for H; -2 for O; -3 for N (ammonia); +6 for S (H2SO4); +5 for P (phosphoric acid)
Reaction of acetaldehyde C2H4O Degree of reduction 2(4)+4(1)+1(-2)=10 or 5 per carbon.
To determine r for O2, 2r(-2) = -10 so r = -2.5 to yield zero on the left of 18.88
On the right of 18.88, For CO2, 1(4)+2(-2) = 0 and for H2O, 2(1)+1(-2) = 0
Two sides balance

## Slide 88
Biological Equilibrium Reactions
Reactions occur with a buffer so [H+] is ignored (indicated by prime)
Water is pure so activity is 1

## Slide 93
Debye-Hückel Model
Mean field

## Slide 94
Debye-Hückel Model
Coulomb’s Law
Work to place an ion in a solution of other ions

## Slide 95
Debye-Hückel Model

## Slide 96
Activity Coefficient of Water
Can be determined by measuring the osmotic pressure

## Slide 97
Chlorination of Water

## Slide 100
Double [H+] makes it about 0.3 higher

## Slide 101
Double [H+] makes it about 0.3 higher

## Slide 103
Mean (Geometric Mean) Ionic Activity Coefficients
Mean Molality:
Mean Ionic Activity Coefficient:
Stoichiometric Number