## Slide 1
Mole fraction of component A = xA
Mass Fraction of component A = mA
Volume Fraction of component A = fA
Typically, we make a binary blend, A + B, with mass fraction, mA, and want volume fraction, fA, or mole fraction , xA.
fA = (mA/rA)/((mA/rA) + (mB/rB))
xA = (mA/MWA)/((mA/MWA) + (mB/MWB))
Solutions

## Slide 2
Solutions
Three ways to get entropy and free energy of mixing
Isothermal free energy expression, pressure expression
Isothermal volume expansion approach, volume expression
From statistical thermodynamics
G = H – TS A = U – ST U = H – PV
Need the Entropy S
-S U V
H A
-p G T

## Slide 3
A. Pressure Expression: Mix two ideal gasses, A and B
p = pA + pB
pA is the partial pressure pA = xAp (Raoult’s Ideal Mixing Law)
For single component molar G = m
m0 is at p0,A = 1 bar
At pressure pA for a pure component isothermal ideal gas
mA = m0,A + RT ln(p/p0,A) = m0,A + RT ln(p)
For a mixture of A and B with a total pressure ptot = p0,A = 1 bar and pA = xA ptot
For component A in a binary mixture
mA(xA) = m0.A + RT ln (xA ptot/p0,A) = m0.A + RT ln (xA)
Notice that xA must be less than or equal to 1, so ln xA must be negative or 0
So, the chemical potential must drop in the solution for a solution to exist.
Ideal gasses only have entropy so entropy drives mixing in this case.
This can be written, xA = exp((mA(xA) - m0.A)/RT)
Which indicates that xA is the Boltzmann probability of finding A
-S U V
H A
-p G T
dG=-SdT+Vdp
Isothermal and Ideal Gas
dG = RTdp/p
G = RT ln(p/p0)
Isothermal ideal gas (no enthalpy)

## Slide 4
Mix two real gasses, A and B
mA* = m0.A if p = 1
Solution
Gas

## Slide 5
Solutions
Three ways to get entropy and free energy of mixing
Isothermal free energy expression, pressure expression
Isothermal volume expansion approach, volume expression
From statistical thermodynamics
G = H – TS A = U – ST U = H – PV
Need the Entropy S
-S U V
H A
-p G T

## Slide 6
For isothermal DU = CV dT = 0 = dQ + dW
dQ = -dW = pdV
For ideal gas dQ = -dW = nRTln(Vf/Vi)
dQ = TDS
DS = nR ln(Vf/Vi)
Consider a process of expansion of a gas from VA to Vtot
The change in entropy is DSA = nARln(Vtot/VA) = - nARln(VA/Vtot)
Consider an isochoric mixing process of ideal gasses A and B.
A is originally in VA and B in VB
Vtot is VA + VB
The change in entropy for mixing of A and B is
DSmixing A and B = - nARln(VA/Vtot) - nBRln(VB/Vtot) = - nR(xAlnxA + xBlnxB)
For an isothermal, isochoric mixture of ideal gasses (also isobaric since P ~ T/V)
For ideal gasses DHmixing = 0 since there is no interaction
DGmixing = DHmixing - TDSmixing = - TDSmixing = nRT(lnxA + lnxB)
So, the molar Gibbs Free energy for mixing is DGmixing = RT(xAlnxA + xBlnxB)
B. Volume Expression: Ideal Gas Mixing
-S U V
H A
-p G T
dU=-pdV+TdS
Isothermal and Ideal Gas
dG = RTdp/p

## Slide 7
Solutions
Three ways to get entropy and free energy of mixing
Isothermal free energy expression, pressure expression
Isothermal volume expansion approach, volume expression
From statistical thermodynamics
G = H – TS A = U – ST U = H – PV
Need the Entropy S
-S U V
H A
-p G T

## Slide 8
C. Statistical Thermodynamics
Boltzmann’s Law: DS = kBlnW
Is the number of states
For mixing of nA and nB with n total molecules
= n!/(nA! nB!)
Sterling’s approximation for large n, n! ~ n ln(n) – n
We assume that n is large then
lnW = -(nA ln(nA/n) + nB ln(nB/n))
DS = -kB (nA ln(nA/n) + nB ln(nB/n)) = -nkB (xA ln(xA) + xB ln(xB))
DGmixing = DHmixing - TDSmixing = - TDSmixing = nRT(xA lnxA + xB lnxB)

## Slide 9
Some Types of Entropy
Thermodynamic entropy measured experimentally, Q/T
Configurational also called Combinatorial
Conformational
Translational and Rotational Entropy (Brownian motion)
Vibrational entropy
Conformational entropy computed in internal or Cartesian coordinates (which can even be different from each other)
Conformational entropy computed on a lattice
Entropy associated with organization on mixing (Hyrophobic effect and many other unexpected features on mixing)

## Slide 10
An “Ideal Solution” means:
The change on mixing:
DS = -nkB (xA ln(xA) + xB ln(xB))
Since (ln x) is always negative or 0, DS is always positive for ideal solutions
DG = -T DS
Since (ln x) is always negative or 0, DG is always negative (or 0) and ideal solutions always mix
DH is 0, there is no interaction in ideal mixtures, there is no excluded volume, particles are ghosts to each other
DV = (dDG/dp)T = 0, there is no loss or gain of volume compared to the summed volume
-S U V
H A
-p G T

## Slide 11
Boltzmann Probability of a Thermally Reversible Event = exp(-DG/kT)
DG is the change in free energy for the event
DG = DH – TDS (Const. T & P, e.g. an experimental measurement)
DA = DU – TDS (Const. T & V, e.g. a simulation on a grid)
Consider an ideal gas with no enthalpic interactions, DH = 0
The probability of finding an atom A in a mixture of A and B is the molar concentration xA
DSA/k = -ln xA from the Boltzmann probability
and
DS/k = - xAln xA - xBln xB by a rule of random mixtures
DGideal/kT = xAln xA + xBln xB this is always negative since “ln” of a number less than 1 is negative, so mixing always reduces the free energy so it always occurs for an ideal mixture
Hildebrandt Real Solution model considers binary interactions.
The odds of a binary interaction of A and B is xAxB
This interaction has an average enthalpy (or internal energy) DH = xAxB WAB or x1x2 A12
Where the first term is the Hildebrandt binary interaction parameter and the second is the Margules one-parameter interaction term. For polymers c12 is used, the Flory –Huggins interaction parameter (with a few modifications).
DGreal solution/kT = x1ln x1 + x2ln x2 + x1x2 A12 = x1ln a1 + x2ln a2 = x1ln g1x1 + x2ln g2x2
DH /kT = DGexcess /kT = x1x1 A12 = x1ln g1 + x2ln g2
-S U V
H A
-p G T

## Slide 12
Excess free energy per mole
GE is the excess free energy value, so nGE
The excess chemical potential of component “i” in phase L or V, miE is given by
This is how you can find the activity coefficients from the Margules one-parameter coefficient (or the Hildebrandt or Flory-Huggins interaction parameters)

## Slide 13
Real Solutions
Molar excess functions or departure functions:
Difference between real value and ideal value
Excess DGmixing = DGmixing - RT(xAlnxA + xAlnxB)
Excess DSmixing = DSmixing + R(xAlnxA + xAlnxB)
Excess DHmixing = DHmixing
Excess DVmixing = DVmixing

## Slide 14
Real Solutions
xA becomes aA the activity so
DGmixing = RT(xAlnaA + xAlnaB)
Excess DGmixing = DGmixing - RT(xAlnxA + xBlnxB)
= RT(xAln(aA/xA) + xBln(aB/xB) )
= RT(xAln(gA) + xBln(gB))
g Is the activity coefficient
Excess DSmixing = -R(xAln(gA) + xBln(gB))
Method to use departure functions for calculations (PREOS.xls)
Calculation of properties in the ideal state is simple
With an equation of state the departure function can be calculated
For any transition first calculate the departure function to the ideal state
Then carry out the desired change as an ideal mixture or gas
Then use the departure function to return to the real state

## Slide 15
DGmixing = nRT(xA lnaA + xB lnaB)
= RT(xAln(gA) + xAln(gB))

## Slide 16
Get the activity coefficient at infinite dilution by extrapolating the slope for pure component to x = 0
This is used for Henry’s Law and a few other places.
(Activity coefficient is a/x)
a = gx so da/dx = g

## Slide 17
We want the infinite dilution activity coefficients to write a function to predict the activity and the activity coefficient.
This is one of the parameters for the functions.
With the function for activity we can predict the free energy and the miscibility.

## Slide 18
Henry’s law for dilute solutions
Vapor pressure of solute = ki xi
ki is the Henry’s Law Constant
xi is the solute molar fraction (low ~0)
Raoult’s Law for solvent or ideal mixtures
Vapor pressure = p* xj
xj is the solvent molar fraction (high ~1)
p* is the vapor pressure of the pure solvent
Solute
Solvent or ideal mixture
If a solution is ideal, then xA = aA and gA = 1
At infinite dilution a solvent is ideal (follows Raoult’s law) so
(daA/dxA)xA =>1 = 1 = (dgAxA/dxA)xA =>1 = gA + xA(dgA/dxA)xA =>1
But gA = 1 at xA = 1, then Raoult’s law is followed if
(dgA/dxA)xA =>1 => 0 (See next slide)
A solute follows Henry’s Law if
(daB/dxB)xB =>0 = gB infinite dilution
= (dgBxB/dxB)xB =>0 = (gB + xB(dgB/dxB))xB =>0
So
(xB(dgB/dxB))xB =>0 = 0
This isn’t that useful

## Slide 19
Henry’s law for dilute solutions
Vapor pressure of solute = ki xi
Raoult’s Law for solvent or ideal mixtures
Vapor pressure = p* xj

## Slide 20
Activity of a component in a solution must be defined relative to a standard state, either Henrian (extrapolated) or Raoultian (measured, x = 1 :: a = 1)
You would use Henrian standard state if the solute had limited solubility like PCBs or oil in water and you wanted the infinite dilution of the water component

## Slide 21
Analytic Solution Models
Want to calculate the miscibility of components
Need to generate a phase diagram
Calculation of the vapor pressure
Simplest approach could be a polynomial. However, this generally doesn’t inherently have any real meaning. The polynomial just reproduces existing data within experimental limits. Extrapolation is dangerous.
Symmetric Feature: Phase behavior
Asymmetric feature: vapor pressure

## Slide 22
Excess DSmixing = -R(xAln(gA) + xAln(gB))
Excess DGmixing = RT(xAln(gA) + xAln(gB))
Interaction coefficients
Zeroth order infinite dilution (trivial)
First order e1B self-interaction coefficient
This is similar to a virial expansion

## Slide 23
Thallium/Mercury
Lower freezing point of Mercury for thermometer and switches 8.5% -60°C versus -40°C
Also Rat poison

## Slide 24
Hildebrand Regular Solution Model
The change on mixing:
DS = -nkB (xA ln(xA) + xB ln(xB)) Ideal Solution
Since (ln x) is always negative or 0, DS is always positive for ideal solutions
DG = DH -T DS
Since (ln x) is always negative or 0, DG is positive or negative depending on DH :: can mix or demix
Depending on the sign of DH
DV = (dDG/dp)T = 0, there is no loss or gain of volume compared to the summed volume
DH = n W xAxB
is the interaction coefficient or regular solution constant
Molar Gibbs free energy of mixing
DGm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
W = zNA[uAB – (uAA+uBB)/2]
The equation is symmetric

## Slide 25
Hildebrand solubility parameter, d
DH = n W xAxB
is the interaction coefficient or regular solution constant
Molar Gibbs free energy of mixing
Gm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
= zNA[uAB – (uAA+uBB)/2]
Flory-Huggins chi parameter, ~W/kT
Hansen solubility parameters

## Slide 26
Hildebrand Solubility Parameter, d
Two materials with similar d are miscible
Luo Y, Chen X, Wu S, Ca S Luo Z, Shi Y, Molecular Dynamics Simulation Study on Two-Component Solubility Parameters of Carbon Nanotubes and Precisely Tailoring the Thermodynamic Compatibility between Carbon Nanotubes and Polymers, Langmuir 36 9291-9305 (2020).
Flory-Huggins Equation
c ~ 1/T
Hildebrand and Scratchard
London dispersion forces (attractive)

## Slide 27
Asymmetric equations for asymmetric phase diagram
Sub-regular solution model
Redlich-Kister Expression

## Slide 30
Non-ideal entropy of mixing
Quasi-regular solution model
This is a non-combinatorial entropy
This would occur if there were ordering on mixing, say when you add oil to water. The enthalpy of mixing favors mixing!!! Water organizes at the surface of oil to a great extent; this reduces entropy and makes oil and water demix. Water actually “likes” oil.
This is called the “hydrophobic effect” and is an important concept for protein folding.

## Slide 31
Graphical Method to Estimate Chemical Potential
Does dG/dxi = dG/dni = mi?
No
dG/dni = dG/dxi dxi/dni
dxi/dni = d(ni/(ni+nj))/dni = 1/(ni+nj) – ni/(ni+nj)2

## Slide 32
Solving the Regular Solution Model
We know that the excess Gibbs free energy for mixing is given by:
GE/RT = xA ln gA + xB ln gB Generic expression using activity coefficient
And we have defined for the regular solution model that
GE/RT = W xA xB Hildebrand Regular Solution expression
If we propose the answer RT ln gA = W xB2
We find by substitution generic expression that it equals the regular solution expression since xB + xA = 1
(Solving this directly see next slide.)

## Slide 34
Use of the Gibbs-Duhem Equation to determine the activity of a component
Constant p, T
If you know gA you can obtain gB by integration
Restatement of Gibbs-Duhem for Solutions