- ASTRA 6 Report PNIPAAm_2-4-15

File Name: C:\Documents and Settings\Ayres Research Group\My Documents\Emily\Other's research\PNIPAAm_2-4-15.afe6 
Collection Operator: AYRESGPC\Ayres Research Group (AYRESGPC\Ayres Research Group (Ayres Research Group)) 
Processing Operator: AYRESGPC\Ayres Research Group (Ayres Research Group)

- Sample: sample

Concentration: 0.000 mg/mL

- Configuration

Concentration Source: RI 
Flow Rate: 1.000 mL/min

- Light Scattering Instrument: miniDAWN TREOS

Band Broadening Correction: Yes (Instrumental: 37.238 μL, Mixing: 76.699 μL) 
Cell Type: Fused Silica 
Wavelength: 656.0 nm 
Calibration Constant: 6.1272×10-5 1/(V cm)

| Detector | Scattering angle | Gain | Normalization coefficient |
| --- | --- | --- | --- |
| 1 | 46.6º | n/a | 0.764 |
| 2 | 90.0º | n/a | 1.000 |
| 3 | 133.4º | n/a | 0.810 |

- RI Instrument: Optilab rEX

Band Broadening Correction: Yes (Instrumental: 27.923 μL, Mixing: 0.732 μL) 
Wavelength: 658.0 nm

- Viscometer: ViscoStar

Band Broadening Correction: n/a 
Dilution Factor: 0.4976

- Solvent: thf

Refractive Index: 1.402

| Fluid Connections |  |  |
| --- | --- | --- |
| Source Instrument | Destination Instrument | Delay Volume (mL) |
| Generic Pump | Injector | 0.000 |
| Injector | Generic Column | 0.000 |
| Generic Column | miniDAWN TREOS | 0.000 |
| miniDAWN TREOS | ViscoStar | 0.359 |
| ViscoStar | Optilab rEX | 0.107 |

- Processing

Collection Time: Wednesday February 04, 2015 02:58:25 PM Eastern Daylight Time 
Processing Time: Wednesday February 04, 2015 03:32:49 PM Eastern Daylight Time

- Basic Collection:

LS Instrument Collection Interval: 1.000 sec

- Baselines:

| Series | Start | Stop | Type |
| --- | --- | --- | --- |
| detector 1 | (18.345, 0.043) | (24.436, 0.043) | manual x, auto y |
| detector 2 | (13.243, 0.029) | (28.661, 0.029) | manual x, auto y |
| detector 3 | (11.136, 0.043) | (27.575, 0.043) | manual x, auto y |
| differential refractive index data | (13.501, 0.000) | (29.337, 0.000) | manual x, auto y |
| Differential Pressure | (9.072, -0.000) | (28.202, -0.000) | manual x, auto y |

- Peak settings:

| Peak Name | Peak 1 |
| --- | --- |
| Light Scattering Model | Zimm |
| Fit Degree | 1 |
| dn/dc (mL/g) | 0.1588 |
| A2 (mol mL/g²) | 0.000 |
| Viscometry Model | Huggins |
| Huggins Equation Parameter | 0 |
| Kraemers Equation Parameter | 0 |

- Results Fitting Procedure:

| Data | Fit Model | Degree | R2 | Extrapolation |
| --- | --- | --- | --- | --- |

- Results

| Peak Results |  |
| --- | --- |
|  | Peak 1 |
| Hydrodynamic radius (v) moments (nm) |  |
| Rh(v)n | 2.353 (±1.547%) |
| Rh(v)w | 2.382 (±1.467%) |
| Rh(v)z | 2.407 (±1.419%) |
| Rh(v)(avg) | 2.370 (±0.073%) |
| Masses |  |
| Calculated Mass (µg) | 396.01 |
| Molar mass moments (g/mol) |  |
| Mn | 6.547×103 (±3.812%) |
| Mp | 6.854×103 (±1.417%) |
| Mv | 6.702×103 (±0.371%) |
| Mw | 6.754×103 (±3.791%) |
| Mz | 6.918×103 (±8.491%) |
| Mz+1 | 7.051×103 (±13.484%) |
| M(avg) | 6.406×103 (±0.076%) |
| Polydispersity |  |
| Mw/Mn | 1.032 (±5.376%) |
| Mz/Mn | 1.057 (±9.307%) |
| rms radius moments (nm) |  |
| Rn | n/a |
| Rw | n/a |
| Rz | n/a |
| R(avg) | n/a |
| Intrinsic viscosity moments (mL/g) |  |
| [η]n | 12.722 (±2.208%) |
| [η]w | 12.75 (±1.80%) |
| [η]z | 12.803 (±1.537%) |
| [η](avg) | 12.569 (±0.092%) |

Mark-Houwink-Sakurada a: 0.432 (±1.854%) 
Mark-Houwink-Sakurada K: 2.753×10-1 (±7.103%) mL/g