051020  Quiz 4  Introduction to Polymers (Chemistry)

This week we looked at synthesis of a polyester network polymer "glyptal", Carother and Flory/Stockmayer (Miller/Macosko)'s interpretation of network formation and the swelling of a hydrogel (sodium polyacrylate).

1)  PET or PETE is a polyester.  Propose a synthesis for PETE based on the synthesis of glyptal in class.

For your synthesis propose

i) monomer(s),

ii) reaction conditions (temperature etc.) and

iii) suggest the PDI that might result from this synthesis.

iv) How might you qualitatively monitor the extent of reaction, p, in this system?

2)  	i) If a network polymer was desired what monomer could be added to your PET synthesis?

ii) What would be the average functionality, <favg> for this system (write an equation)?

iii) Using the Carothers equation what would be the critical extent of reaction based on your equation for average functionality?

3)  	i)  How would you measure/observe when the system forms a gel? (Define a gel)  That is how did we determine the system was a gel in class?  (Sketch a plot of this versus reaction time).

ii)  Give three definitions of a gel based on molecular weight and topology (network structure).  These are due to Carothers; Miller/Macosko; and Flory/Stockmayer.

iii)  Percolation is a feature of many disordered, complex systems.  Percolation was first seriously considered in polymers by Flory and Stockmeyer.  Explain in your own terms what "percolation of a network" means .

4)  The hydrogel we observed in class can swell more than 100 times its volume with water.  The plot below, from Flory's first book, shows the swelling behavior of an early polyacrylic acid hydrogel as a function of the degree of ionization and molecular weight between crosslinks, n.

i) Explain in your own words this behavior.

ii)Guess at the reason for the plateau in swelling ratio.

iii) Why does salt make the hydrogel deswell?

ANSWERS:                 051020  Quiz 4  Introduction to Polymers (Chemistry)

1)  i)  You would use terephthalic acid and ethylene glycol in a condensation reaction,

iii) PDI = 2 for condensation

iv) As the reaction proceeds water is produced and acid is consumed so the reaction could be monitored by the pH of the system.

2)  i)  Glycerol (glycerin) can be added to give branching.

ii) If the mole fractions of terephthalic acid, ethylene glycol and glycerin are A, B and C, then the average functionality is <favg> = 2 (A+B) + 3*C

iii) pc = 2/<favg>.  If C = 0.1 then <favg> = 2.1 and pc = 0.95 .

3)  i) The (low shear rate) viscosity becomes infinite for a gel as shown in Flory's Plot.

ii) Carothers:  n1 => infinity

Miller/Macosko: nw => infinity

Flory/Stockmayer:  => 1

where  is a way to measure when you have reached the percolation threshold, that is when the network connects across the sample.   is the average number of bonds a crosslink site sees in looking away from a networked chain.