## Slide 1
Long Range Interactions

## Slide 2
Long-Range Interactions
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End to End Distance R
By Comparison The Energy to stretch a Thermally Equilibrated Chain Can be Written
For a Chain with Long-Range Interactions There is and Additional Term
So,
Flory-Krigbaum Theory
Result is called a Self-Avoiding Walk
The Secondary Structure for Synthetic Polymers
Number of pairs

## Slide 4
Linear Polymer Chains have Two Possible Secondary Structure States:
Self-Avoiding Walk
Good Solvent
Expanded Coil
(The Normal Condition in Solution)
Gaussian Chain
Random Walk
Theta-Condition
Brownian Chain
(The Normal Condition in the Melt/Solid)
The Secondary Structure for Synthetic Polymers
These are statistical features. That is, a single simulation of a SAW and a GC could look identical.

## Slide 5
Linear Polymer Chains have Two Possible Secondary Structure States:
Self-Avoiding Walk
Good Solvent
Expanded Coil
(The Normal Condition in Solution)
Gaussian Chain
Random Walk
Theta-Condition
Brownian Chain
(The Normal Condition in the Melt/Solid)
The Secondary Structure for Synthetic Polymers
Consider going from dilute conditions, c < c*, to the melt by increasing concentration.
The transition in chain size is gradual not discrete.
Synthetic polymers at thermal equilibrium accommodate concentration changes through a scaling transition. Primary, Secondary, Tertiary Structures.

## Slide 7
We have considered an athermal hard core potential
But Vc actually has an inverse temperature component associated with enthalpic interactions between monomers and solvent molecules
The interaction energy between a monomer and the polymer/solvent system is on average <E(R)> for a given end-to-end distance R (defining a conformational state). This modifies the probability of a chain having an end-to-end distance R by the Boltzmann probability,
<E(R)> is made up of pp, ps, ss interactions with an average change in energy on solvation of a polymer Δε = (εpp+εss-2εps)/2
For a monomer with z sites of interaction we can define a unitless energy parameter
χ = zΔε/kT that reflects the average enthalpy of interaction per kT for a monomer

## Slide 8
For a monomer with z sites of interaction we can define a unitless energy parameter
χ = zΔε/kT that reflects the average enthalpy of interaction per kT for a monomer
The volume fraction of monomers in the polymer coil is nVc/R3
And there are n monomers in the chain with a conformational state of end-to-end distance R so,
We can then write the energy of the chain as,
This indicates that when χ = ½ the coil acts as if it were an ideal chain, excluded volume disappears. This condition is called the theta-state and the temperature where χ = ½ is called the theta-temperature. It is a critical point for the polymer coil in solution.

## Slide 11
Flory-Huggins Equation
Miscibility Limit
Binodal
Spinodal
Critical Point
All three equalities apply
At the critical point
http://rkt.chem.ox.ac.uk/lectures/liqsolns/regular_solutions.html

## Slide 13
Tc = θ(1-2Φc)
Linear Relationship

## Slide 14
Consider also Φ* which is the coil composition, generally below the critical composition for normal n or N
Overlap Composition

## Slide 15
Overlap Composition
Φ*
Both Φ* and Φc depend on 1/√N
Below Φ* the composition is fixed since the coil can not be diluted!

## Slide 16
Overlap Composition
Φ*
Both Φ* and Φc depend on 1/√N
Below Φ* the composition is fixed since the coil can not be diluted!
So there is a regime of coil collapse below the binodal at Φ* in composition and temperature
Coil
Collapse

## Slide 17
Overlap Composition
Φ*
Both Φ* and Φc depend on 1/√N
Below Φ* the composition is fixed since the coil can not be diluted!
So there is a regime of coil collapse below the binodal at Φ* in composition and temperature
Coil
Collapse
Phase
Separation
Θ
Coil
GS-Coil

## Slide 18
For a polymer in solution there is an inherent concentration to the chain
since the chain contains some solvent
The polymer concentration is Mass/Volume, within a chain
When the solution concentration matches c* the chains “overlap”
Then an individual chain is can not be resolved and the chains entangle
This is called a concentrated solution, the regime near c* is called semi-dilute
and the regime below c* is called dilute

## Slide 19
In concentrated solutions with chain overlap
chain entanglements lead to a higher solution viscosity
J.R. Fried Introduction to Polymer Science

## Slide 20
Lower-Critical Solution Temperature (LCST)
Polymers can order or disorder on mixing leading to a noncombinatorial entropy term, A in the interaction parameter.
If the polymer orders on mixing then A is positive and the energy is lowered.
If the polymer-solvent shows a specific interaction then B can be negative.
This Positive A and Negative B favors mixing at low temperature and demixing at high temperature, LCST behavior.

## Slide 21
Lower-Critical Solution Temperature (LCST)
Poly vinyl methyl ether/Water
PVME/PS

## Slide 22
Coil Collapse Following A. Y. Grosberg and A. R. Khokhlov “Giant Molecules”
Grosberg uses:
Rather than the normal definition used by Flory:
What Happens to the left of the theta temperature?

## Slide 24
Generally B is negative and C is positive, i.e. favors coil collapse
So C is important below the theta temperature to model the coil to globule transition
For simplicity we ignore higher order terms because C is enough to give the gross features
Of this transition. Generally it is known that this transition can be either first order for
Biopolymers such as protein folding, or second order for synthetic polymers.
First order means that the first derivative of the free energy is not continuous, i.e. a jump in
Free energy at a discrete transition temperature, such as a melting point.

## Slide 25
Φ*
Coil
Collapse
Phase
Separation
Θ
Coil
GS-Coil
Consider the coil of length n as composed of g* chain subunits each with (n/g*) Kuhn units of length lk. g* can be any value between one and n.
Small size g* units have a lower Tc compared to large size g* units.

## Slide 26
Blob model for coil collapse
Assume Gaussian
Collection of
Blobs

## Slide 28
Ratio of C/B determines behavior, the collapsed coil is 3d

## Slide 31
Generally it is known that this transition can be either first order for
Biopolymers such as protein folding, or second order for synthetic polymers.
First order means that the first derivative of the free energy is not continuous, i.e. a jump in
Free energy at a discrete transition temperature, such as a melting point.

## Slide 33
Size of a Chain, “R”
(You can not directly measure the End-to-End Distance)

## Slide 34
What are the measures of Size, “R”, for a polymer coil?
Radius of Gyration, Rg
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf

## Slide 35
What are the measures of Size, “R”, for a polymer coil?
Radius of Gyration, Rg
2.45 Rg = Reted
Rg is a direct measure of the end-to-end distance for a Gaussian Chain
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf

## Slide 36
Static Light Scattering for Rg
Guinier’s Law
Guinier Plot linearizes this function
The exponential can be expanded at low-q and linearized to make a Zimm Plot

## Slide 37
Zimm Plot
Concentration part will be described later

## Slide 54
Static Light Scattering for Radius of Gyration
Guinier’s Law
Beaucage G J. Appl. Cryst. 28 717-728 (1995).
Lead Term is
A particle with no surface
Consider binary interference at a distance “r” for a particle with arbitrary orientation
Rotate and translate a particle so that two points separated by r lie in the particle for all rotations
and average the structures at these different orientations
Binary Autocorrelation
Function
Scattered Intensity is the Fourier Transform of
The Binary Autocorrelation Function

## Slide 55
Debye Scattering Function for Gaussian Polymer Coil

## Slide 57
Low-q and High-q Limits of Debye Function
At high q the last term => 0
Q-1 => Q
g(q) => 2/Q ~ q-2
Which is a mass-fractal scaling law with df = 2
At low q the last term => 1-Q+Q2/2-Q3/6+…
Bracketed term => Q2/2-Q3/6+…
g(q) => 1-Q/3+… ~ exp(-Q/3) = exp(-q2Rg2/3)
Which is Guinier’s Law

## Slide 58
Ornstein-Zernike Function, Limits and Related Functions
The Zimm equation involves a truncated form of the Guinier Expression intended
For use at extremely low-qRg:
If this expression is generalized for a fixed composition and all q, Rg is no longer
the size parameter and the equation is empirical (no theoretical basis) but has a form
similar to the Debye Function for polymer coils:
This function is called the Ornstein-Zernike function and ξ is called a correlation length.
The inverse Fourier transform of this function can be solved and is given by
(Benoit-Higgins Polymers and Neutron Scattering p. 233 1994):
This function is empirical and displays the odd (impossible) feature that the correlation
function for a “random” system is not symmetric about 0, that is + and – values for r
are not equivalent even though the system is random. (Compare with the “normal
behavior of the Guinier correlation function.)

## Slide 59
Ornstein-Zernike Function, Limits and Related Functions
Low-q limit
High-q limit
Ornstein-Zernike (Empirical)
Debye (Exact)

## Slide 60
Ornstein-Zernike Function, Limits and Related Functions
Empirical Correlation Function
Transformed Empirical Scattering Function
Ornstein-Zernike Function
Debye-Bueche Function
Teubner-Strey Function
Sinha Function
c2 is negative to create a peak
Correlation function in all of these cases is not symmetric about 0 which is physically impossible for a random system. The resulting scattering functions can be shown to be non-physical, that is they do not follow fundamental rules of scattering. Fitting parameters have no physical meaning.

## Slide 62
Measurement of the Hydrodynamic Radius, Rh
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
Kirkwood, J. Polym. Sci. 12 1(1953).
http://theor.jinr.ru/~kuzemsky/kirkbio.html

## Slide 64
Intrinsic, specific & reduced “viscosity”
Shear Flow (may or may not exist in a capillary/Couette geometry)
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
We can approximate (1) as:
Martin Equation
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1

## Slide 65
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Concentration Effect

## Slide 66
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Concentration Effect, c*

## Slide 67
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Solvent Quality

## Slide 68
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Molecular Weight Effect

## Slide 71
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
Temperature Effect

## Slide 72
Intrinsic, specific & reduced “viscosity”
n = order of interaction (2 = binary, 3 = ternary etc.)
(1)
We can approximate (1) as:
Martin Equation
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1
Huggins Equation
Kraemer Equation
(exponential expansion)

## Slide 73
Intrinsic “viscosity” for colloids (Simha, Case Western)
For a solid object with a surface v is a constant in molecular weight, depending only on shape
For a symmetric object (sphere) v = 2.5 (Einstein)
For ellipsoids v is larger than for a sphere,
J = a/b
prolate
oblate
a, b, b :: a>b
a, a, b :: a<b

## Slide 74
Intrinsic “viscosity” for colloids (Simha, Case Western)
Hydrodynamic volume for “bound” solvent
Partial Specific Volume
Bound Solvent (g solvent/g polymer)
Molar Volume of Solvent

## Slide 75
Intrinsic “viscosity” for colloids (Simha, Case Western)
Long cylinders (TMV, DNA, Nanotubes)
J=L/d
End Effect term ~ 2 ln 2 – 25/12 Yamakawa 1975

## Slide 76
Shear Rate Dependence for Polymers
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)
Capillary Viscometer

## Slide 77
Branching and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 78
Branching and Intrinsic Viscosity
Utracki and Jamieson “Polymer Physics From Suspensions to Nanocomposites and Beyond” 2010 Chapter 1

## Slide 79
Polyelectrolytes and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 80
Polyelectrolytes and Intrinsic Viscosity
Kulicke & Clasen “Viscosimetry of Polymers and Polyelectrolytes (2004)

## Slide 81
Hydrodynamic Radius from Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HydrodyamicRadius.pdf
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/HiemenzRajagopalanDLS.pdf

## Slide 82
Consider motion of molecules or nanoparticles in solution
Particles move by Brownian Motion/Diffusion
The probability of finding a particle at a distance x from the starting point at t = 0 is a Gaussian Function that defines the diffusion Coefficient, D
A laser beam hitting the solution will display a fluctuating scattered intensity at “q” that varies with q since the particles or molecules move in and out of the beam
I(q,t)
This fluctuation is related to the diffusion of the particles
The Stokes-Einstein relationship states that D is related to RH,

## Slide 83
For static scattering p(r) is the binary spatial auto-correlation function
We can also consider correlations in time, binary temporal correlation function
g1(q,τ)
For dynamics we consider a single value of q or r and watch how the intensity changes with time
I(q,t)
We consider correlation between intensities separated by t
We need to subtract the constant intensity due to scattering at different size scales
and consider only the fluctuations at a given size scale, r or 2π/r = q

## Slide 84
Dynamic Light Scattering
a = RH = Hydrodynamic Radius
The radius of an equivalent sphere following Stokes’ Law

## Slide 85
Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
my DLS web page
Wiki
http://webcache.googleusercontent.com/search?q=cache:eY3xhiX117IJ:en.wikipedia.org/wiki/Dynamic_light_scattering+&cd=1&hl=en&ct=clnk&gl=us
Wiki Einstein Stokes
http://webcache.googleusercontent.com/search?q=cache:yZDPRbqZ1BIJ:en.wikipedia.org/wiki/Einstein_relation_(kinetic_theory)+&cd=1&hl=en&ct=clnk&gl=us

## Slide 86
Diffusing Wave Spectroscopy (DWS)
Will need to come back to this after introducing dynamics
And linear response theory
http://www.formulaction.com/technology-dws.html

## Slide 87
Static Scattering for Fractal Scaling

## Slide 91
For qRg >> 1
df = 2

## Slide 92
Ornstein-Zernike Equation
Has the correct functionality at high q
Debye Scattering Function =>
So,

## Slide 93
Ornstein-Zernike Equation
Has the correct functionality at low q
Debye =>
The relatoinship between Rg and correlation length differs for the two regimes.

## Slide 95
How does a polymer chain respond to external perturbation?

## Slide 96
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End to End Distance R
By Comparison The Energy to stretch a Thermally Equilibrated Chain Can be Written
Force
Force
Assumptions:
-Gaussian Chain
-Thermally Equilibrated
-Small Perturbation of Structure (so it is still Gaussian after the deformation)

## Slide 97
Tensile Blob
For weak perturbations of the chain
Application of an external stress to the ends of a chain create a transition size where the coil goes from Gaussian to Linear called the Tensile Blob.
For Larger Perturbations of Structure
-At small scales, small lever arm, structure remains Gaussian
-At large scales, large lever arm, structure becomes linear
Perturbation of Structure leads to a structural transition at a size scale

## Slide 98
For sizes larger than the blob size the structure is linear, one conformational state so the conformational entropy is 0. For sizes smaller the blob has the minimum spring constant so the weakest link governs the mechanical properties and the chains are random below this size.

## Slide 99: Semi-Dilute Solution Chain Statistics

## Slide 100
In dilute solution the coil contains a concentration c* ~ 1/[η]
for good solvent conditions
At large sizes the coil acts as if it were in a concentrated solution (c>>>c*), df = 2. At small sizes the coil acts as if it were in a dilute solution, df = 5/3. There is a size scale, ξ, where this “scaling transition” occurs.
We have a primary structure of rod-like units, a secondary structure of expanded coil and a tertiary structure of Gaussian Chains.
What is the value of ξ?
ξ is related to the coil size R since it has a limiting value of R for c < c* and has a scaling relationship with the reduced concentration c/c*
There are no dependencies on n above c* so (3+4P)/5 = 0 and P = -3/4
For semi-dilute solution the coil contains a concentration c > c*

## Slide 101
Coil Size in terms of the concentration
This is called the “Concentration Blob”

## Slide 102
Three regimes of chain scaling in concentration.

## Slide 103
Thermal Blob
Chain expands from the theta condition to fully expanded gradually.
At small scales it is Gaussian, at large scales expanded (opposite of concentration blob).

## Slide 104
Thermal Blob

## Slide 105
Thermal Blob
Energy Depends on n, a chain with a mer unit of length 1 and n = 10000
could be re cast (renormalized) as a chain of unit length 100 and n = 100
The energy changes with n so depends on the definition of the base unit
Smaller chain segments have less entropy so phase separate first.
We expect the chain to become Gaussian on small scales first.
This is the opposite of the concentration blob.
Cooling an expanded coil leads to local chain structure collapsing to a Gaussian structure first.
As the temperature drops further the Gaussian blob becomes larger until the entire chain is
Gaussian at the theta temperature.

## Slide 106
Thermal Blob
Flory-Krigbaum Theory yields:
By equating these:

## Slide 108
Fractal Aggregates and Agglomerates

## Slide 109
Polymer Chains are Mass-Fractals
RRMS = n1/2 l
Mass ~ Size2
3-d object
Mass ~ Size3
2-d object
Mass ~ Size2
1-d object
Mass ~ Size1
df-object
Mass ~ Sizedf
This leads to odd properties:
density
For a 3-d object density doesn’t depend on size,
For a 2-d object density drops with Size
Larger polymers are less dense

## Slide 112
Tortuosity
Connectivity
How Complex Mass Fractal Structures
Can be Decomposed
z
df
p
dmin
s
c
R/d
27
1.36
12
1.03
22
1.28
11.2

## Slide 114
Disk
Random Coil
Extended β-sheet
(misfolded protein)
Unfolded Gaussian chain

## Slide 115
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates

## Slide 116
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
http://www.phys.ksu.edu/personal/sor/publications/2001/light.pdf
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.koboproductsinc.com/Downloads/PS-Measurement-Poster-V40.pdf

## Slide 117
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.koboproductsinc.com/Downloads/PS-Measurement-Poster-V40.pdf

## Slide 118
For static scattering p(r) is the binary spatial auto-correlation function
We can also consider correlations in time, binary temporal correlation function
g1(q,τ)
For dynamics we consider a single value of q or r and watch how the intensity changes with time
I(q,t)
We consider correlation between intensities separated by t
We need to subtract the constant intensity due to scattering at different size scales
and consider only the fluctuations at a given size scale, r or 2π/r = q

## Slide 119
Dynamic Light Scattering
a = RH = Hydrodynamic Radius

## Slide 120
Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/DLS.pdf
my DLS web page
Wiki
http://webcache.googleusercontent.com/search?q=cache:eY3xhiX117IJ:en.wikipedia.org/wiki/Dynamic_light_scattering+&cd=1&hl=en&ct=clnk&gl=us
Wiki Einstein Stokes
http://webcache.googleusercontent.com/search?q=cache:yZDPRbqZ1BIJ:en.wikipedia.org/wiki/Einstein_relation_(kinetic_theory)+&cd=1&hl=en&ct=clnk&gl=us

## Slide 121
Gas Adsorption
http://www.chem.ufl.edu/~itl/4411L_f00/ads/ads_1.html
A + S <=> AS
Adsorption
Desorption
Equilibrium
=

## Slide 122
Gas Adsorption
http://www.chem.ufl.edu/~itl/4411L_f00/ads/ads_1.html
Multilayer adsorption

## Slide 123
http://www.eng.uc.edu/~gbeaucag/Classes/Nanopowders/GasAdsorptionReviews/ReviewofGasAdsorptionGOodOne.pdf

## Slide 124
From gas adsorption obtain surface area by number of gas atoms times an area for the adsorbed gas atoms in a monolayer
Have a volume from the mass and density.
So you have S/V or V/S
Assume sphere S = 4πR2, V = 4/3 πR3
So dp = 6V/S
Sauter Mean Diameter dp = <R3>/<R2>

## Slide 125
Log-Normal Distribution
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Geometric standard deviation and geometric mean (median)
Mean
Gaussian is centered at the Mean and is symmetric. For values that are positive (size) we need an asymmetric distribution function that has only values for greater than 1. In random processes we have a minimum size with high probability and diminishing probability for larger values.
http://en.wikipedia.org/wiki/Log-normal_distribution

## Slide 126
Log-Normal Distribution
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Geometric standard deviation and geometric mean (median)
Mean
Static Scattering Determination of Log Normal Parameters

## Slide 127
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
-Dynamic Light Scattering
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf

## Slide 128
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
-Particle counting from TEM
-Gas adsorption V/S => dp
-Static Scattering Rg, dp
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Smaller Size = Higher S/V
(Closed Pores or similar issues)

## Slide 129
Fractal Aggregates and Agglomerates
Primary Size for Fractal Aggregates
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Fractal Aggregate Primary Particles

## Slide 130
Fractal Aggregates and Agglomerates
http://www.eng.uc.edu/~gbeaucag/Classes/Nanopowders/AggregateGrowth.pdf
Aggregate growth
Some Issues to Consider for Aggregation/Agglomeration
Path of Approach, Diffusive or Ballistic (Persistence of velocity for particles)
Concentration of Monomers
persistence length of velocity compared to mean separation distance
Branching and structural complexity
What happens when monomers or clusters get to a growth site:
Diffusion Limited Aggregation
Reaction Limited Aggregation
Chain Growth (Monomer-Cluster), Step Growth (Monomer-Monomer to Cluster-Cluster) or a Combination of Both (mass versus time plots)
Cluster-Cluster Aggregation
Monomer-Cluster Aggregation
Monomer-Monomer Aggregation
DLCA Diffusion Limited Cluster-Cluster Aggregation
RLCA Reaction Limited Cluster Aggregation
Post Growth: Internal Rearrangement/Sintering/Coalescence/Ostwald Ripening

## Slide 131
Fractal Aggregates and Agglomerates
Aggregate growth
Consider what might effect the dimension of a growing aggregate.
Transport Diffusion/Ballistic
Growth Early/Late (0-d point => Linear 1-d => Convoluted 2-d => Branched 2+d)
Speed of Transport Cluster, Monomer
Shielding of Interior
Rearrangement
Sintering
Primary Particle Shape
DLA df = 2.5 Monomer-Cluster (Meakin 1980 Low Concentration)
DLCA df = 1.8 (Higher Concentration Meakin 1985)
Ballistic Monomer-Cluster (low concentration) df = 3
Ballistic Cluster-Cluster (high concentration) df = 1.95

## Slide 132
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes
Reaction Limited,
Short persistence of velocity

## Slide 133
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 134
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 135
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/MeakinVoldSunderlandEdenWittenSanders.pdf
Vold-Sutherland Model particles with random linear trajectories are added to a growing cluster of particles at the position where they first contact the cluster
Eden Model particles are added at random with equal probability to any unoccupied site adjacent to one or more occupied sites
(Surface Fractals are Produced)
Witten-Sander Model particles with random Brownian trajectories are added to a growing cluster of particles at the position where they first contact the cluster
Sutherland Model pairs of particles are assembled into randomly oriented dimers. Dimers are coupled at random to construct tetramers, then octoamers etc. This is a step-growth process except that all reactions occur synchronously (monodisperse system).
In RLCA a “sticking probability is introduced in the random growth process of clusters. This increases the dimension.
In DLCA the “sticking probability is 1. Clusters follow random walk.

## Slide 136
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 137
Fractal Aggregates and Agglomerates
Aggregate growth
From DW Schaefer Class Notes

## Slide 138
Fractal Aggregates and Agglomerates
From DW Schaefer Class Notes
http://www.eng.uc.edu/~gbeaucag/PDFPapers/ks5024%20Japplcryst%20Beaucage%20PSD.pdf
Primary: Primary Particles
Secondary: Aggregates
Tertiary: Agglomerates
Primary: Primary Particles
Tertiary: Agglomerates

## Slide 139
Hierarchy of Polymer Chain Dynamics

## Slide 140
Dilute Solution Chain
Dynamics of the chain
The exponential term is the “response function”
response to a pulse perturbation

## Slide 141
Dilute Solution Chain
Dynamics of the chain
Damped Harmonic
Oscillator
For Brownian motion
of a harmonic bead in a solvent
this response function can be used to calculate the
time correlation function <x(t)x(0)>
for DLS for instance
τ is a relaxation time.

## Slide 142
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Beads 0 and N are special
For Beads 1 to N-1
For Bead 0 use R-1 = R0 and for bead N RN+1 = RN
This is called a closure relationship

## Slide 143
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
The Rouse unit size is arbitrary so we can make it very small and:
With dR/dt = 0 at i = 0 and N
Reflects the curvature of R in i,
it describes modes of vibration like on a guitar string

## Slide 144
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Describes modes of vibration like on a guitar string
For the “p’th” mode (0’th mode is the whole chain (string))

## Slide 145
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts
Relaxation time follows N2 (actually follows N3/df)
Diffusion constant follows 1/N (zeroth order mode is translation of the molecule) (actually follows N-1/df)
Both failings are due to hydrodynamic interactions (incomplete draining of coil)
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution

## Slide 146
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts
Relaxation time follows N2 (actually follows N3/df)
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution

## Slide 147
Hierarchy of Entangled Melts

## Slide 148
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/SukumaranScience.pdf
Chain dynamics in the melt can be described by a small set of “physically motivated, material-specific paramters”
Tube Diameter dT
Kuhn Length lK
Packing Length p
Hierarchy of Entangled Melts

## Slide 149
Quasi-elastic neutron scattering data demonstrating the existence of the tube
Unconstrained motion => S(q) goes to 0 at very long times
Each curve is for a different q = 1/size
At small size there are less constraints (within the tube)
At large sizes there is substantial constraint (the tube)
By extrapolation to high times
a size for the tube can be obtained
dT

## Slide 150
There are two regimes of hierarchy in time dependence
Small-scale unconstrained Rouse behavior
Large-scale tube behavior
We say that the tube follows a “primitive path”
This path can “relax” in time = Tube relaxation or Tube Renewal
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 151
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 152
Reptation predicts that the diffusion coefficient will follow N2 (Experimentally it follows N2)
Reptation has some experimental verification
Where it is not verified we understand that tube renewal is the main issue.
(Rouse Model predicts D ~ 1/N)

## Slide 153
Reptation of DNA in a concentrated solution

## Slide 154
Simulation of the tube

## Slide 155
Simulation of the tube

## Slide 156
Plateau Modulus
Not Dependent on N, Depends on T and concentration

## Slide 157
Kuhn Length- conformations of chains <R2> = lKL
Packing Length- length were polymers interpenetrate p = 1/(ρchain <R2>)
where ρchain is the number density of monomers

## Slide 158
this implies that dT ~ p

## Slide 163
McLeish/Milner/Read/Larsen Hierarchical Relaxation Model
http://www.engin.umich.edu/dept/che/research/larson/downloads/Hierarchical-3.0-manual.pdf

## Slide 164
Block Copolymers
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/BCP%20Section.pdf

## Slide 165
Block Copolymers
SBR Rubber

## Slide 166
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Amphiphilic.pdf

## Slide 167
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/BCP%20Modeling.pdf

## Slide 168
Hierarchy in BCP’s and Micellar Systems
We consider primary structure as the block nature of the polymer chain.
This is similar to hydrophobic and hydrophilic interactions in proteins.
These cause a secondary self-organization into rods/spheres/sheets.
A tertiary organizaiton of these secondary structures occurs.
There are some similarities to proteins but BCP’s are extremely simple systems by comparison.
Pluronics (PEO/PPO block copolymers)

## Slide 169
What is the size of a Block Copolymer Domain?
-For and symmetric A-B block copolymer
-Consider a lamellar structure with Φ = 1/2
-Layer thickness D in a cube of edge length L, surface energy σ
- so larger D means less surface and a lower Free Energy F.
-The polymer chain is stretched as D increases. The free energy of
a stretched chain as a function of the extension length D is given by
- where N is the degree of polymerization for A or B,
b is the step length per N unit, νc is the excluded volume for a unit step
So the stretching free energy, F, increases with D2.
-To minimize the free energies we have
Masao Doi, Introduction to Polymer Physics

## Slide 171
Chain Scaling (Long-Range Interactions)
Long-range interactions are interactions of chain units separated by such a
great index difference that we have no means to determine if they are from the same chain
other than following the chain over great distances to determine the connectivity. That is,
Orientation/continuity or polarity and other short range linking properties are completely lost.
Long-range interactions occur over short spatial distances (as do all interactions).
Consider chain scaling with no long-range interactions.
The chain is composed of a series of steps with no orientational relationship to each other.
So <R> = 0
<R2> has a value:
We assume no long range interactions so that the second term can be 0.