## Slide 1
General Descriptions
Overview
Physical description of an isolated polymer chain
Dimensionality and fractals
Short-range and long-range interactions
Packing length and tube diameter
Long-range interactions and chain scaling
Flory-Krigbaum theory
The semi-dilute and concentrated regimes
Blob theory (the tensile, concentration, and thermal blobs)
Coil collapse/protein folding
Analytic Techniques for Polymer Physics
Measurement of the size of a polymer chain
Rg, Rh, Reted
Small-angle neutron, x-ray scattering and static light scattering
Intrinsic viscosity
Dynamic light scattering
Polymer melt rheology
DSC/DMTA/TGA
Polymer Physics
10:10 – 11:05
Baldwin 757
Greg Beaucage
Prof. of Chemical and Materials Engineering
University of Cincinnati, Cincinnati OH
Rhodes 491
beaucag@uc.edu
https://www.eng.uc.edu/~beaucag/Classes/Properties.html
Zoom Meeting: https://us02web.zoom.us/j/87233679564?pwd=ak1XbmprdFBUQnRZOWszWU91VHdyUT09

## Slide 2
Polymers
http://www.eng.uc.edu/~gbeaucag/Classes/IntrotoPolySci/PolymerChemicalStructure.html

## Slide 3
http://www.eng.uc.edu/~gbeaucag/Classes/IntrotoPolySci/PolymerChemicalStructure.html
Polymers

## Slide 4
Polymers
http://www.eng.uc.edu/~gbeaucag/Classes/IntrotoPolySci/PolymerChemicalStructure.html
From Bird, Armstrong, Hassager, "Dynamics of Polymeric Liquids, Vol. 1"
Polymer Rheology

## Slide 5
Polymers
Paul Flory [1] states that "…perhaps the most significant structural characteristic of a long polymer chain… (is) its capacity to assume an enormous array of configurations."
1) Principles of Polymer Chemistry, Flory PJ, (1953).
ww.eng.uc.edu/~gbeaucag/Classes/IntrotoPolySci/WhatIsAPolymerPlastic.html
http://www.eng.uc.edu/~gbeaucag/Classes/IntrotoPolySci/MacroMolecularMaterials.html
http://www.eng.uc.edu/~beaucag/Classes/IntrotoPolySci/PicturesDNA.html
Which are Polymers?
http://www.eng.uc.edu/~beaucag/Classes/IntrotoPolySci/What Does Searching Configurational Space Mean for Polymers.html

## Slide 6
Random Walk Generator (Manias Penn State)
http://zeus.plmsc.psu.edu/~manias/MatSE443/Study/7.html
-Polymers do not have a discrete size, shape or conformation.
-Looking at a single simulation of a polymer chain is of no use.
-We need to consider average features.
-Every feature of a polymer is subject to a statistical description.
-Scattering is a useful technique to quantify a polymer since it describes structure from a statistically averaged perspective.
-Rheology is a major property of interest for processing and properties
-Simulation is useful to observe single chain behavior in a crowded environment etc.
http://e.sci.osaka-cu.ac.jp/yoshino/download/rw/

## Slide 7
Polymers

## Slide 8
Polymers
Fold surface energy ~ 2 e-5 J/cm2
Enthalpy of melting ~ 300 J/cm3
T∞ ~ 414K (141°C)
T ~ 110°C
t = 2sT∞/(DHm (T∞-T)) (Hoffman-Lauritzen)
~ 1.78e-6 cm or 17.8 nm thick crystals regardless of N

## Slide 9
Polymers
From J. R. Fried,
"Polymer Science and Technology"
From Bird, Armstrong, Hassager, "Dynamics of Polymeric Liquids Vol. 1"
Viscosity versus Rate of Strain
Zero Shear Rate Viscosity versus Molecular Weight
Specific Viscosity versus Concentration for Solutions

## Slide 10
Polymers
If polymers are defined by dynamics, why should we consider first statics?
Statistical Mechanics: Boltzmann (1896)
Statistical Thermodynamics: Maxwell, Gibbs (1902)
We consider the statistical average of a thermally determined structure, an equilibrated structure
Polymers are a material defined by dynamics and described by statistical thermodynamics
Newtonian Bulk Flow
Mesh or
Entanglement
Size
Power Law Fluid/Rubbery Plateau
Kuhn Length/Tube Diameter
Local Molecular Dynamics
G’ ~ w2
G” ~ w

## Slide 11
Polymers
Newtonian Bulk Flow
Mesh or
Entanglement
Size
Power Law Fluid/Rubbery Plateau
Kuhn Length
Local Molecular Dynamics

## Slide 12
Small Angle Neutron Scattering
The vector r ~ 2p/q

## Slide 13
The vector d ~ 2p/q
d = l/(2 sin q)
q = 4p/l sin q

## Slide 15
Synthetic Polymer Chain Structure
(A Statistical Hierarchy)

## Slide 16
Synthetic Polymer Chain Structure
(A Statistical Hierarchy)
Consider that all linear polymer chains can be reduced to a step length and a free, universal joint
This is the Kuhn Model, and the step length is called the Kuhn length, lK
This is extremely easy to simulate
Begin at the origin, (0,0,0)
Take a step in a random direction to (i, j, k)
Repeat for N steps
On average for a number of these “random walks” we will find that the final position tends towards (0,0,0) since there is no preference for direction in a “random” walk
The walk does have a breadth (standard deviation), i.e. depending on the number of steps, N, and the step length lK, the breadth of the walk will change.
lK just changes proportionally the scale of the walk so <R2>1/2 ~ lK
https://www.doitpoms.ac.uk/tlplib/polymerbasics/HTML5/Kuhn_randomwalk2.html

## Slide 17
Synthetic Polymer Chain Structure
(A Statistical Hierarchy)
The walk does have a breadth, i.e. depending on the number of steps, N, and the step length lK, the breadth of the walk will change.
lK just changes proportionally the scale of the walk so <R2>1/2 ~ lK
The chain is composed of a series of steps with no orientational relationship to each other.
So <R> = 0
<R2> has a value:
We assume no long-range interactions so that the second term can be 0.
<R2>1/2 ~ N1/2 lK
https://www.doitpoms.ac.uk/tlplib/polymerbasics/HTML5/Kuhn_randomwalk2.html

## Slide 18
Synthetic Polymer Chain Structure
(A Statistical Hierarchy)
<R2>1/2 ~ N1/2 lK
This function has the same origin as the function describing the root mean square distance of a diffusion pathway
<R2>1/2 ~ t1/2(2D)1/2
So, the Kuhn length bears some resemblance to the diffusion coefficient
And the random walk polymer chain bears some resemblance to Brownian Motion
The random chain is sometimes called a “Brownian Chain”, a drunken walk, a random walk, a Gaussian Coil or Gaussian Chain among other names.

## Slide 19
<R2>1/2 = n1/2 l
Concentration within a coil = n/(n3/2 l3) ~ n-1/2 = c* overlap concentration
Below c* ~ 1 mg/ml dilute conditions (most analytic measurements), Above c* “semi-dilute”
Below c*, dilute scattering curve; above c*;
the scattering is screened in the semi-dilute regime;
when screening/mesh size matches the persistence length we reach the concentrated regime or the melt

## Slide 20
<R2>1/2 = n1/2 l
Concentration within a coil = n/(n3/2 l3) ~ n-1/2 = c* overlap concentration
Below c* ~ 1 mg/ml dilute conditions (most analytic measurements), Above c* “semi-dilute”
Below c*, dilute scattering curve; above c*;
the scattering is screened in the semi-dilute regime;
when screening/mesh size matches the persistence length we reach the concentrated regime or the melt
Rheology view linear below c*, c* and entanglement concentration might be similar

## Slide 21
Random Walk Generator (Manias Penn State)
http://zeus.plmsc. http://e.sci.osaka-cu.ac.jp/yoshino/download/rw/psu.edu/~manias/MatSE443/Study/7.html
-Polymers do not have a discrete size, shape or conformation.
-Looking at a single simulation of a polymer chain is of no use.
-We need to consider average features.
-Every feature of a polymer is subject to a statistical description.
-Scattering is a useful technique to quantify a polymer since it
describes structure from a statistically averaged perspective.
http://e.sci.osaka-cu.ac.jp/yoshino/download/rw/
https://www.doitpoms.ac.uk/tlplib/polymerbasics/HTML5/Kuhn_randomwalk2.html

## Slide 22
Worm-like Chain
Freely Jointed Chain
Freely Rotating Chain
Rotational Isomeric State Model Chain (RISM)
Persistent Chain
Kuhn Chain
These refer to the local state of the polymer chain.
Generally, the chain is composed of chemical bonds
that are directional, that is they are rods connected at their ends.
These chemical steps combine to make an effective
rod-like base unit, the persistence length,
for any synthetic polymer chain (this is larger than the chemical step).
The persistence length can be measured in scattering
or can be inferred from rheology through the Kuhn length
lK = 2 lP
The Primary Structure for Synthetic Polymers

## Slide 23
Small Angle Neutron Scattering

## Slide 24
The vector r ~ 2p/q
d = l/(2 sin q)
q = 4p/l sin q

## Slide 25
The Primary Structure for Synthetic Polymers

## Slide 26
The synthetic polymer is composed of linear bonds, covalent or ionic bonds have a direction.
Coupling these bonds into a chain involves some amount of memory of this direction for each coupled bond.
Cumulatively this leads to a persistence length that is longer than an individual bond.
Observation of a persistence length requires that the persistence length is much larger than the diameter of the chain. Persistence can be observed for worm-like micelles, synthetic polymers, DNA but not for chain aggregates of nanoparticles, strings or fibers where the diameter is on the order of the persistence length.
https://www.eng.uc.edu/~beaucag/Classes/IntrotoPolySci/PicturesDNA.html

## Slide 27
The Gaussian Chain
Gaussian chain is based on Brownian walk or Brownian motion that was described mathematically by Einstein in a 1905 paper
For particles (or a particle) subject to thermal, diffusive motion initially at a fixed position, the density of the particles is a function of time and space. These dependencies can be expressed as Taylor series expansions. For simplicity consider a one-dimensional space (though this can be worked out in any dimensional space). Particles have an equal probability of moving to the left or to the right. The motion is symmetric about the zero point. The dependence with time, in contrast, is in only one direction. (This, it turns out, is the essence of Brownian motion as compared to ballistic motion where both space and time move in only one direction.)
PG(Dx) is a normalized, symmetric probability distribution where Dx is the change in x from 0. The integral of PG(Dx) is 1 since it is normalized. The integral of is zero since it it symmetric.
with

## Slide 28
The Gaussian Chain
For N particles starting at x = 0 and time = 0,
First moment in space is 0, second moment (variance of Gaussian) is:
= 2Dt
For polymer chain <R2> = lK2 N

## Slide 29
The Einstein-Stokes Equation/Fluctuation Dissipation Theorem
Consider a particle in a field which sets up a gradient mitigated by thermal diffusion such as sedimentation of particles in the gravitational field.
The velocity of the particles due to gravity is vg = mg/(6phRh) following Stokes Law. For particles at x = 0 and x=h height, the density difference is governed by a Boltzmann probability function,
Fick’s law gives the flux of particles, J = -D dr/dh, and J = rv, so v = -(D/r) dr/dh, and dr/dh = -r0mg/(kT) e-mgh/kT = -rmg/(kT). Then, v = Dmg/(kT). At equilibrium this speed equals the gravitational speed, vg = mg/(6phRh). Equating the two removes the details of the field, making a universal expression for any particle in any field, the Stokes-Einstein equation based on the Fluctuation Dissipation Theorem. (This was done in 1-d, the same applies in 3d.)
The latter expression was used to determine Avagadro’s number from colloidal particles that could be counted. NA was then applied to molecular species to determine, for the first time, the molecular weight.

## Slide 30
The Einstein-Stokes Equation/Fluctuation Dissipation Theorem
For a particle in a field the velocity can be calculated from Fick’s First Law
or from a balance of acceleration and drag forces
vg = mg/6pRhh = -D/r dr/dh = Dmg/kT
This yields the Einstein-Stokes Equation D = kT/6pRhh

## Slide 31
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End-to-End Distance R
By Comparison, The Energy to stretch a Thermally Equilibrated Chain Can be Written

## Slide 32
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End-to-End Distance R
By Comparison, The Energy to stretch a Thermally Equilibrated Chain Can be Written
Force
Force
Assumptions:
-Gaussian Chain
-Thermally Equilibrated
-Small Perturbation of Structure (so it is still Gaussian after the deformation)

## Slide 33
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End-to-End Distance R
Use of P(R) to Calculate Moments:
Mean is the 1’st Moment:

## Slide 34
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End-to-End Distance R
Use of P(R) to Calculate Moments:
Mean is the 1’st Moment:
This is a consequence of symmetry of the Gaussian function about 0.

## Slide 35
The Gaussian Chain
Boltzman Probability
For a Thermally Equilibrated System
Gaussian Probability
For a Chain of End-to-End Distance R
Use of P(R) to Calculate Moments:
Mean Square is the 2’ndMoment:

## Slide 36
The Gaussian Chain
Gaussian Probability
For a Chain of End-to-End Distance R
Mean Square is the 2’nd Moment:
There is a problem to solve this integral since we can solve an integral of the form k exp(kR) dR
R exp(kR2) dR but not R2 exp(kR2) dR
There is a trick to solve this integral that is of importance to polymer science and to other random systems that follow the Gaussian distribution.

## Slide 37
http://www.eng.uc.edu/~gbeaucag/Classes/Properties/GaussianProbabilityFunctionforEnd.pdf

## Slide 38
The Gaussian Chain
Gaussian Probability
For a Chain of End-to-End Distance R
Mean Square is the 2’nd Moment:
So, the Gaussian function for a polymer coil is:

## Slide 39
The Gaussian Chain
Means that the coil size scales with n1/2
Or
Mass ~ n ~ Size2
Generally, we say that
Mass ~ Sizedf
Where df is the mass fractal dimension
A Gaussian Chain is a kind of 2-dimensional object like a disk.

## Slide 40
The Gaussian Chain
A Gaussian Chain is a kind of 2-dimensional object like a disk.
The difference between a Gaussian Chain and a disk lies in other dimensions of the two objects.
Consider an electric current flowing through the chain, it must follow a path of n steps. For a disk the current follows a path of n1/2 steps since it can short circuit across the disk. If we call this short circuit path p we have defined a connectivity dimension c such that:
pc ~ n
And c has a value of 1 for a linear chain and 2 for a disk

## Slide 41
The Gaussian Chain
A Gaussian Chain is a kind of 2-dimensional object like a disk.
A linear Gaussian Chain has a connectivity dimension of 1 while the disk has a connectivity dimension of 2.
The minimum path p is a fractal object and has a dimension, dmin so that,
p ~ Rdmin
For a Gaussian Chain dmin = 2 since p is the path n
For a disk dmin = 1 since the short circuit is a straight line.
We find that df = c dmin
There are other scaling dimensions, but they can all be related to two independent structural scaling dimensions such as c and dmin
or dmin and df

## Slide 42
Disk
Random Coil
Extended β-sheet
(misfolded protein)
Unfolded Gaussian chain

## Slide 43
Tortuosity
Connectivity
How Complex Mass Fractal Structures
Can be Decomposed
z
df
p
dmin
s
c
R/d
27
1.36
12
1.03
22
1.28
11.2

## Slide 44
Fibers follow either Gaussian or Self-avoiding structure depending on binding of fibers
Orientation partly governs separation
Pore size and fractal structure govern wicking

## Slide 45
The persistence length is created due to interactions between
units of the chain that have similar chain indices
These interactions are termed “short-range interactions” because they
involve short distances along the chain minimum path
Short-range interactions lead to changes in the chain persistence. For example,
restrictions to bond rotation such as by the addition of short branches can lead to increases
in the persistence length in polymers like polyethylene. Short-range interactions can be
more subtle. For instance, short branches in a polyester can disrupt a natural tendency to
form a helix leading to a reduction in the persistence length, that is making the chain more
flexible.
All interactions occur over short spatial distances, short-range interactions occur over
short-distances but the distinguishing feature is that they occur over short differences in
chain index.
Short-range interactions do not have an effect on the chain scaling.
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 46
Consider the simplest form of short-range interaction
We forbid the chain from the preceding step
Consider a chain as a series of steps ri
ri is a vector of length r and there are n such vectors in the chain
The mean value for ri+1 is 0
bk is a unit vector in a coordinate system,
6 of these vectors in a cubic system
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 47
For exclusion of the previous step this sum does not equal 0
so
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 48
For Gaussian Chain
yields
For SRI Chain the first term is not 0.
and
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
For Cartesian simulation z = 6 and beff is 1.22 b so about a 25% increase for one step self-avoidance.
Short-Range Interactions
The Primary Structure for Synthetic Polymers
See slide 68

## Slide 49
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
Short-Range Interactions
Increase the persistence length
Chain scaling is not affected by short-range interactions.
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 50
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
-Steric interactions
-Tacticity
-Charge (poly electrolytes)
-Hydrogen bonds
-Helicity
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 51
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
Characteristic Ratio, C∞
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 52
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
The Characteristic Ratio varies with N due to chain end effects. There is generally an increase in C with N and it plateaus at high molecular weight.
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 53
LD = Low branch density
HD = High branch density
Molecular weight dependence of persistence length
This is a 5 parameter model for persistence length!
(used to model 5 or 6 data points!!!)
nb = backbone length

## Slide 54
Molecular weight dependence of persistence length
This is a 5-parameter model for persistence length!
(used to model 5 or 6 data points!!!)
(Also, this model fails to predict an infinite molecular weight
persistence length.)

## Slide 55
LD = Low branch density
HD = High branch density
Molecular weight dependence of persistence length
Proposed End Group Functionality

## Slide 56
Proposed End Group Functionality
This works better for Yethiraj’s data.
(Except that the infinite persistence length is not monotonic in branch length)

## Slide 57
Persistence Length ~ Bending Modulus/(Thermal Energy)
lp = lK/2 ~ Ebending/kT
(We will derive this later with respect to the persistent chain Colby/Rubenstein pp. 58)
Motion of the end-groups is proportional to thermal energy and reduces the persistence length
The energy is related to the flexibility of the chain not the stiffness, 1/lp, so we should consider 1/lp as the parameter of interest in terms of an end group effect not lp

## Slide 58
Alternative Functionality
based on increase in chain flexibility

## Slide 59
Alternative Functionality
based on increase in chain flexibility

## Slide 60
LD = Low branch density
HD = High branch density
Alternative Functionality
based on increase in chain flexibility

## Slide 61
LD = Low branch density (0.5 branch per chain unit)
HD = High branch density (1 branch per chain unit)
Alternative Functionality
based on increase in chain flexibility
Equation fails at low nb since it predicts lp => 0 when nb => 0
Fit Parameters versus branch density

## Slide 62
Alternative Functionality
based on increase in chain flexibility
Equation fails at low nb since it predicts lp => 0 when nb => 0

## Slide 63
Alternative Functionality
based on increase in chain flexibility
Equation fails at low nb since it predicts lp => when nb => 0

## Slide 64
Alternative Functionality
based on increase in chain flexibility
The 2K values imply that end groups become less important for more rigid chains

## Slide 65
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
-Steric interactions
-Tacticity
-Charge (poly electrolytes)
-Hydrogen bonds
-Helicity
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 66
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
http://cbp.tnw.utwente.nl/PolymeerDictaat/node4.html
Polyethylene
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 67
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
Butane
Ethane
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 68
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
Characteristic Ratio, C∞
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 69
http://www.eng.uc.edu/~gbeaucag/Classes/Physics/Chapter1.pdf
What kinds of short-range interactions can we expect
-Bond angle restriction
-Bond rotation restriction
Consider a freely rotating chain that has a bond angle restriction of 109.5 °
Short-Range Interactions
The Primary Structure for Synthetic Polymers
Ising Chain Model in Colby/Rubenstein, pp. 59

## Slide 70
Consider a freely rotating chain that has a bond angle restriction of 109.5 ° = τ
C
C
C
109.5°
θ
Short-Range Interactions
The Primary Structure for Synthetic Polymers
Ising Model
See slide 46

## Slide 71
Consider a freely rotating chain that has a bond angle restriction of 109.5 ° = τ
For a Freely Rotating Polyethylene Chain
http://books.google.com/books?id=Iem3fC7XdnkC&pg=PA23&lpg=PA23&dq=coil+expansion+factor&source=bl&ots=BGjRfhZYaU&sig=I0OPb2VRuf8Dm8qnrmrhyjXyEC8&hl=en&sa=X&ei=fSV0T-XqMMHW0QHi1-T_Ag&ved=0CF0Q6AEwBw#v=onepage&q=coil%20expansion%20factor&f=false
Moderate Flexibility
High Rotational Flexibility
Lower Rot. Flexibility
Bond angles 109.5°: 104.5°
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 72
Consider a freely rotating chain that has a bond angle restriction of 109.5 ° = τ
http://books.google.com/books?id=Iem3fC7XdnkC&pg=PA23&lpg=PA23&dq=coil+expansion+factor&source=bl&ots=BGjRfhZYaU&sig=I0OPb2VRuf8Dm8qnrmrhyjXyEC8&hl=en&sa=X&ei=fSV0T-XqMMHW0QHi1-T_Ag&ved=0CF0Q6AEwBw#v=onepage&q=coil%20expansion%20factor&f=false
If we consider restrictions to bond rotation for first order interactions
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 73
Alexei Khokhlov in Soft and Fragile Matter (2000)
Contour length per monomer is 2 * bond length
Short-Range Interactions
The Primary Structure for Synthetic Polymers

## Slide 74
From Colby/Rubeinstein pp. 66

## Slide 75
The Primary Structure for Synthetic Polymers

## Slide 76
Linear absorption
dI = -I a dx change is linear in intensity
dl/l = - a dx integrate
ln(I/I0) = - ax or
I = I0 exp(-ax)

## Slide 77
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Persistence/Persistence.html

## Slide 79
From Strobl p. 57

## Slide 80
Scattering Observation of the Persistence Length
A power-law decay of -1 slope has only one structural interpretation.
The Primary Structure for Synthetic Polymers
θ

## Slide 81
Scattering Observation of the Persistence Length
A power-law decay of -1 slope has only one structural interpretation.
The Primary Structure for Synthetic Polymers
θ

## Slide 82: Electric Double Layers
Helmholtz (100+ years ago) proposed that surface charge is balanced by a layer of oppositely charged ions.
COUNTER IONS
+
+
+
+
-
-
-
+
-
CO IONS
HOP
Helmholtz Outer Plane
-
-
-
-
SOLVENT MOLECULES
Φ0
x
Surface Potential
+
All colloids should flocculate.
Dale Schaefer Slides 2010
Notes: All colloids should flocculate

## Slide 83: Zeta (ζ) Potential (Electric potential at the slipping (shear) plane)
Stern Plane (δ)
Φsurface
Φ = electrostatic potential (Volt = J/coulomb)
Gouy/Chapman diffuse double layer + layer of adsorbed charge.
-
-
-
-
-
-
-
+
+
+
+
+
Shear Plane
Diffuse layer
+
-
-
+
-
Bulk Solution
-
-
Φstern
x
ζ
-
-
+
+
Dale Schaefer Slides 2010
Notes: The unit of electrostatic potential is the volt (V), and 1 V = 1 J/C = 1 Nm/C. Equation (25.4) shows that as the unit of the electric field we can also use V/m. A common used unit for the energy of a particle is the electron-volt (eV) which is defined as the change in kinetic energy of an electron that travels over a potential difference of 1 V. The electron-volt can be related to the Joule via eq.(25.3). Equation (25.3) shows that the change in energy of an electron when it crosses over a 1 V potential difference is equal to 1.6 . 10-19 J and we thus conclude that 1 eV = 1.6 . 10-19 J

## Slide 85: Debye-Hückel approximation for Φ(x)
Gouy-Chapman Model
+
+
+
+
+
+
-
-
-
+
-
-
-
Exponential
function
x
Φ
Dale Schaefer Slides 2010
Potential is stronger than kT
Counter ions (n0) screen the charge

## Slide 86
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Persistence/Persistence.html
Polyelectrolytes (proteins, charged polymers (sulfonated polystyrene), polyacrylic acid, polyethylene oxide, polypropylene oxide, poly nucleic acids, etc.)
Strongly charged polyelectrolytes = each monomer unit is charged
Weakly charged polyelectrolytes = some monomers are charged
This can depend on the counter ion concentration
For SCPE the electrostatic persistence length dominates, for WCPE there is a competition between Coulombic and non-electrostatic persistence.
Debye-Hückel Potential (U(r)) between two charges (e) separated by a distance r,
rD is the Debye screening length, n is the counter ion (salt) concentration, rD determines how quickly the electrostatic potential decays
Soft and Fragile Matter, M. E. Cates, M.R. Evans Chapter 3 Alexi Khokhlov (2000); Chines review of polyelectrolytes from web
SCPE WCPE

## Slide 87
Consider two isolated charges subject to thermal motion at kT
The energy associated with the charge attraction/repulsion
is equal to the thermal energy, kT, at the Bjerrum length, lB.
https://ocw.mit.edu/courses/chemical-engineering/10-626-electrochemical-energy-systems-spring-2014/study-materials/MIT10_626S14_S11lec28.pdf
In water at room temperature lB ~ 7 Å
Below the Bjerrum length charges will feel specific interactions and will form ordered structures. Above lB, charges feel a ”mean field” and do not form ordered structures but can still feel repulsive and attractive forces.
You hear the report of a gun but can’t tell its location, so you take cover, you are beyond its Bjerrum length. You hear the report of the gun and run in the opposite direction; you are within its Bjerrum length.
Distances where a mean field is felt.
Thermal diffusion/Brownian motion takes over
Potential is similar to kT

## Slide 88
https://ocw.mit.edu/courses/chemical-engineering/10-626-electrochemical-energy-systems-spring-2014/study-materials/MIT10_626S14_S11lec28.pdf
Hard
Core
Mean
Field

## Slide 89
Debye length is the distance where kT random motion balances the U(r) potential in the presence of n counter ion density
For Charges separated by distance r in the presence of n = number/volume counter ions or other charges
Below the Debye screening length charges will feel interactions, either specific if r < lB and or mean field if r > lB . Above lD, charges do not feel interactions at all, they act as uncharged species.
Distances where charges are not felt at all.
You hear the report of a gun but can’t tell its location so you take cover, you are beyond its Bjerrum length but within its Debye screening length. You can’t hear the gun due to too many other guns firing closer to you, you are beyond its Debye screening length.

## Slide 90
Charge spacing, a
Counterion
concentration, n
Counterion
condensation
Polymeric
contribution
to screening
Micelles, liquid-
crystalline phases

## Slide 91
-Electrostatic Persistence Length
Persistence is increased by electrostatic charge. lper = lo + le
For a << lper<< rD
Interaction between charges separated by distance less than rD, short range repulsion increases persistence length (short-range interactions)
Interaction between charges separated by a distance > lper effect chain scaling (long-range interactions)
A new size scale is introduced: Charge spacing “a” which contributes an electrostatic persistence length, le
Increase in persistence length due to charges on chain

## Slide 92
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Persistence/Persistence.html
-Counterion Condensation
A counter ion has translational entropy that drives it away from a chain of charged monomers
V2 and V1 are the initial and final cylinders
A counter ion has an enthalpy that attracts it to a chain of charged monomers (a = distance of charge separation on chain)
Balancing these two we have the parameter u,
u < 1 entropy is favored, and counter ions move out (disperse into solution),
u > 1 enthalpy favored and counter ions move in (condense on chain)
Counter ions condense until the chain charge is neutralized, when
ρeff is the final chain charge and condensed counter ion charge
Soft and Fragile Matter, M. E. Cates, M.R. Evans Chapter 3 Alexi Khokhlov (2000); Chines review of polyelectrolytes from web
Ideal gas
dU = -pdV (for dQ = 0)
dU = -RT(dV/V)
U = -RTln(V2/V1)
D-H Potential
dU = -e2/ea dr/r
U = -er/e (ln(r2/r1))
U = -er/2e (ln(V2/V1))

## Slide 93
Condensing counterions to neutralize charge on the chain
This removes counterions from the solution so that there is less Debye screening

## Slide 95
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/Persistence/Persistence.html
Polyelectrolytes (proteins, charged polymers, polyethylene oxide, polypropylene oxide, poly nucleic acids, etc.)
-Electrostatic Persistence Length
Persistence is increased by electrostatic charge. lper = lo + le
For a << lper<< rD
Interaction between charges separated by distance less than rD, short range repulsion increases persistence length
Interaction between charges separated by a distance > lper effect chain scaling
When charge condensation stops since all charge on the chain is neutralized
and a maximum effective linear charge density is reached
Soft and Fragile Matter, M. E. Cates, M.R. Evans Chapter 3 Alexi Khokhlov (2000); Chines review of polyelectrolytes from web

## Slide 96
Summary of Polyelectrolyte Persistence Length
3 size scales are important,
“a” spacing of charge groups on the chain
rD or κ-1 Debye Screening length
lp,0 bare persistence length with no charge
“a” must be smaller than rD for there to be a change in persistence, this is so that neighboring charges can interact
rD must be smaller than lp,0 for there to be a change in persistence
The parameter “u” enthalpy of attraction divided by T*entropy of dispersion of charge governs u>1 charge condense; u<1 charges disperse

## Slide 98
Dobrynin AV Macro. 38 9304 (2005)

## Slide 99: Other measures of Local Structure
Kuhn Length, Persistence Length: Static measure of step size
Tube Diameter: Dynamic measure of chain lateral size
Packing Length: Combination of static and dynamic measure of local structure

## Slide 100
http://www.eng.uc.edu/~gbeaucag/Classes/MorphologyofComplexMaterials/SukumaranScience.pdf
Chain dynamics in the melt can be described by a small set of “physically motivated, material-specific parameters”
Tube Diameter dT
Kuhn Length lK
Packing Length p
Packing Length and Tube Diameter
Larson Review of Tube Model for Rheology

## Slide 101
Larson Review of Tube Model for Rheology

## Slide 102
Quasi-elastic neutron scattering data demonstrating the existence of the tube
Unconstrained motion => S(q) goes to 0 at very long times
Each curve is for a different q = 1/size
At small size there are less constraints (within the tube)
At large sizes there is substantial constraint (the tube)
By extrapolation to high times
a size for the tube can be obtained
dT
Strobel Chapter 8
u reflects Rouse behavior. In plots versus u, deviations from ideal Rouse Behavior indicate tube constraints.

## Slide 103
Julia Higgins Review Article (2016)

## Slide 104
There are two regimes of hierarchy in time dependence
Small-scale unconstrained Rouse behavior
Large-scale tube behavior
We say that the tube follows a “primitive path”
This path can “relax” in time = Tube relaxation or Tube Renewal
A model called Tube Dilation also exists to describe deviations between the tube model and experiment
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 105
Without tube renewal the Reptation model predicts that viscosity follows N3 (observed is N3.4)

## Slide 106
Reptation predicts that the diffusion coefficient will follow N2 (Experimentally it follows N2)
Reptation has some experimental verification
Where it is not verified, we understand that tube renewal is the main issue.
(Rouse Model predicts D ~ 1/N)
Fick’s Second Law

## Slide 107
Reptation of DNA in a concentrated solution

## Slide 108
Simulation of the tube

## Slide 109
Simulation of the tube

## Slide 110
Origin of the Packing Length:
Contemporary Topics in Polym. Sci. Vol. 6 Multiphase Macromolecular Systems, Culbertson BM Ed.
Theory of Stress Distribution in Block Copolymer Microdomains, Witten TA, Milner ST, Wang Z-G p. 656
Consider a di-block copolymer domain interface
(and blends with homopolymers as a compatibilizer)
http://pubs.rsc.org/en/content/articlehtml/2012/cs/c2cs35115c
Packing Length

## Slide 111
http://pubs.rsc.org/en/content/articlehtml/2012/cs/c2cs35115c

## Slide 112
Free Energy Contributions:
Interfacial Energy Proportional to the Total Surface Area
(makes domains larger to reduce surface area; χ is the average energy per kT per mer unit in a mixture of A and B)
One Chain Interfacial Energy = χkT(Adt)/Vc
dt is the thickness of the interfacial layer where the A-B junction is located
A is the cross-sectional area of a polymer chain
Vc is the occupied volume of a unit segment of a polymer chain
The total occupied volume of a block copolymer chain is Voccupied = NAB Vc;
This occupied volume is also given by Voccupied = dAB A where dAB is the length of the block copolymer chain assuming it forms a cylindrical shaped object and the block copolymer domain spacing. So, dAB = NABVc /A.
Energy of Elongation of Polymer Chains, Elastic Energy
(makes domains smaller, 3kTR2/(2nl2))
Assumes that one end is at the interface and the other end must fill the space.
Chain Energy of Elongation = -3kT dAB2/(2<R2>) = -3kT NABVc2/(lK2A2)
dAB = NAB Vc/A from above and <R2> = NABlK2
The free energy will be minimized in A to obtain the optimum phase size dAB. So, it is the packing of the chains at the interface that governs the phase behavior of BCP’s.
ΔG/kT = χAdt/Vc - 3 NABVc2/(2(lKA) 2
d(ΔG/kT)/dA = χdt/Vc + 3 NABVc2/(lK2A3) = 0
A = {3 NABVc3/(lK2χdt)}1/3
dAB = NAB Vc/A = NAB2/3/(3lK2χdt) 1/3 This is verified by experiment (Hashimoto papers)
dAB

## Slide 113
A is the cross-sectional area of a polymer chain
Vc is the occupied volume of a unit segment of a polymer chain
Voccupied = NAB Vc The total occupied volume of a block copolymer chain
Witten defines the term “a” that he calls the intrinsic elasticity of a polymer chain
Elastic Energy/(3kT) = a <R2>/(2Voccupied) where a =Voccupied/<R02> = Voccupied/(NK lK2)
(Previously we had the spring constant kspr/kT = 3/<R02> = 3a/Voccupied; a = kspr Voccupied/3)
“a” has units of length and is termed by Witten the “packing length” since it relates to the packing or occupied volume for a chain unit, Voccupied. “a” is a ratio between the packing volume and the molar mass as measured by <R02>.
Since Voccupied = NK Vc, and <R02> = NK lK2, then a = Vc/lK2, so the packing length relates to the lateral occupied size of a Kuhn unit, the lateral distance to the next chain. This is a kind of “mesh size” for the polymer melt. The cross-sectional area, A, is defined by “a”, A = πa2, and Vc = a lK2, so the BCP phase size problem can be solved using only the parameter “a”.
Three terms arise from the consideration of microphase separation
Contemporary Topics in Polym. Sci. Vol. 6 Multiphase Macromolecular Systems, Culbertson BM Ed.
Theory of Stress Distribution in Block Copolymer Microdomains, Witten TA, Milner ST, Wang Z-G p. 656

## Slide 114
Other uses for the packing length
The packing length is a fundamental parameter for calculation of dynamics for a polymer melt or concentrated solution.
Plateau modulus of a polymer melt G0 ~ 0.39 kT/a3
Structural Control of “a”
a = m0/(ρ lK l0)
Vary mass per chain length, m0/l0
Contemporary Topics in Polym. Sci. Vol. 6 Multiphase Macromolecular Systems, Culbertson BM Ed.
Theory of Stress Distribution in Block Copolymer Microdomains, Witten TA, Milner ST, Wang Z-G p. 656
Lin, Y-H Macro. 20 3080 (1987)
Lohse DT J. Macromol. Sci. Part C Polym. Rev. 45 298 (2005).

## Slide 115
Low Frequency G’ ~ ω2
From definition of viscoelastic
High Frequency G’ ~ ω1/2
From Rouse Theory for Tg
Plateau follows rubber elasticity
G’ ~ 3kT/(NK,e lK2)
Strobl, Physics of Polymers

## Slide 116
Plateau Modulus
Not Dependent on N, Depends on T and concentration

## Slide 117
this implies that dT ~ p

## Slide 118
Kuhn Length- conformations of chains <R2> = lKL
Packing Length- length where polymers interpenetrate p = 1/(ρchain <R2>)
where ρchain is the number density of monomers

## Slide 119
“Packing Length” Anywhere Web of Science

## Slide 120
“Packing Length” Anywhere Web of Science

## Slide 121
Structure and linear viscoelasticity of flexible polymer solutions: comparison of polyelectrolyte and neutral polymer solutions R. Colby, Rheo. Acta 49 425-442 (2010)

## Slide 122
Summary