Cast Film Quiz

- Based on the work by Kanai, describe how film thickness, temperature, and localized velocity change with respect to distance away from the die.

- Holding all other variables constant how would the change in temperature relative to distance from the die (dT/dz) change with an increase in polymer density?  Explain this observation in thermodynamic terms (H).  What process conditions would have to change to obtain the same final film temperature with the higher density film?

- Holding all other variables constant how would a change in shear viscosity effect the stress in the machine direction?  How would this be detected in a commercial process?

- With all other parameters held constant, which would have a higher cooling rate between the die lip and the chill roll, a clear polymer film or a polymer film that has been heavily loaded with carbon black?  Why?

- Would a faster quench rate improve or worsen the clarity of the film?  How is this done commercially?  You may need to visit the crystallization web page to fully answer this question.