### Avrami model for crystallization kinetics

Phillips review paper.

### Thermodynamic model of lamella formation

This section is dedicated to giving the reader some insight into the molecular and thermodynamic process involved in the nucleation and growth of a polymer crystal.  Much effort has been spent by many researchers in this field (including, but not limited to Flory, Bassett, Mendelkern, Strobl, Crist, Phillips, Hsiao, etc.) with still much debate over the exact mechanism of crystallization.  The traditional thoughts regarding the crystallization process involve the epitaxial growth of a polymer crystal in the form of a lamella.  This model will be the one we present (from a thermodynamic aspect) and has been the long accepted means of crystallization.  Recent work (REFERENCES) propose a different mechanism, similar to an ordered amorphous pre-crystal phase that is represented by the emergence of a SAXS peak prior to a WAXS peak that is observed in in-situ synchrotron scattering experiments.  Regardless of the mechanism, several consistencies have been observed for the dynamics of crystallization, which include:

- Polymer crystals are usually thin and lamellar when crystallized from either dilute solution or a melt.

- Lamellar thickness is proportional to the reciprocal of the difference between the “equilibrium” melting temperature of a crystal with no surface area (T0M) and the process temperature (T).

- Chain folding occurs in crystallization from both solution and melt.

- The growth rates of the polymer crystals are strongly dependent upon the crystallization temperature and the molar mass of the polymer.

A thermodynamic approach to lamella formation

This section will present the thermodynamic argument for the formation of a nucleation site and the growth of a lamella.

The most widely accepted approach to crystallization involves a kinetic perspective that has been modified from the theory of crystallization for small molecules.  The crystallization process is divided into two sections, nucleation and growth, with the Gibbs free energy serving as the key parameter for explaining both aspects.  As we recall from the thermodynamics section, the Gibbs free energy is given by:

ΔG=ΔH−TΔS

The traditional vision of the nucleation step involves the close packing of a few molecules to form a small, cylindrical embryo.  Such a process involves an increase in the Gibbs free energy since the formation of a crystal results in an increase in the overall energy due to the presence of surfaces (surface energy).  A competing effect, the incorporation of molecules into the embryo, causes the Gibbs free energy to decrease.  It's the battle between these two competing forces that controls the kinetics of nucleation.  The following figure represents the relationship between the change in the Gibbs free energy for the nucleation process relative to embryo size.

INSERT FIG 4.27 P. 282 FROM Y&L

When the embryo is small, the surface area to volume ratio of the embryo is large, resulting in a larger Gibbs free energy cause by the surface energy of the embryo.  The process then reaches a point where a critical embryo size is reached, and the Gibbs free energy begins to decrease as a result of the incorporation of more molecules into the embryo (thus reducing the surface to volume ratio).  Once this critical size is reached, the molecule will grow spontaneously.  Eventually, the embryo will reach a size where it becomes stable and the Gibbs free energy is less than that of the melt.  The peak in the above figure is an energy barrier that must be overcome to have stable nuclei.  It is envisioned that at the crystallization temperature, there is enough thermal energy for this barrier to be overcome.

A key issue with comparing the nucleation of small molecules and polymers are the geometries of the embryos.  In its simplest form, the previous discussion of nucleation can be applied to a spherical entity, where asymmetries and variations in surface energies can be neglected.  Polymer scientists are unfortunate in that they can not ignore such issues.  The theories of polymer crystallization envisage the growth taking place via a secondary nucleation process from the face of a pre-existing crystal surface.  The following figure shows such a process:

INSERT FIG4.28 P283 Y&L

The new polymer crystals add to a molecularly smooth surface, which is similar to the previously discussed primary nucleation process, but differs in that less surface area per volume is created.  This mean the energy barrier is lower for this type of process.  This secondary nucleation process can be described in a series of steps:

- a molecular strand lays down on an otherwise smooth crystal surface

- for freely rotating, flexible molecules*, further segments are subsequently added via the chain folding process

*rigid molecules for extended chains

The energies associated with this process include the surface energy of the folds (e), the surface energy of the lateral surface (s), and the free energy change of crystallization per unit volume (Gv).

The increase in surface free energy involved in laying down n adjacent molecular strands of length l is:

ΔGn=2blγs+2nabγe

Where the cross section of the strand is a*b.

Combating this increase in G from the additional surface energy is the reduction in G due to the incorporation of molecular strands in the crystal, given by:

ΔGn=−nablΔGv

Balancing these two equations gives:

ΔGn=2blγs+2nabγe−nablΔGv

At this point, we have an expression that gives the overall change in Gibbs free energy when n strands are laid down on a molecularly smooth surface.

The next step is to determine the free energy change upon crystallization per unit volume (Gv).  To do so, we recall our relationship between the Gibbs free energy and the enthalpy, temperature, and entropy of a system from thermodynamics.  First, we assume that the polymer crystal has an equilibrium melting temperature (T0M), which is the temperature at which a crystal without any surface area melts (i.e. the melting temperature of a “perfect” crystal).  We can then state:

ΔGv=ΔHv−TΔSv

Where Hv and Sv are the enthalpy and entropy of fusion per unit volume.

At T0M, there is no change in the Gibbs free energy since melting and crystallization are equally probable, so Gv is equal to zero at this temperature, resulting in:

ΔSv=ΔHvTm0

When crystallization occurs below this equilibrium melting temperature, we can approximate Gv by substituting the above expression for Sv into the general equation for the Gibbs free energy, giving:

ΔGv=ΔHv−TΔHvTm0

We are typically interested in the degree of undercooling, which is defined as:

ΔT=Tm0−T

Which upon substitution gives:

ΔGv=ΔTΔHvTm0

Substitution this equation into the overall Gibbs free energy equation previously derived, and simplifying by stating that 2bss is relatively small compared to the other components in the equation, we derive a relationship between the lamella thickness and the undercooling:

l≈2γeTm0ΔTΔHv

This relationship (also known as the Hoffman equation) shows that large supercooling results in thinner lamellae.